FLORIDA INTERNATIONAL UNIVERSITY

Miami, Florida

STRUCTURAL CHARACTERIZATION OF METAL HYDRIDES

FOR ENERGY APPLICATIONS

A dissertation submitted in partial fulfillment of the

requirements for the degree of

DOCTOR OF PHILOSOPHY

in

Materials Science and Engineering

by

Lyci George

2010

To:  Dean Amir Mirmiran

College of Engineering and Computing

This dissertation, written by Lyci George, and entitled Structural Characterization of Metal Hydrides for Energy Applications, having been approved in respect to style and intellectual content, is referred to you for judgment.

We have read this dissertation and recommend that it be approved.

_______________________________________

Arvind Agarwal

_______________________________________

Chunlei Wang

_______________________________________

Gautam Sen

_______________________________________

Surendra K. Saxena, Major Professor

Date of Defense: May 19, 2010

The dissertation of Lyci George is approved.

_______________________________________

Dean Amir Mirmiran

College of Engineering and Computing

_______________________________________

Interim Dean Kevin O’Shea

University Graduate School

Florida International University, 2010

ACKNOWLEDGMENTS

First of all, I wish to thank my Major Professor Dr. Surendra Saxena for his advices, support and guidance throughout the dissertation period. I greatly acknowledge him for the opportunities availed to me during my dissertation such as to work in national synchrotron facilities and to attend many national and international conferences.  Those experiences molded me towards different aspects of my goal and helped me to expand my knowledge.

I would like to thank my dissertation committee members, Dr. Arvind Agarwal, Dr. Gautam Sen and Dr. Chunlie Wang, for their suggestions and encouragement for this endeavor. I also acknowledge Dr. Jiuhua Chen for his help and useful discussuions about the hydride research. I greatly appreciate Dr. Vadym Drozd for his guidance and also his help during different stages of the experiments. I thank Dr. Andriy Durygin for making me friendly with the instruments and Dr. Selva Raju for introducing me to high pressure techniques. I always remember the efforts of Dr. Marek Tkacz, Dr. Taras Palasyuk at Polish Academy of Sciences, to teach me the high pressure gas loading technique. I appreciate Mr. Jose Herrera for his help whenever needed during the experiments. I wish to thank Dr. Maximilian Fichtner at Institute of Nanotechnology, Germany, for providing two of the samples used for the study. I extend my thanks to all other colleagues at the Center for the Study of Matter at Extreme Conditions (CeSMEC) for their help and support.

I greatly acknowledge the financial support from Florida International University graduate school in the form of doctoral evidence acquisition (DEA) fellowship and dissertation year fellowship (DYF). I would like to acknowledge the financial support from National Science Foundation (International Materials Institute subcontract) to carry out the PCA work and also to attend two international conferences conducted in India. I am grateful to Carnegie DOE Alliance Center (CDAC) for their financial support and also for the special allocation of beam time at Advanced Photon Source (APS).

Portions of this work were performed at HPCAT of Advanced Photon Source (APS), Argonne National Laboratory. HPCAT is supported by DOE-BES, DOE-NNSA, NSF, and the W.M. Keck Foundation. APS is supported by DOE-BES, under Contract No. DE-AC02-06CH11357.  A portion of this work is based upon research conducted at the Cornell High Energy Synchrotron Source (CHESS) which is supported by the National Science Foundation and the National Institutes of Health/National Institute of General Medical Sciences under award DMR-0225180. Part of this work was also carried out at the National Synchrotron Light Source (stations  X17C and X17B2), Brookhaven National Laboratory, which was supported by the U.S. Department of Energy, Office of Science, Office of Basic Energy Sciences, under Contract No. DE-AC02-98CH10886.  I also thank all the beam line staffs at these synchrotron facilities especially Dr. Yue Meng, Dr. Peter Lierman, Dr. Zhiqiang Chen and Dr. Sanjit Ghose for helping with experimental setups.

I always remember all those good teachers who inspired me for this goal. I greatly acknowledge my loving husband Ved for boosting my confidence and also for his invaluable assistance at various stages of this work. I also thank my twin sister Lincy and all my friends for motivating me and being with me whenever I needed. Lastly, I would like to thank my family members for encouraging me to pursue higher studies and being supportive through out my education.

ABSTRACT OF THE DISSERTATION

STRUCTURAL CHARACTERIZATION OF METAL HYDRIDES

FOR ENERGY APPLICATIONS

by

Lyci George

Florida International University, 2010

Miami, Florida

Professor Surendra K. Saxena, Major Professor

Hydrogen can be an unlimited source of clean energy for future because of its very high energy density compared to the conventional fuels like gasoline.  An efficient and safer way of storing hydrogen is in metals and alloys as hydrides. Light metal hydrides, alanates and borohydrides have very good hydrogen storage capacity, but high operation temperatures hinder their application. Improvement of thermodynamic properties of these hydrides is important for their commercial use as a source of energy. Application of pressure on materials can have influence on their properties favoring hydrogen storage. Hydrogen desorption in many complex hydrides occurs above the transition temperature. Therefore, it is important to study the physical properties of the hydride compounds at ambient and high pressure and/or high temperature conditions, which can assist in the design of suitable storage materials with desired thermodynamic properties.

The high pressure-temperature phase diagram, thermal expansion and compressibility have only been evaluated for a limited number of hydrides so far. This situation serves as a main motivation for studying such properties of a number of technologically important hydrides. Focus of this dissertation was on X-ray diffraction and Raman spectroscopy studies of Mg2FeH6, Ca(BH4)2, Mg(BH4)2, NaBH4, NaAlH4, LiAlH4, LiNH2BH3 and mixture of MgH2 with AlH3 or Si, at different conditions of pressure and temperature, to obtain their bulk modulus and thermal expansion coefficient.  These data are potential source of information regarding inter-atomic forces and also serve as a basis for developing theoretical models. Some high pressure phases were identified for the complex hydrides in this study which may have better hydrogen storage properties than the ambient phase. The results showed that the highly compressible B-H or Al-H bonds and the associated bond disordering under pressure is responsible for phase transitions observed in brorohydrides or alanates. Complex hydrides exhibited very high compressibility suggesting possibility to destabilize them with pressure. With high capacity and favorable thermodynamics, complex hydrides are suitable for reversible storage. Further studies are required to overcome the kinetic barriers in complex hydrides by catalytic addition.  A comparative study of the hydride properties with that of the constituting metal, and their inter relationships were carried out with many interesting features.

TABLE OF CONTENTS

CHAPTER										 PAGE

| 1. INTRODUCTION | 1 |
| --- | --- |
| 1.1. Overview | 2 |
| 1.2. Challenges | 3 |
| 1.3. Purpose of the Dissertation | 4 |
| 1.4. Description of Experiments and Analyses | 6 |
| 2. LITTERATURE REVIEW | 8 |
| 2.1. Metal Hydrides | 9 |
| 2.2. Complex Hydrides | 12 |
| 2.3. Equations of State | 14 |
| 2.3.1. Pressure equations of state | 15 |
| 2.3.2. Thermal equations of state | 16 |
| 2.4. Investigation of Hydrides under High- Pressure and Temperature | 17 |
| 2.5. Applications of Hydrides | 22 |
| 3. EXPERIMENTAL TECHNIQUES AND DETAILS | 24 |
| 3.1. Diamond Anvil Cell Technique | 24 |
| 3.1.1. Measurement of pressure in a DAC | 26 |
| 3.1.2. Sample loading in the DAC | 28 |
| 3.1.3. Resistive heating in a DAC | 29 |
| 3.2. X-Ray Diffraction Techniques | 30 |
| 3.2.1. Powder X-ray diffraction | 30 |
| 3.2.2. Synchrotron X-ray source | 32 |
| 3.2.3. Rotating anode X-ray generator | 34 |
| 3.2.4. Indexing of X-ray diffraction patterns | 36 |
| 3.3. Raman Spectroscopy | 37 |
| 3.4. Analysis of Powder X-ray Diffraction Data | 40 |
| 3.4.1. Rietveld method | 40 |
| 3.4.2. Le Bail method | 40 |
| 3.4.3. Data processing and analysis tools used in the study | 41 |
| 4. STRUCTURAL STABILITY OF Mg2FeH6 UNDER HIGH PRESSURES AND TEMPERATURES | 43 |
| 4.1. Introduction | 43 |
| 4.2. Synthesis and Characterization of Mg2FeH6 | 45 |
| 4.2.1. Synthesis | 45 |
| 4.2.2. Electron microscopy | 45 |
| 4.2.3. X-ray diffraction | 46 |
| 4.2.4. Computation | 46 |
| 4.3. Results and Discussions | 47 |
| 4.3.1. Electron microscopy | 47 |
| 4.3.2. High pressure micro X-ray diffraction | 49 |
| 4.3.3. High temperature X-ray diffraction | 54 |
| 4.3.4. Raman spectroscopy | 55 |
| 5. STRUCTURAL STABILITY OF DIFFERENT POLYMORPHS OF Mg(BH4)2 | 57 |
| 5.1. Introduction | 57 |
| 5.2. Experimental Details | 59 |
| 5.2.1. Synthesis | 59 |
| 5.2.2. High pressure micro X-ray diffraction | 59 |
| 5.3. Results and Discussion | 60 |
| 5.3.1. X-ray diffraction of as synthesized Mg(BH4)2 | 60 |
| 5.3.2. Raman spectroscopy measurements | 64 |
| 5.3.2.1. As synthesized Mg(BH4)2 | 64 |
| 5.3.2.2. The high temperature phase of Mg(BH4)2 | 69 |
| 5.3.2.3. High pressure phase of Mg(BH4)2 | 71 |
| 6. HIGH PRESSURE INVESTIGATION OF Ca(BH4)2 | 73 |
| 6.1. Introduction | 73 |
| 6.2. Experimental Details | 74 |
| 6.2.1. Synthesis | 74 |
| 6.2.2. High pressure micro X-ray diffraction | 75 |
| 6.3. Results and Discussion | 75 |
| 6.3.1. X-ray diffraction | 75 |
| 6.3.2. Raman spectroscopy | 79 |
| 7. HIGH PRESSURE INVESTIGATION AND P-T PHASE DIAGRAM OF NaBH4 | 84 |
| 7.1. Introduction | 84 |
| 7.2. Experimental Details | 86 |
| 7.3. Results and Discussion | 86 |
| 7.3.1. In situ high P-T X-ray diffraction | 86 |
| 7.3.1.1. Angle dispersive micro X-ray diffraction | 86 |
| 7.3.1.2. Energy dispersive micro X-ray diffraction | 91 |
| 7.3.2. Raman spectroscopy | 93 |
| 7.3.2.1. High pressure in situ Raman spectroscopy | 93 |
| 7.3.2.2. High P-T Raman spectroscopy | 98 |
| 7.3.3. P-T phase diagram | 100 |
| 7.3.4. Correlation of site group to factor group and Raman activity | 101 |
| 8. STRUCTURAL INVESTIGATION OF NaAlH4 AND THE INFLUENCE OF BALL MILLING ON COMPRESSION PROPERTIES | 104 |
| 8.1. Introduction | 104 |
| 8.2. Unmilled NaAlH4 | 106 |
| 8.2.1. Experimental details | 106 |
| 8.2.2. Results and discussion | 106 |
| 8.2.2.1. X-ray diffraction | 106 |
| 8.2.2.2. Raman spectroscopy | 109 |
| 8.3. Mechano-chemically Milled NaAlH4 | 110 |
| 8.3.1. Experimental details | 110 |
| 8.3.2. Results and discussions | 111 |
| 9. HIGH PRESSURE INVESTIGATION OF STRUCTURAL STABILITY OF LiAlH4 112 |  |
| 9.1. Introduction | 115 |
| 9.2. Experimental Details | 116 |
| 9.3. Results and Discussion | 116 |
| 9.3.1. X-ray diffraction | 116 |
| 9.3.2. Raman spectroscopy | 118 |
| 10. PRINCIPAL COMPONENT ANALYSIS ON PROPERTIES OF BINARY AND TERNARY HYDRIDES | 121 |
| 10.1. Introduction | 121 |
| 10.2. Data | 122 |
| 10.3. Method | 122 |
| 10.4. Results and Discussion | 125 |
| 11. INVESTIGATION OF MIXTURES OF HYDRIDES | 131 |
| 11.1. High Pressure Raman Spectroscopic Investigation of LiNH2BH3 | 131 |
| 11.1.1. Introduction | 131 |
| 11.1.2. Results and Discussions | 134 |
| 11.2. High P-T investigation of mixture of MgH2 and AlH3 | 142 |
| 11.2.1. Introduction | 142 |
| 11.2.2. Results and discussions | 145 |
| 11.2.2.1. X-ray diffraction | 145 |
| 11.2.2.2. Raman spectroscopy | 149 |
| 11.3. Mixtures of Si and MgH2 | 151 |
| 11.3.1. Introduction | 151 |
| 11.3.2. Results and discussion | 152 |
| 12. COMPARISON OF PROPERTIES OF HYDRIDES | 154 |
| 12.1. Properties of Metals and Hydrides: A Comparison | 154 |
| 12.2. Inter-relationships of Thermodynamic Properties of Hydrides | 160 |
| 12.3. Structural Properties of Complex Metal Hydrides | 167 |
| 13. SUMMARY | 172 |
| 13.1. Conclusions | 172 |
| 13.2. Recommendations for Future Research | 175 |
| LIST OF REFERENCES | 177 |
| APPENDIX | 192 |
| VITA | 198 |

LIST OF TABLES

TABLE									             PAGE

| Table 2. 1: Weight, gravimetric (wt %) and volumetric (kg/m3) hydrogen contents and decomposition temperature of alkali and alkali- earth metal hydrides. | 10 |
| --- | --- |
| Table 2. 2: A comparison of structure and bulk modulus values of alkali and alkali- earth metals. | 11 |
| Table 2. 3: Weight, gravimetric (wt %) and volumetric (kg/m3) hydrogen content, decomposition reaction and corresponding temperature of alkali and alkali- earth complex hydrides. | 13 |
| Table 2. 4: A comparison of transition pressure, temperature, structure and bulk modulus data of alkali and alkali- earth metal hydrides. The data marked * is from computation results and others are experimental values. | 19 |
| Table 2. 5: A comparison of transition pressure, temperature, structure and bulk modulus data of alkali and alkali- earth alanates. The data marked * is from computation results and others are experimental values. | 20 |
| Table 2. 6: A comparison of transition pressure, temperature, structure and bulk modulus of alkali and alkali- earth borohydrides. The data marked * is from computation results and others are experimental values. | 21 |
| Table 3. 1: High pressure apparatuses and pressure- temperature ranges that can be achieved using each of them. | 24 |
| Table 3. 2: Different information available from the condition of Debye rings in a 2D X-ray diffraction experiment. | 31 |
| Table 4. 1: Weight % of elemental components O, Mg and Fe obtained from EDS analysis at spots marked 1-3 in the secondary image. | 49 |
| Table 4. 2: Data obtained from fitting P-V data with Birch-Murnaghan EoS for various Mg2FeH6 samples with a comparison of pressure ranges. PTM abbreviates pressure transmitting medium. | 53 |
| Table 5. 1: Raman frequency shifts as a function of pressure for liberational, translational and bending modes from fitting the compression data of as synthesized sample. | 69 |
| Table 5. 2: Raman frequency shifts as a function of pressure for B- H stretching modes during both compression and decompression of as prepared Mg(BH4)2. | 69 |
| Table 5. 3: Raman frequency shifts as a function of pressure for B-H stretching modes during both compression and decompression for the high temperature phase of Mg(BH4)2. | 71 |
| Table 6. 1: Change in Raman shift frequencies as a function of pressure for B-H stretching modes of Ca(BH4)2 during compression and decompression. | 83 |
| Table 7. 1: The observed B-H stretching modes in cm-1 (sh- shoulder) for different phases of NaBH4. | 98 |
| Table 7. 2: The pressure dependence of Raman shift frequency for NaBH4 during both compression and decompression. | 98 |
| Table 7. 3: Symmetry analysis and irreducible representation of lattice modes of NaBH4. | 103 |
| Table 10. 1: The component matrix obtained from PCA of a set of data with both binary and ternary hydrides. Subscript M denotes metal and MH abbreviates metal hydride. | 127 |
| Table 10. 2: Correlation matrix obtained from PCA of a set of data with both binary and ternary hydrides. M and MH abbreviates metal and metal hydride, respectively. | 127 |
| Table 11. 1: Raman shift frequencies in cm-1for LiNH2BH3 (LAB) in this study at ambient conditions in comparison with that of NH3BH3 (AB); str. Abbreviates stretching modes. The mode frequencies marked * are from FTIR study [229]. | 138 |
| Table 11. 2: B-H and N-H stretching modes of the LiNH2BH3 in cm-1 at 4.2 GPa as observed from Raman spectra of two different phase regions, D and W. The wave numbers given in bold are of an unidentified phase. | 140 |
| Table 12. 1: Approximate values of molar volumes of hydrogen atoms in boron hydrides. | 155 |
| Table 12. 2: Variation of the entropy of hydrogen in some binary metal hydrides (MHx). | 155 |
| Table 13.1. Summary of the results obtained from the high pressure and/or temperature investigations of the complex hydrides. Data marked * are of ball milled sample. | 174 |

LIST OF FIGURES

FIGURE									             PAGE

| Figure 1. 1: Summary of the research work performed in the dissertation. |  | 1 |
| --- | --- | --- |
| Figure 1. 2: A comparison of the specific energy content of hydrogen with that of other fuels. |  | 3 |
| Figure 3. 1: a) A loaded Mao- Bell type DAC; b) schematic of the sample chamber in a diamond anvil cell, 1- diamond, 2- gasket hole, 3- sample, 4- gasket, 5- ruby chip. |  | 25 |
| Figure 3. 2: The shift of ruby fluorescent spectrum with the application of a pressure of 4.4 GPa. |  | 27 |
| Figure 3. 3: Drilling machine which is employed to drill holes in the gaskets using spark erosion method. |  | 29 |
| Figure 3. 4: Schematics of an X-ray diffractometer with transmission geometry; adapted from X17C hutch at NSLS [107]. |  | 33 |
| Figure 3. 5: The X-ray diffractometer stage at the beam line 16 IDB- HPCAT of Argonne National Laboratory. |  | 35 |
| Figure 3. 6: A Bruker- GADDS/D8 X-ray system with molybdenum rotating anode X-ray generator at CeSMEC. |  | 37 |
| Figure 3. 7: Raman spectroscopy setup with in situ ruby pressure measurement system at CeSMEC. |  | 38 |
| Figure 4. 1: a) Selective area electron diffraction pattern of annealed Mg2FeH6. b) TEM image of as synthesized sample. |  | 48 |
| Figure 4. 2: (a) Backscattered SEM image and; (b) secondary image of annealed Mg2FeH6. |  | 48 |
| Figure 4. 3: The EDS spectrum collected from spot 3 marked in the secondary image. |  | 49 |
| Figure 4. 4: Synchrotron XRD pattern collected at ambient conditions with the results of the Rietveld analysis. Inset is the simulated crystal structure of Mg2FeH6. |  | 50 |
| Figure 4. 5: (a) Debye diffraction rings collected from sample loaded in DAC, at ambient conditions. (b) X-ray diffraction patterns of Mg2FeH6 for some selected pressures during compression and decompression (pressure indicated by *). Peaks correspond to hcp phase of Fe are marked by closed circles in the patterns at 18.9 GPa. |  | 51 |
| Figure 4. 6: A comparison of calculated and experimental variation of unit cell volume of Mg2FeH6 (MFH) with pressure fitted with the third order Birch-Murnaghan EoS under different conditions. PTM abbreviates pressure transmitting medium. |  | 52 |
| Figure 4. 7: High temperature XRD patterns of the Mg2FeH6 collected at various temperatures. In the pattern taken at 450 ºC, peak marked by asterisks is due to Fe and that marked by closed circle is MgO, and others are of Mg. |  | 54 |
| Figure 4. 8: Plot of normalized volume versus temperature for Mg2FeH6 fitted with a second order polynomial. |  | 55 |
| Figure 4. 9: Raman spectrum of Mg2FeH6 at ambient conditions. Liberational modes (x); Fe-H bending modes (*); Fe-H stretching mode (o). |  | 56 |
| Figure 5. 1: Synchrotron XRD pattern of low pressure phase of Mg(BH4)2 at ~ 1GPa with the results of Le Bail profile fitting and inset shows the corresponding hexagonal P61 structure. |  | 60 |
| Figure 5. 2: The synchrotron XRD pattern obtained for Mg(BH4)2; (a) during compression (λ = 0.4066 Å) up to ~ 11GPa, (b) during decompression (λ = 0.368138 Å) at various pressures. |  | 61 |
| Figure 5. 3: Pressure dependence of volume (circles) for the high pressure phase of Mg(BH4)2, during compression, fitted with third order Birch- Murnaghan EoS (line). |  | 63 |
| Figure 5. 4: The Raman spectra of Mg(BH4)2 collected during compression up to ~ 21 GPa at some selected pressures; (a) B-H bending modes, (b) B-H stretching modes. The peak around 1350 cm-1 is because of diamond in DAC. |  | 65 |
| Figure 5. 5: The Raman spectra of Mg(BH4)2 collected during decompression to ambient pressure; (a) B-H bending modes, (b) B-H stretching modes. Peak marked with asterisks is due to impurities in diamond. |  | 66 |
| Figure 5. 6: Change in vibrational frequency with pressure for as prepared Mg(BH4)2 during compression; (a) liberational and translational modes, (b) B-H bending modes. The pressures corresponding to change in vibrational modes during compression is marked by grid lines parallel to Y axis. |  | 67 |
| Figure 5. 7: Change in vibrational frequency of B-H stretching modes with pressure for as prepared Mg(BH4)2; (a) during compression, (b) during decompression. The pressures corresponding to change in vibrational modes during compression is marked by grid lines parallel to Y axis. |  | 68 |
| Figure 5. 8: (a) Raman spectra of as prepared Mg(BH4)2 in comparison with the high temperature phase during compression; peak marked with asterisks is due to impurities in diamond; BH- before heating (as synthesized); AH- after heating (high temperature phase). (b) Change in B-H stretching modes with pressure for the high temperature phase. |  | 70 |
| Figure 5. 9: Raman spectra of Mg(BH4)2; (a) as synthesized phase in comparison with the high pressure phase during compression at some selected pressures,(b) high pressure phase up to 375 ºC at some selected temperatures. |  | 72 |
| Figure 6. 1: Synchrotron X-ray diffraction pattern of the sample containing α and β polymorphs of Ca(BH4)2 at ambient conditions; (a) Debye ring, (b) integrated plot with the results of Rietveld analysis. |  | 76 |
| Figure 6. 2: The refined crystal structures of Ca(BH4)2 polymorphs; (α) orthorhombic and (β) tetragonal- P42/ m phases. The atoms Ca, B and H are represented by symbols of color blue, red, and black, respectively. |  | 77 |
| Figure 6. 3: Synchrotron XRD patterns of Ca(BH4)2; during compression up to 13.6 GPa and after decompression to 0.5 GPa (marked **). |  | 78 |
| Figure 6. 4: Pressure dependence of the volume (circles) for α-Ca(BH4)2 during compression, fitted with the third-order Birch-Murnaghan equation of state (line). |  | 79 |
| Figure 6. 5: Raman spectrum (blue line) of Ca(BH4)2 containing both α (yellow colored peaks) and β (black colored peaks) polymorphs collected at ambient conditions. |  | 80 |
| Figure 6. 6: Raman spectra of Ca(BH4)2; (a) during compression up to 25 GPa, (b) during decompression for B-H stretching modes. The peak (marked *) around 2650 cm-1 is because of diamond in the DAC. |  | 81 |
| Figure 6. 7: Change in the Raman shift with pressure for B-H stretching modes of Ca(BH4)2; (a) during compression and (b) during decompression. The pressures corresponding to the change in vibrational modes are marked by grid lines parallel to the Y axis. |  | 82 |
| Figure 7. 1: Micro X-ray diffraction pattern of the cubic phase of NaBH4 collected at 0.8 GPa using a synchrotron source with the results of Rietveld analysis. The peak positions marked in green (a) corresponds to that of NaBH4 and that marked in pink (b) are of NaCl. |  | 87 |
| Figure 7. 2: Selected XRD patterns of the three different phases of the NaBH4, at room temperature; (a) the cubic (3.4 GPa), tetragonal (6.5 GPa) and orthorhombic (9 GPa). (b) at various temperatures and 6.5 GPa. Between 323 and 373 K, tetragonal to cubic phase transition occurs. Peaks marked * are of NaCl which was used as a pressure marker. |  | 88 |
| Figure 7. 3: Crystal structures of (a) the cubic, (b) tetragonal and (c) orthorhombic phases of NaBH4. The Na, B, and H are marked in green, orange and black symbols, respectively. |  | 89 |
| Figure 7. 4: Selected high pressure XRD patterns of NaBH4 above 13.4 GPa up to 34 GPa. The arrow indicated new peaks, and decompressed pattern is marked *. |  | 90 |
| Figure 7. 5: An EDXRD pattern of cubic- NaBH4 at 0.2 GPa. The peaks marked (*), (o) and (#) are due to BN, NaCl and Kα, respectively. |  | 91 |
| Figure 7. 6: Pressure dependence of the unit cell volume (circles) for the high-pressure phase of cubic NaBH4 during compression at room temperature and at 573 K, fitted with third order Birch- Murnaghan EoS (line). |  | 92 |
| Figure 7. 7: Raman spectra of NaBH4 during compression; (a) at selected pressures and the spectrum marked ? corresponds to the appearance of a new phase, (b) spectra in the range 14-30 GPa. |  | 94 |
| Figure 7. 8: Selected Raman spectra of NaBH4 during decompression. |  | 95 |
| Figure 7. 9: The Raman shift versus pressure obtained by peak fitting of B-H stretching modes at each pressure; (a) during compression and (b) decompression. Pressures corresponds to phase transition are marked with grid lines parallel to the Y axis. |  | 96 |
| Figure 7. 10: The high temperature Raman spectra of NaBH4 in the B-H stretching mode region; (a) while heating at 9.5 GPa in comparison with a spectrum at 3 GPa, (b) at 14 GPa and different temperatures. |  | 99 |
| Figure 7. 11: P-T phase diagram of NaBH4 investigated through DAC technique using XRD and Raman spectroscopic measurements (circles) including the results of low temperature study of Sundqvist et al. [169], (asterisks). The phase regions marked C, T, O and M are cubic, tetragonal, orthorhombic and monoclinic, respectively. The region marked ? implies structure of phase is not confirmed. |  | 100 |
| Figure 8. 1: The XRD patterns of unmilled NaAlH4 recorded at various pressures up to 13.6 GPa. Peaks due to orthorhombic phase are marked by asterisks at 12.4 GPa. |  | 107 |
| Figure 8. 2: The P-V plot of unmilled NaAlH4 (circles) fitted with Birch- Murnaghan equation of state (line). |  | 108 |
| Figure 8. 3: Raman spectra of unmilled NaAlH4 at various pressures up to 15GPa. The change in Raman modes under pressure are marked with arrow. |  | 109 |
| Figure 8. 4: The XRD patterns of the ball-milled NaAlH4 collected at various pressures. Pattern marked * is from decompressed sample, and Pt metal was used as a pressure marker. |  | 112 |
| Figure 8. 5: Birch Murnaghan EoS fit (line) to the P-V data (circles) of ball milled NaAlH4. |  | 114 |
| Figure 9. 1: Comparison of the high pressure XRD patterns of LiAlH4 collected at room temperature. |  | 117 |
| Figure 9. 2: The P-V data (circles) obtained for monoclinic phase of LiAlH4 fitted with third order Birch-Murnaghan EoS (line). |  | 118 |
| Figure 9. 3: Raman spectrum of LiAlH4 in at ambient conditions (dotted line) fitted with a Gaussian profile function. |  | 119 |
| Figure 9. 4: Raman spectra of LiAlH4 collected at various pressures and at room temperature. |  | 120 |
| Figure 10. 1: Eigen value and total variance explained by each component obtained from PCA of a set of data with both binary and ternary metal hydrides. |  | 126 |
| Figure 10. 2: Component plots for a set of data with both binary and ternary hydrides. Subscript M denotes metal and MH denotes metal hydride. S- entropy, Cp- specific heat, V- molar volume and H wt %- hydrogen weight percent in each compound. |  | 128 |
| Figure 10. 3: Plot of score 2 versus score 1of a set of data with both binary and ternary hydrides. |  | 129 |
| Figure 10. 4: Plot of scores of first two principal components for binary hydrides. |  | 130 |
| Figure 10. 5: Plot of scores of first two principal components for ternary hydrides. |  | 130 |
| Figure 11. 1: Lattice, bending and B-H stretching modes in the Raman spectrum of LiNH2BH3, collected at ambient conditions fitted with a Gaussian profile function. |  | 135 |
| Figure 11. 2: N-H stretching modes in the Raman spectrum of LiNH2BH3, collected at ambient conditions fitted with a Gaussian profile function. |  | 136 |
| Figure 11. 3: The sample loaded in DAC with two phase regions marked W and D at different pressures. DP0 implies decompressed sample at ambient conditions. |  | 136 |
| Figure 11. 4: Raman spectra of LiNH2BH3 during compression (right) and decompression (left) for the regions W (top) and D (bottom), respectively. |  | 137 |
| Figure 11. 5: Change of Raman shift with pressure for LiNH2BH3 during compression of B-H (left) and N-H (right) stretching modes for the regions W (top) and D (bottom), respectively. |  | 141 |
| Figure 11. 6: The micro XRD patterns of mixture of AlH3 and MgH2 collected at various pressures and room temperature. Abbreviations: bh- before heating, ah- after heating. |  | 146 |
| Figure 11. 7: The XRD pattern from decompressed sample at room temperature after heating under pressure up to 9 GPa matched with peaks corresponds to MgH2 (shorter lines) and Al (longer lines). |  | 147 |
| Figure 11. 8: XRD patterns of Mg(AlH4)2 containing LiCl (marked *) at some selected pressures. |  | 148 |
| Figure 11. 9: Raman spectra of the 2AlH3+ MgH2 mixture collected at various pressures in comparison with the Raman spectra of Mg(AlH4)2 . |  | 149 |
| Figure 11. 10: Raman spectra of Mg(AlH4)2 collected at various pressures. Spectrum marked * is of the decompressed sample and ‘ah’ abbreviates after heating. |  | 150 |
| Figure 11. 11: (a) The XRD pattern of the mixture of Si and MgH2 in comparison to that of pure components. (b) Raman spectra of MgH2+ Si mixture before and after heating at 0.5 GPa and 600 ºC and that of pure Mg2Si; bh and ah abbreviates before and after heating, respectively. |  | 153 |
| Figure 12. 1: Comparison of molar volume of binary hydrides and corresponding metal. |  | 157 |
| Figure 12. 2: Molar volume of Li containing hydrides versus the element sum [70, 71, 73, 83, 170, 247-249]. |  | 157 |
| Figure 12. 3: A comparison of entropy versus molar volume of metals and metal hydrides. Subscript M denotes metal and MH denotes metal hydride. |  | 158 |
| Figure 12. 4: Plots of entropy of binary metal hydrides versus that of corresponding metals. |  | 159 |
| Figure 12. 5: Plot of specific heat of various binary metal hydrides versus that of the host metal. The dotted line corresponds to the specific heat of metals. |  | 159 |
| Figure 12. 6: A comparison of molar volumes (cm3/mol) of various alkali hydrides with that of the corresponding host metals. |  | 160 |
| Figure 12. 7: Variation of entropy with molar volume of various hydrides [62, 249-253]. |  | 161 |
| Figure 12. 8: The variation of hydrogen content versus molar volume for the rare-earth metal hydrides. |  | 162 |
| Figure 12. 9: The variation of specific heat versus molar volume for binary metal hydrides [70, 71, 73, 83, 170]. |  | 162 |
| Figure 12. 10: Plot of enthalpy versus molar volume of alkali and alkali- earth metal hydrides. |  | 163 |
| Figure 12. 11: Plot of bulk modulus versus molar volume of alkali and alkali- earth metal hydrides. |  | 164 |
| Figure 12. 12: Plot of decomposition temperature versus density of alkali and alkali- earth metal hydrides. |  | 165 |
| Figure 12. 13: Plot of decomposition temperature versus density of alkali and alkali- earth complex hydrides. |  | 166 |
| Figure 12. 14: Plot of bulk modulus versus molar volume of alkali and alkali- earth complex hydrides. |  | 166 |
| Figure 12. 15: A comparison of the change of molar volume with pressure for the complex hydrides investigated in this study. |  | 171 |

# CHAPTER 1. INTRODUCTION

This dissertation focuses on investigation of the structural stability of light hydrides with high gravimetric and volumetric hydrogen storage capacities under high pressures or temperatures.  The goal of this study, as summarized in Figure 1.1, is to obtain thermodynamic and physical properties of hydrides which are important to determine the factors affecting their stability.

Study of physical properties of metal hydrides

Analysis of hydride property data

–Principal component analysis

–Comparison of properties of metals and hydrides

Structural characterization

– Investigation of promising phases over wide P-T ranges

–Crystal structure, bonding and phase transitions

–Construction of P-T phase diagram

Raman spectroscopy

–Effect of pressure on Raman shift

–Determination of phase boundary

X-ray diffraction

–Change of unit cell volume under pressure or temperature

–P-V-T data fit to determine bulk modulus and thermal expansion of hydrides

–Study of the influence of ball milling on the physical properties of hydrides

Figure 1. 1: Summary of the research work performed in the dissertation.

## Overview

The depletion of fossil fuels, increase in pollution and related environmental hazards require us to discover alternate energy sources. Hydrogen is a zero emission fuel with very high specific energy content of about 120 MJ/kg and an energy density of 10Wh/kg. A comparison of energy contents of various fuels are illustrated in Figure 1.2. Storage is a challenging issue that cuts across production, delivery and commercial applications of hydrogen as an energy carrier. Use of pure H2 is not economical as it requires high pressure gas cylinders that can handle pressures up to 80 MPa, or cryogenic tanks which have to be maintained at 21 K.  Hydrogen stored in solid materials are safe alternative to liquid or compressed form and convenient for long time storage with high yield. Hydrogen storage in materials can be categorized into two types;

- Metal and complex hydrides (eg. LiH, LiNH2, NaBH4, Mg(AlH4)2 etc.),

- High surface area sorbents (eg. carbon based materials, clatherates, conducting polymers, nanotubes/fibers, metal-organic frameworks and aero gels).

Among the above discussed hydrogen storage materials, hydrides are interesting because of their high volumetric and gravimetric density.  The fuel cell technology requires hydrides of high hydrogen storage densities with moderate hydrogenation kinetics.

Figure 1. 2: A comparison of the specific energy content of hydrogen with that of other fuels.

## Challenges

A hydrogen storage material should release H2 at low temperature with wide range of operation, high volumetric density and mass density. A hydride should also have rapid hydrogenation/dehydrogenation rates, high resistance to oxidation, high capacity, low cost, good reversibility, fast reactivity and sustainability. Main issues of hydrides are weight, volume, cost, safety, efficiency, refueling time and durability. Minimum requirements for automobile applications of hydrides are:

- Gravimetric energy density: 2 kWh/kg

- Volumetric energy density: 1.5 kWh/liter

- H2 storage capacity: 6 wt %,

- Operating temperature: 30 to 50 ºC

- Refueling time:< 5 min

- Refueling rate: 1.5 kg H2/min

- Recoverable amount of hydrogen: 90 %

- Cycle life: 500 times

- Cost target: US $5/kWh (without peripheral components)

The transport sector requires not only cheap, safe and reliable way of storing hydrogen but also high storage capacity, fast kinetics and favorable thermodynamics. A potential hydrogen storage candidate has yet to be discovered, which meets all the mentioned criteria. One of the high-priority goals of the Department of Energy is “finding effective hydrogen storage materials” which they list as one of the most difficult challenges of commercial use of hydrides for transportation. Light metal hydrides have good hydrogen storage capacity but operation temperature is very high while transition metal hydrides release H2 at room temperature but with less storage capacity. Therefore it is important to study thermodynamic stability of light hydrides in order to understand possibilities to improve the temperature of operation. Study of physical properties of hydrides under pressure/temperature conditions can assist in the design of suitable storage materials.

## Purpose of the Dissertation

The high pressure-temperature phase diagram, thermal expansion and compressibility have only been evaluated for a limited number of hydrides so far. This situation serves as a main motivation for studying such properties of a number of technologically important hydrides. The application of pressure on materials can have influence on their properties favoring hydrogen storage. Study of hydrides under pressure is interesting because it can help to understand atomic, electronic and structural properties of hydrogen which in turn will shed light on improving the storage properties. The high pressure investigations can reveal if a polymorph with higher storage capacity can be retained at ambient conditions.

This dissertation is targeting high volumetric and gravimetric storage capacities as the criteria for selection of hydride materials for the study. Eventhough the selected hydrides have high hydrogen storage capacity, their dehydrogenation properties are not good due to kinetic barriers. To modify the hydrides for commercial applications we need to understand the crystal structure, bonding and related properties. Crystal structure, compressibility and thermal expansion of a number of complex hydrides (eg., LiAlH4, NaAlH4, NaBH4, Mg2FeH6, Mg(BH4)2, and Ca(BH4)2 ) has been studied at high pressures using diamond anvil cell (DAC) technique and observed interesting new phases for most of them. Reactions of MgH2 with AlH3 and Si under P-T conditions, and structural phase trasitions of LiNH2BH3 also have been investigated. The main focus is on Mg and Al based hydrides as they are light and abundant materials, and has relatively low operating temperatures. Alanates and borohydrides of alkali or alkali-earth metals have improved thermodynamic and kinetic properties as compared to their metal hydride counterparts. Structural measurements on the hydride compounds at ambient and high pressure or temperature conditions can result in a better understanding of the stability of the hydride structures and can assist us in the design of suitable storage materials with desired thermodynamic properties.  Furthermore, it is reported that the crystallite size and processing conditions influence the H2 sorption kinetics of the hydrogen storage materials. The investigation of the influence of crystallite size is essential in order to obtain a reliable reference for evaluation of the kinetic effects of doping with catalytic additives. Therefore, the effect of ball milling on the properties   of Mg2Fe2H6 and NaAlH4 also has been investigated. Hydrides are light materials with low scattering power and the use of diamond anvil cell limits the amount of sample we can use. In order to resolve dynamical structural changes under pressure, high quality data is required and hence the micro X-ray diffraction using synchrotron radiation source is availed for the study. To confirm the phase transitions and to obtain the accurate transition pressures, Raman spectroscopic study also has been carried out.

## Description of Experiments and Analyses

The main focus of this dissertation is to investigate the structural phase transitions of selected hydrides at high pressures and to determine their thermodynamic properties.

- Micro X-ray diffraction studies of structural phase transitions under high pressures up to 10-35 GPa for LiAlH4, NaAlH4, NaBH4, Mg2FeH6, Mg(BH4)2 and Ca(BH4)2, using synchrotron radiation source.

- Raman spectroscopic investigation of structural stability under high pressures up to 30 GPa for LiAlH4, NaAlH4, NaBH4, Mg(BH4)2, Ca(BH4)2 and LiNH2BH3.

- Thermal decomposition studies of Mg2FeH6 in the range 25-500 ⁰C in quartz capillary and high pressure phase of Mg(BH4)2 in a DAC using resistive heating.

- Construction of P-T phase diagram for NaBH4 using resistive heating (P < 15 GPa, T< 500 ⁰C) in the DAC from the results of micro X-ray diffraction and Raman spectroscopic studies.

- Investigation of the effect of ball milling as well as that of mineral oil and silicone oil on the physical properties of NaAlH4 and Mg2FeH6.

- Micro structural characterization of Mg2FeH6 using scanning and transmission electron microscopy techniques.

- Determination of the change of lattice parameters and hence the molar volume with pressure and temperature using Rietveld analysis or Le Bail fitting methods.

- Determination of bulk modulus and thermal expansion coefficient using equation of state fit to the unit cell volume data as a function of pressure and temperature, respectively.

- Systematic investigation of frequency shift with pressure to determine the boundary of phase transition in the Raman spectroscopy results.

- A comparison of the properties of hydrides to find any interrelationship among them.

- The investigation of correlation among the properties of hydrides with the help of principal component analysis.

- Investigation of mixtures 2AlH3+ MgH2 and 3MgH2+ Si under pressure and temperature as a route to synthesize complex hydrides.

The discussion of this work is divided into different chapters in the dissertation which include introduction, literature review, experimental procedures, results and discussion of each hydrides selected for the study, conclusions and recommendations for future research. The first pages of the publications arising out of this research work are included in the appendix.

# CHAPTER 2. LITTERATURE REVIEW

Metal can absorb H2 until it attains equilibrium and the reaction rate is a function of pressure and temperature. In most cases, a structural transformation occurs when the material absorbs H2 due to isotropic cell volume expansion. Hydrogen desorption from hydrides may proceed through thermal decomposition of the hydride at the hydride-metal interface, interstitial diffusion of hydrogen through metal phase, surface penetration of hydrogen atoms, recombination of chemisorbed hydrogen atoms and physisorption, and molecular hydrogen degassing [1].  Hydrogen sorption/desorption rate and corresponding activation energies depend on applied pressure, temperature, surface contamination, crystallite size and additives or catalysts. In most cases, the rate-limiting factor cannot be determined in a straightforward manner. It is believed that hydrogen desorption is not controlled by diffusion or any phase transformation, but by a process involving hydrogen transport through the surface. Minimum inter nuclear distance between H- atoms should be 2.1Å which limits the number of interstitial atoms. Therefore, in crystals only octrahedral and tetrahedral sites can be occupied by H-atoms.

A stronger H-M bond than the H-H bond implies chemisorption is exothermic and a stronger H-H bond as compared to H-M bond means chemisorption is endothermic. A solid solution is formed by penetration of H-atoms into the subsurface metal atomic layer through an activated process from which it can diffuse into the bulk of the metal. Kleperis et al. [2], have stated that the enthalpy (ΔH) of hydride formation should be between - 25 kJ mol-1 and - 50 kJ mol-1, for an alloy to be suitable for battery applications. When ΔH < –15 kJ mol-1, the alloy hydride is not stable enough for charging the metal hydride electrode at room temperature. For practical applications, hydrides should release hydrogen in the temperature range 60-120 ºC and pressure below 10 MPa. The operation temperature and pressure are related by the van’t Hoff equation;lnp= ΔHRT+ΔSR, where H and S are absorption/ desorption enthalpy and entropy, respectively. Heat of formation and decomposition of the hydrides are important to estimate the operation temperature and pressure. Hydrides are mainly classified into metal hydrides and complex hydrides depending on their bonding nature.

## Metal Hydrides

The light metal hydrides are good candidates for use as hydrogen storage materials. Alkali and alkali- earth metal hydrides have good hydrogen storage capacity (> 12.6 wt %) but their operation temperature is very high, while transition metal hydrides release H2 at room temperature but with less storage capacity (< 2.5 wt %). Therefore, it is important to study thermodynamic stability of metal hydrides in order to understand possibilities to improve their temperature of operation. The hydrogen storage capacity and decomposition temperature for various alkali and alkali-earth metal hydrides are listed in Table 2.1. Metal hydrides can be synthesized directly from corresponding metals under high hydrogen pressure because of increased hydrogen solubility [3-8]. Bonding in metal hydrides can be ionic (eg. alkali metal hydrides), covalent (eg. AlH3, CuH etc.) or metallic (eg. transition metal and rare earth metal hydrides). The alkali metal hydrides have high degree of ionic nature (i.e. the electrons are localized around the atomic nuclei) and thus high decomposition temperatures.

Table 2. 1: Weight, gravimetric (wt %) and volumetric (kg/m3) hydrogen contents and decomposition temperature of alkali and alkali- earth metal- hydrides.

| Hydride | Weight (g/mol) | H (wt%) | H (kg/m3) | Td [9] (ºC) |
| --- | --- | --- | --- | --- |
| LiH | 7.95 | 12.59 | 98.60 | 720 |
| NaH | 23.99 | 4.17 | 57.73 | 425 |
| KH | 40.11 | 2.49 | 36.01 | 417 |
| RbH | 86.47 | 1.18 | 30.44 | 170 |
| CsH | 133.91 | 0.75 | 25.86 | 170 |
| BeH2 | 11.01 | 18.16 | 138.08 | 250 |
| MgH2 | 26.31 | 7.60 | 110.03 | 327 |
| CaH2 | 42.09 | 4.75 | 92.37 | 600 |
| SrH2 | 89.62 | 2.23 | 74.00 | 675 |
| BaH2 | 139.34 | 1.44 | 60.41 | 675 |

The alkaline earth metal hydrides include BeH2 with covalent bonding character (due to a small difference in electro-negativity between beryllium and hydrogen) and ionic hydrides of CaH2, SrH2, and BaH2 [9-11]. But MgH2 is having a more complex bonding character. Generally the electronic density is located around the atoms with a net charge of Mg close to +2 and H atoms with a charge of -0.94 to -0.26 [12, 13]. The remaining electron density is distributed evenly in the interstitial region. The recent experiments have revealed regions with increased electron density between Mg and H atoms clearly suggesting a partial covalent bonding character to MgH2 [12]. At ambient conditions except Be and Mg, all other alkali and alkali-earth group metals have cubic structure (Table 2.2). Both Be and Mg crystallize in the hexagonal close packed (hcp) structure but transforms into an orthorhombic structure and a tetragonal structure, respectively, for the corresponding hydrides. Due to lower atomic packing density compared to the close packed hosts the density of the hydrides of Be and Mg are lower than the metals. Ca, Ba, and Sr all have cubic crystal systems and their hydrides have orthorhombic structures [13, 14].

| Metal | Structure/ space group | K0 (GPa) [15] | K′0 |
| --- | --- | --- | --- |
| Li | Cubic/ Im‾3m | 11.6 | 3.51 |
| Na | Cubic/ Im‾3m | 6.3 | 4.13 |
| K | Cubic/ Fm‾3m | 3.1 | 3.91 |
| Rb | Cubic/ Im‾3m | 2.5 | 3.62 |
| Cs | Cubic/ Fm‾3m | 1.57 | 3.79 |
| Be | Hexagonal/ P63/mmc | 100.3 | - |
| Mg | Hexagonal/ P63/mmc | 45 | 4.8 |
| Ca | Cubic/ Fm‾3m | 15.2 | 2.5 |
| Sr | Cubic/ Fm‾3m | 11.61 | 2.5 |
| Ba | Cubic/ Im‾3m | 9.6 | 2.1 |

Table 2. 2: A comparison of structure and bulk modulus values of alkali and alkali- earth metals.

The hydrides of the alkali- earth metals are insulators with band gaps in the range 3-6 eV for Be, Mg, and Ca [11, 13, 14]. Alkali metal hydrides have cubic structure similar to the metals, and except MgH2 (tetragonal) all other alkali-earth metal hydrides exist in orthorhombic structure. A comparative study of properties of metal and corresponding hydrides suggests decrease or increase of entropy, molar volume and specific heat of hydrides from that of the metals can be attributed to hydrogen bond formation, charge transfer and corresponding change in crystal structure [16]. Metal hydrides are not considered as practical hydrogen storage material as such, due to their stability arising from ionic bonding. Both additives and processing like ball milling are found to be improving the kinetics of the hydrides [17-21].

## Complex Hydrides

Binary metal hydrides of the alkali metal and alkali earth metal hydrides do not fulfill the hydrogen storage requirement of operation temperature below 120 ºC. To achieve potentially improved thermodynamics it is necessary to form complex hydrides with addition of Al, B etc., to alkali or alkali earth metal hydrides. Complex hydrides are salts in which molecular anions contain hydride ions. Complex metal hydrides recently got much notice as a promising material due to their high hydrogen storage capacity and lower production costs. The hydrogen storage capacities, possible decomposition reaction and corresponding temperatures are listed in Table 2.3. Alanates are less stable than corresponding borohydrides and the decomposition temperature increases as size of metal increases from Li to Cs for alkali borohydrides.  Also, B-H bond energy is larger than the Al-H bond energy [22]. Due to strong covalent and ionic bonding nature, dissociation temperatures of borohydrides are very high. The improvement of the hydride properties by catalytic addition requires better understanding of the phases and their structural stability.

Nature of chemical bonds in the complex hydrides of the form MXHn, eg. NaAlH4, LiBH4, LiNH2 etc., was computationally studied by Yoshino et al.  [22]. Their results show covalent bonding between X and H ions in the [XHn]- complex which in turn has an ionic bonding with the metal ion M+. Computational studies of Mg(AlH4)2 show the bonding within [AlH4]- complex involves hybridization between Al and H orbital but with a strong ionic character [23]. The destabilization of alkali alanates by Ti is reported to be caused by the rearrangements of the tetrahedral [AlH4]- ion into octahedral [AlH6]3- ion [24]. Complex hydrides are good solid electrolytes because of their high ionic conductivity [25].

Table 2. 3: Weight, gravimetric (wt %) and volumetric (kg/m3) hydrogen content, decomposition reaction and corresponding temperature of alkali and alkali- earth complex hydrides.

| Hydride | Wt (g/ mol) | H Wt % | H (kg/ m3) | Decomposition reaction | Td (ºC) | ref. |
| --- | --- | --- | --- | --- | --- | --- |
| LiAlH4 | 37.95 | 10.55 | 74.02 | 3LiAlH4 Li3AlH6+2Al+3H2 Li3AlH63LiH +Al +3/2H2 3LiH 3Li + 3/2H2 | 112 127 720 | [26] |
| NaAlH4 | 53.97 | 7.41 | 97.41 | 3NaAlH4Na3AlH6+2Al+3H2 Na3AlH63NaH +Al +3/2H2 3NaH 3Na + 3/2H2 | 220 250 425 | [27-29] |
| KAlH4 | 70.08 | 5.71 | 70.31 | 3KAlH4 K3AlH6+2Al+3H2 K3AlH63KH +Al +3/2H2 3KH 3K+ 3/2H2 | 300 340 417 | [30] |
| RbAlH4 | 116.45 | 3.44 | 124.4 |  |  |  |
| CsAlH4 | 163.88 | 2.44 | 108.9 |  |  |  |
| Be(AlH4)2 | 71.04 | 11.35 | -- |  |  |  |
| Mg(AlH4)2 | 86.3 | 9.27 | 98.15 | - Mg(AlH4)2MgH2+2Al+3H2 MgH2Mg+H2 2Al+Mg1/2Al3Mg2 +1/2Al b. Mg(AlH4)2→MgAlH5+Al+1.5H2 MgAlH5+Al→MgH2+2Al+1.5H2 | 110–200 240–380 400 120–155 210–255 | [31, 32] |
| Ca(AlH4)2 | 102.04 | 7.84 | 96.97 | Ca(AlH4)2CaAlH5+ Al + 3/2H2 CaAlH5CaH2+ Al + 3/2H2 CaH2Ca + H2 | 200 260–550 600–700 | [33] |
| Sr(AlH4)2 | 149.65 | 5.39 | -- |  |  |  |
| Ba(AlH4)2 | 199.36 | 4.044 | -- |  |  |  |
| LiBH4 | 21.75 | 18.39 | 124 | LiBH4→ LiH + B + 3/2H2 | 400 | [34] |
| NaBH4 | 37.81 | 10.58 | 118 | NaBH4 → Na + B + 2H2 | 565 | [35] |
| KBH4 | 53.90 | 7.42 | 85.57 |  | 500 | [9] |
| RbBH4 | 100.28 | 3.99 | 77.2 |  | 600 | [9] |
| CsBH4 | 147.72 | 2.71 | 65.66 |  | 660 | [9] |
| Be(BH4)2 | 38.69 | 20.84 | 126.9 | Be(BH4)2→ Be + 2B + 4H2 |  | [36] |
| Mg(BH4)2 | 53.93 | 14.84 | 117.2 | Mg(BH4)2 MgH2+ 2B+3H2 MgH2 Mg+H2 | 290 317 | [37, 38] |
| Ca(BH4)2 | 69.70 | 11.48 | 124.0 | Ca(BH4)2 CaH2+ 2B+3H2 CaH2 Ca+H2 | 347-497 | [39] |
| Sr(BH4)2 | 117.24 | 6.88 | -- |  |  |  |
| Ba(BH4)2 | 166.95 | 4.79 | -- |  | 375 | [9] |

## Equations of State

The phase change in solids at high pressure usually involves a change in crystal structure or in the atomic arrangements. Co-ordination number (z) is important in the high pressure studies of phase transition. This is because; thermodynamically the molar volume of high pressure phase must be smaller than that of the low pressure phase. The reduction in molar volume is achieved either by a more efficient packing of co-ordination polyhedra or by an increase in co-ordination number or by both. Theoretically all materials become metallic at extremely high pressures. A variation in pressure (P), temperature (T) or composition (x) can cause a phase transition in materials. In solid- solid phase transformations, generally T and P remain constant while entropy (S) and molar volume (V) undergo finite changes [40]. Phase transitions involve change in entropy and volume (ΔSt and ΔVt) according to the Clapeyron equation (Eq. 1).

(1)

This equation implies that phase transition is induced either by a change in T at constant P or by a change in P at a constant T. In the first order phase transitions the value of ΔSt for temperature induced transition must be positive, where as ΔVt may be any value. While for pressure induced transitions as P increases ΔVt must be negative but there will not be any restriction on the values of ΔSt. In the case of second order phase transitions, phase changes occur at constant P and T with no volume or entropy changes. Both first and second order phase transitions must exhibit finite changes in the heat capacity (Cp), compressibility (β) and thermal expansion (α) which is expressed by the Ehrenfest’s equation (Eq. 2)

(2)

Past few years, researchers have attempted to reveal the properties of materials in terms of universal relationship with minimum parameters. A fair knowledge of the behavior of thermodynamic parameters at elevated pressure is significant for devising a system independent equation of state (EoS) of materials. A mathematical expression defining the physical state of homogeneous material which relates thermodynamic parameters P, V and T is referred to as an EoS.

### 2.3.1. Pressure equations of state

When the applied pressure is high, the number of nearest neighbor atoms increases as the core repulsions dominates which results in efficiently packed structures. At equilibrium volume the Madelung energy gives the dominant contribution to the total energy [41]. The change in volume during the phase transition can be computed if the EoS for the state is known. EoS can provide analytical expressions for cohesive energy which is an important thermodynamic parameter. EoS is widely applied in engineering and scientific research to get information on non-linear compression of materials at high pressure.   During the last few decades, much work has been carried out to determine an EoS which uses volume as a function of pressure and thus obtain the various energies directly as a function of pressure and temperature for thermodynamic calculations. It was a long awaited goal for researchers to find an EoS with the ability to predict compression curve of a material only using its compression properties at low pressures. Isothermal EoS comprises K0 (isothermal bulk modulus), K0′ and K0″ (first and second derivatives of K0 with pressure, respectively). The most commonly used EoSs for fitting isothermal P-V datasets are due to Murnaghan and Birch. The Murnaghan EoS [42] can be derived from the assumption that the bulk modulus varies linearly with pressure K= K0+ P.K0′, where K0′ being independent of pressure, integration of which yields the P-V relationship as given in Eq.3.

(3)

This EoS reproduces P-V data and yields correct values of the room pressure bulk modulus for compressions up to about 10% (i.e. V/V0 > 0.9), and has the advantage of algebraic simplicity over other formulations such as the Vinet or Birch- Murnaghan EoS [43], which should be used if the range of compression is greater than 10 %. Birch- Murnaghan EoS [44] is fairly good up to compressions of 0.85 (V/V0).  This is a finite strain EoS, and is based upon the assumption that the strain energy of a solid undergoing compression can be expressed as a Taylor series which on expansion to fourth-order in the strain yields the Eq. 4.

(4)

### 2.3.2. Thermal equations of state

The high-temperature value of the zero-pressure volume can be obtained by integrating the expression of thermal expansion coefficient (α) which gives Eq. 5.

V0(T) = V0(T0) exp ∫ α(T) dT							(5)

At the lowest level of approximation α(T) can be considered a constant, or varying linearly with temperature as α(T) = α0 + α1T.  From the temperature dependent α zero pressure volume obtained can be expressed as Eq.6.

V0(T) = V0(T0) exp [ α0 (T-T0) + (½) α1(T2-T02)]					(6)

In this case, the actual values of α0 and α1 that describe a V-T curve depend on the value of the reference temperature, T0. As per the experimental results the variation of bulk modulus with temperature is considered to be linear (Eq. 7) and can be used to fit most experimental P-V-T data sets up to around 725 ºC.

K(T) = K0 + (T-T0) (dK/dT)p							(7)

## Investigation of Hydrides under High- Pressure and Temperature

The structural investigations at different temperatures and pressures can help to identify various polymorphs of the material which may have better thermodynamics for hydrogen storage. X-ray diffraction, neutron diffraction and Raman spectroscopy are powerful tools to detect phase transition at elevated pressures and temperatures. Some complex hydrides like LiBH4 release H2 only above the transition temperature. In such cases it is important to understand the structural stability of high temperature phase to calculate its hydrogen desorption energy [45]. Diamond anvil cell technique is generally used to apply high pressure during in situ experiments. Equation of state fit of the unitcell volume data obtained from high temperature or pressure investigations can provide thermal expansion coefficient, bulk modulus etc., which in turn grant basis for the validation of theoretical models. Different crystal structures of metal hydrides are associated with different degrees of iconicity due to increase in coordination number with compression [46]. A comparison of change of molar volume of metal with metal hydride as a function of pressure can be used to determine compressibility of hydrogen in the host [47].

The crystal structure data for alkali and alkali-earth metal hydrides are tabulated in Table 2.4. From Tables 2.2 and 2.4, it is clear that the bulk modulus of alkali and alkali earth metals are lower than that of their hydrides, suggesting a hydrogen induced hardening of these materials. The lower bulk modulus (high compressibility) observed for alkali metal hydrides as compared to the corresponding halides can be due to partial charge transfer between metal and hydrogen atom [48]. X-ray scattering power of hydrides is very weak and hence atomic positions of hydrogen are determined with neutron diffraction or computation. Alkali hydrides show a phase transition at low pressures with 8-13 % volume change and the transition pressure increases with radius of corresponding metal ion [49]. Addition of elements of low atomic weight such as Si, Al, B, C, N, P, S etc., or an appropriate hydride at desirable stochiometry could destabilize metal hydrides without reducing much storage capacities [50].

Complex hydrides show a number of phase transitions with pressure and temperature which are summarized in Tables 2.5 and 2.6. The transition pressure is found to be independent of size of metal atoms in complex hydrides unlike the metal hydrides. Alanates and borohydrides have high compressibility with the bulk modulus range 5- 31 GPa, which suggest possible destabilization under pressure. Except LiAlH4 (monoclinic) and NaAlH4 (tetragonal), alkali alanates are of orthorhombic symmetry. Similar to the metals, ambient phase of alkali borohydrides exist in cubic symmetry except LiBH4 which has an orthorhombic structure.

Table 2. 4: A comparison of transition pressure, temperature, structure and bulk modulus data of alkali and alkali- earth metal hydrides. The data marked * is from computation results and others are experimental values.

| Hydride | P (GPa) | T(ºC) | Structure/Space group [ref.] | K0 (GPa) | K′0 |
| --- | --- | --- | --- | --- | --- |
| LiH | 0-660 >660* | 25 25 | Cubic/ Fm‾3m [51, 52] Cubic/ Pm‾3m [53] | 34.7 31 * | 0.016 |
| NaH | 0-29 >29 | 25 25 | Cubic/ Fm‾3m [48] Cubic/ Pm‾3m | 19.4 28 | 4.4 4.3 |
| KH | 0-4 >4 >176 * | 25 25 25 | Cubic/ Fm‾3m [54] Cubic/ Pm‾3m Orthorhombic/cmcm [41] | 15.6 28.5 | 4 4 |
| RbH | 0-2.2 >2.2 >35 * | 25 25 25 | Cubic/ Fm‾3m [55] Cubic/ Pm‾3m Orthorhombic/cmcm [41] | 10 18.4 | 3.9 3.9 |
| CsH | 0-0.83 1.2-17.5 >17.5 | 25 25 25 | Cubic/ Fm‾3m [56] Cubic/ Pm‾3m [57] Orthorhombic/ cmcm [46] | 8, 7.6 14.2, 22.3 - | 4 4,4.8 - |
| BeH2 |  | 25 | Orthorhombic/ Ibam [58] Amorphous [59] | 24.7 14.2 | 3.9 5.3 |
| MgH2 | 0-5.5 5.5-9.5 9.3-10.4 >10 0 2 | 25 25 25 25 >300 >800 | Tetragonal/ P42/mnm [60] Orthorhombic/ Pbcn Cubic/ Pa‾3 Orthorhombic/ Pbca Tetragonal [60] Orthorhombic | 45 44.03 47.41 49.83 | 3.35 3.49 3.17 3.49 |
| CaH2 | 0-16 15.5-21 >138 * | 25 25 25 | Orthorhombic/ Pnma [61, 62] Hexagonal/ P63/mmc [62, 63] Hexagonal/ P63/mmm [64] | 190 *, 40.7 63.6 | 4.5 3.24 |
| SrH2 | 0-8.3 8.3-113 >113 | 25 25 25 | Orthorhombic/ Pnma [65] Hexagonal/ P63/mmc Hexagonal/ P63/mmm | 57, 41.4 * 75, 42.3 * 39* | 3.13 3.87 3.92 |
| BaH2 | 0-2.5 2.5-50 >50 | 25 25 25 | Orthorhombic/Pnma [66, 67] Hexagonal/ P63/mmc [68] Hexagonal/ ? | 31.2*, 24 34.7 * | 3.2 3.6 |

Table 2. 5: A comparison of transition pressure, temperature, structure and bulk modulus data of alkali and alkali- earth alanates. The data marked * is from computation results and others are experimental values.

| Hydride | P (GPa) | T(ºC) | Structure/ space group [ref.] | K0 (GPa) | K′0 |
| --- | --- | --- | --- | --- | --- |
| LiAlH4 | 0-2.16 >3 >34 7 7 | 25 25 25 >300 >500 | Monoclinic/ P21/c [69, 70] Tetragonal/ I41/a [69] Orthorhombic/ Pnma [71] Tetragonal Orthorhombic/Pnma [72] | 13.87,12.9 * 25.64 * 14.25 * | 4,4.1 4.35 4.85 |
| NaAlH4 | 0-14 >6.4 >14 | 25 25 25 | Tetragonal/ I41/a [73] Orthorhombic/ Cmc21* [74] Monoclinic/ P21/c | 27 | 5 |
| KAlH4 | >0 | 25 | Orthorhombic/ Pnma [75, 76] | 10.34 * | 4.61 |
| RbAlH4 | >0 >xx | 25 25 | Orthorhombic/ Pnma [76] Orthorhombic/ Cmc21 | 9.2 * 14.1 * | 5.2 3.5 |
| CsAlH4 | >0 >x >xx | 25 25 25 | Orthorhombic/ Pnma [76] Tetragonal/ I41/a [26] Orthorhombic/ Cmc21 | 8.6 *, 8.22 * 9.5 * 9.1 * | 4.6, 5.2* 5.1 4.9 |
| Mg(AlH4)2 | 0-0.67 0.67-10.3 >10.3 | 25 25 25 | Trigonal/ P‾3m1 [77, 78] Monoclinic/ C2/m Orthorhombic/ Pbca | 10.9 *, 9.2 * 6.8* 34.7* | 5.7 |
| Ca(AlH4)2 | >0 | 25 | Orthorhombic/ Pbca* [33] |  |  |

High pressure phase transitions of alkali-metal borohydrides are found to be first-order and fully reversible. Therefore, it is interesting to study structural behavior of metal borohydrides under various conditions of pressures and temperatures. MBH4 (M = Na, K, Rb, Cs) compounds show a similar structural phase transition with respect to temperature. At high temperature they crystallize into NaCl-type structures, in which BH4− is octahedrally surrounded by M+. The H atoms in a BH4− unit are tetrahedrally oriented about B and along all cube diagonals. This gives a random distribution of BH4− tetrahedron in two different configurations.

Table 2. 6: A comparison of transition pressure, temperature, structure and bulk modulus of alkali and alkali- earth borohydrides. The data marked * is from computation results and others are experimental values.

| Hydride | P (GPa) | T(ºC) | Structure/ Space group [ref.] | K0 (GPa) | K′0 |
| --- | --- | --- | --- | --- | --- |
| LiBH4 | 0-0.8 1.1-10 >2.4 >10 0 0 | 25 25 25 25 111 -48 | Orthorhombic/Pnma [79-81] Monoclinic/ P21/c [79] Tetragonal/Ama2 [82] Cubic/ Fm‾3m [79] Hexagonal/ P63mc [83] Orthorhombic/ Pnma [45, 82] | 14.4, 15 * 23.23 26 | 3.5 3.5 3.5 |
| NaBH4 | 0-6.3 6.3-8.9 8.9-14 >14 0 6.5 9.5 | 25 25 25 25 <-83 >100 >150 | Cubic/ Fm‾3m [84, 85] Tetragonal/ P‾421c Orthorhombic/ Pnma Monoclinic/ P21/c [86] Tetragonal / P‾421c Cubic/ Fm-3m [86] Tetragonal / P‾421c | 19.9, 18.76 30.6 * 31.1 | 3.5, 3.48 3.9 |
| KBH4 | 0-3.8 3.8-6.8 >6.8 0 | 25 25 25 -197 | Cubic/ Fm‾3m [87] Tetragonal/ P‾421c Orthorhombic/ Pnma Tetragonal/ P42/nmc [88, 89] | 16.8 | 4 |
| RbBH4 | 0-2.5 2.5-8 >8 0 | 25 25 25 -229 | Cubic/ Fm‾3m [90] Orthorhombic/ Pnma Monoclinic/ P21/c Tetragonal [88] | 14.5 | 4 |
| CsBH4 | 0 >x >xx 0 | 25 25 25 -246 | Cubic/ Fm‾3m [91] Tetragonal/ P‾421c Orthorhombic/ P42/nmc Tetragonal [88] | 5.2 * 10.4 * 5.3 * | 5.9 4.9 5.9 |
| Be(BH4)2 | 0 | 25 | Tetragonal/ I41cd [36, 92] |  |  |
| Mg(BH4)2 | 0 0-2.5 2.5-14 >14 0 | 25 25 25 25 >180 | Orthorhombic/Pmc21 [78] Hexagonal/ P6122 [93] Hexagonal/ P63 [94] ? unidentified Orthorhombic/Fddd [95] | 7.82 * 10.16 | 5.2 4 |
| Ca(BH4)2 | >0 0-10.2 0 0 0 0 | 25 25 <-182 >32 >222 >207 | Orthorhombic/ F2dd [96, 97] Tetragonal/ P42/m Orthorhombic/F2dd [96] Tetragonal / P‾4 Tetragonal / I‾42d Tetragonal / P42/m [98] | 22.95 | 2.63 |

In the case of MBH4 (where M is an alkali metal), as the cation size increase from Li to Cs the unit cell expands and H-H bond length increases. Therefore the H-H repulsion will be weaker in heavier MBH4 which results in reduction of cubic to tetragonal transition temperature or increase in corresponding transition pressure [99]. The high pressure structural behavior of alkali borohydrides is widely investigated. Nevertheless, the high pressure structural data of alkali-earth alanates and borohydrides are scarce owing to their high reactivity and difficulty to synthesize.

## Applications of Hydrides

Hydrides are important materials both for possible use in transportation and for nuclear industry. The use of metal hydrides and borohydrides as advanced shielding materials in nuclear power plants is well known [100]. Examples are Mg(BH4)2, TiH2 and ZrH2 which can reduce the thickness of the outboard shield by 23, 20 and 19 %, respectively, compared to the combination of steel and water. Hydrides have a variety of applications as listed below [101].

- Electrochemical (rechargeable batteries, catalysis, fuel cells)

- Thermal (heat storage, refrigeration, heat engine/ actuator, heat pumping)

- Nuclear industry (fuel cladding, neutron shielding and reflection, fuel-moderator)

- Sensors and optical switch

- Hydrogen processing (purification, isotope separation, compression)

To power a fuel cell, a metal hydride has remarkable advantages in regard to cryogenic or pressure storage tanks as it does not require additional power supply, there is no loss, and hydrogen can be safely supplied at an optimum and constant pressure. Main issue in using complex metal hydrides is the difficulty in thermal management during refueling because of the reaction enthalpies involved. The advantage of using a fuel cell system is that the dehydrogenation of complex hydrides does not require water [102].

# CHAPTER 3. EXPERIMENTAL TECHNIQUES AND DETAILS

## 3.1. Diamond Anvil Cell Technique

The diamond anvil cell (DAC) is a portable high pressure device which use the force applied to a smaller area to maximize the pressure generated. Table 3.1 summarizes the devices with which ultra high pressures can be applied in the laboratory setting. With the help of external or internal heaters it is possible to study properties of materials under both pressure and temperature in these devices. The DAC technique is based upon the opposed-diamond configuration, in which a sample is placed in the hole of a gasket (metal, rhenium, graphite etc.) inserted between the polished culets of two diamonds.  With this configuration, very small force can create extremely large pressures on the sample.

Table 3. 1: High pressure apparatuses and pressure- temperature ranges that can be achieved using each of them.

| Method | Pressure P (GPa) | T (°C) |
| --- | --- | --- |
| Gas apparatus | 3 | 1500 |
| Piston- cylinder | 5 | 2000 |
| Bridgman anvils | 20 | 2000 |
| Belt apparatus | 20 | 2000 |
| Multi anvil press | 30 | 2500 |
| DAC | 200 | 2000 (resistive) 4000 (laser) |
| Shock wave | 800 | 5000 |

Because the diamonds are transparent to most part of the electromagnetic spectrum (X-rays, gamma rays, UV, IR, visible light etc.), the sample may be examined in situ by spectroscopic and diffraction techniques. Different types of DACs generally used are Merril- Baset, P series, Mao- Bell, compact cylinder cell, and four post high pressure cells. Figure 3.1 shows a loaded Mao- Bell type DAC and a schematic of the sample chamber in DAC.

- (b)

Figure 3. 1: a) A loaded Mao- Bell type DAC;  b) schematic of the sample chamber in a diamond anvil cell, 1- diamond, 2- gasket hole, 3- sample, 4- gasket, 5- ruby chip.

Compressive strength, hardness, and transparency to a wide electromagnetic spectrum are the main properties of diamond that make it a good choice for anvils. Two of the most important properties of a material are crystal structure and lattice parameters that can be used for determining basic thermodynamic quantities, such as the effect of pressure and temperature on molar volume. X-ray diffraction using DAC is the best tool for such studies as the building block of diamond, the C atoms, has low atomic number and hence low absorption. DACs can also be used for a number of investigations using IR, UV, gamma rays, sound waves etc., because of the extraordinary optical and elastic properties of diamonds [103]. Insertion of a gasket between the diamonds of the DAC helps to encapsulate a hydrostatic pressure medium, also to carry out viscosity measurements, chemical reactions, and structure determinations of molecular species in solution.

### 3.1.1. Measurement of pressure in a DAC

The pressure in the DAC can be measured by an embedded pressure marker or ruby (Cr3+ doped Al2O3). A  material of known pressure- volume EoS such as NaCl, MgO, Pt, Au, W, Ag, Cu etc., are generally used as pressure marker. If the pressure marker is mixed with sample, the lattice parameters can be obtained by X-ray diffraction which in turn can be used in ‘calibration’ software to determine pressure.  Ruby pressure scale is a faster method to measure pressure in the DAC experiments. Ruby has a series of spectral bands (R, U, B and Y) in the visible ranges. The high energy lines U, B and Y can be excited by a laser and they relax to R lines. The R lines (R1 and R2 with wave lengths 694.2 and 692.8 nm, respectively at ambient conditions) are metastable with long lifetime which shift to higher wave length under pressure (Figure 3.2), and relax to ground state by fluorescence. The ruby method is not suitable for measuring pressure at high temperatures, because of the shift and fading away of the fluorescence signal with temperature. Metal pressure markers such as Pt are chemically inert and scatter X-rays efficiently, and the effects of both pressure and temperature on lattice dimensions are well known. Another method good for high temperature pressure measurement is fluorescence of a samarium doped compound (SrB4O7:Sm 2+). In the present study, both ruby and NaCl are used for pressure measurement in high pressure- temperature experiments.

Figure 3. 2: The shift of ruby fluorescent spectrum with the application of a pressure of 4.4 GPa.

Mao et al. [104], carried out the calibration of the pressure shift of R1 emission line of ruby up to 80 GPa under quasi hydrostatic conditions with argon gas as a pressure transmitting medium. The shift of R1 line with pressure was found to be linear with pressure about 0.274 GPa Å–1 and can be fitted to the formula; P(GPa) = (A/B)[(λ/λ0)B-1]  where A =1904 GPa, B = 7.665, λ is the wavelength of R1 line at pressure P and λ0 is that at ambient conditions. Later, with helium as pressure medium Silvera et al. [105], calibrated the ruby pressure gauge up to 150 GPa with a difference in A and B parameters. The pressure can be determined from the reduced equation using change in wave length of R1 line; P = Δλ/0.365 where P is in GPa. Reduction in the X-ray beam divergence and collimation diameter (~0.15 mm) can be useful to minimize the effect of pressure gradients in the compressed sample. The ruby fluorescence is recorded using a USB based fluorescence spectrometer (Ocean Optics) and the operating software-OOIBase32.

### 3.1.2. Sample loading in the DAC

All sample handlings were carried out in an argon atmosphere. Mao-Bell type DAC with diamonds of 0.4-0.5 mm culets and stainless steel (T302) gasket of 0.18-0.21 mm hole was used. Steel gaskets were of thickness 0.27-0.32 mm and were indented to 0.05-0.07 mm using the DAC before drilling hole. A motorized electric discharge machine from BETSA is used to drill holes in the gaskets (Figure 3.3). The principle used for drilling is the spark erosion in which a high voltage spark erodes the metallic gasket immersed into a dielectric liquid like isopropanol. For medium and high pressures steel and rhenium gaskets, respectively are good. At high pressures, all materials can develop shear strength leading to non hydrostatic conditions. Fluids like helium, hydrogen, xenon etc., are used to create quasi hydrostatic conditions. For pressures less than 15 GPa, a 4:1 methanol: ethanol mixture and silicone oil are found to be effective. In heating experiments, a resistive ring-heater and specially designed thermocouples were employed around diamond culets. The outer surface of the DAC was cooled by water circulating setup or argon gas.   To accurately measure the pressure, both NaCl and ruby chips were added to the sample in the high temperature experiments. Measurements were conducted with and without a pressure transmitting medium (silicone oil or mineral oil) and observed highly non hydrostatic behavior above 12 GPa in both cases because of their solidification under pressure. In the heating experiments no pressure transmitting medium was used. Because of high refractive index of diamonds in DAC, a correction has been carried out on the diffractometer stage or goniometer to obtain accurate sample position.

Figure 3. 3: Drilling machine which is employed to drill holes in the gaskets using spark erosion method.

### 3.1.3. Resistive heating in a DAC

For high temperature study under pressure, samples in DAC can be electrically heated with a ring heater placed around the anvils or wrapping resistance wires around the diamond supports. A specially designed gasket also can be used as a heater [106]. Resistive heaters can provide temperatures up to 1000 ◦C. Thermocouple attached to diamond surface is the most satisfactory way to measure temperature because of its high thermal conductivity.  In the present study, a ring type heater consisting of pyrophilite (AlSi2O5OH) disc wounded with nickel-chromium (nichrome) wire of resistance about 6 ohm was placed around diamonds with proper insulation. Specially designed K-type (Ni-Cr/ Ni-Al) thermocouple junction was employed close to the diamond culet, which in turn connected to a temperature controller and DC power supply of ~30V. The thermocouple used is good to measure temperatures in the range -270 to 1260 ◦C.

## 3.2. X-Ray Diffraction Techniques

### 3.2.1. Powder X-ray diffraction

Powder X-ray diffraction (XRD) is an efficient tool to determine crystal structure of a material. The X-ray beam may be white having a broad spectrum (Laue) or monochromatic (Bragg) having essentially a single energy. The white beam can be used to produce diffraction patterns by the energy-dispersive (ED) method which analyzes energies (wavelengths) of X-rays scattered in a specific direction. Monochromatic radiation is used for angle dispersive (AD) method which has better resolution. The intensities around each diffraction ring can be integrated using computer processing with improved signal-to-noise ratio and accuracy.

In reflection (Bragg) geometry, data collection is confined within a plane. Only crystallites having reflection planes (hkl) parallel to the specimen surface will contribute to the reflected intensities. In powder or polycrystalline diffraction it is important to have a sample with plane surface. To obtain better diffraction, samples should be ground down to particle sizes of few microns and pressed into a sample holder such as quarts capillary. With a 2D diffraction detection in transmission geometry, a large portion of the diffraction rings (Debye ring) can be measured simultaneously. The 2D pattern can be analyzed after integrating which gives better intensity and statistics for phase identification and quantitative analysis.

Table 3. 2: Different information available from the condition of Debye rings in a 2D X-ray diffraction experiment.

Debye diffraction rings Condition of the sample

Continuous Fine grained

Spotty Coarse grained

Narrow Strain free

Broad Residual stress, small particle size

Uniform intensity Random orientation

Non uniform intensity Preferred orientation

In a diffraction pattern, unit cell determine the line positions and atomic positions attribute to the line intensity. Low symmetry crystals like triclinic have more lines in powder XRD pattern than a more symmetric system like cubic, due to introduction of new plane spacing by non uniform distortion. Therefore a new peak at high pressure or temperature experiments implies low to high symmetry transition. And, disappearance of a peak means low to high symmetry transition; for example orthorhombic to tetragonal. Sample orientation has no effect on profile from 2D frame. A 2D diffraction pattern contains more information than the conventional pattern (2θ versus intensity) for applications such as phase identification, percent of crystalline phase, particle size and shape, texture and stress as summarized in Table 3.2. In order to get beam center and detector distance accurately, a powder pattern should be acquired with standards like CeO2, LaB6, Si, Al etc. Lattice parameters as a function of pressure or temperature can be obtained by the Rietveld analysis of the diffraction pattern.

### 3.2.2. Synchrotron X-ray source

Hydrides are light materials with low scattering power. Furthermore, the use of DAC limits the amount of sample we can use. To resolve dynamic structural data, good quality diffraction patterns are required which can be obtained using a synchrotron XRD. A high-energy synchrotron source produces a very intense, small, and well collimated beam of X-rays with high resolution which can be used to study small samples such as in a DAC. Synchrotron X-rays are electromagnetic (EM) radiation generated by accelerating electrons. The high-energy electron beam is directed into auxiliary components such as bending magnets and insertion devices (undulaters or wigglers) in storage rings and free electron lasers. This generates strong magnetic fields perpendicular to the beam which helps to convert the high-energy of electron into an EM radiation. Finally, the radiation is projected at a tangent to the electron storage ring and captured by beam lines. The beam lines can be at the bending magnets located at the corners, or insertion devices placed in the straight sections of the storage ring and both types have different spectrum and energy.  A beam line includes optical devices (slits, attenuators, crystal monochromators, and mirrors) which control the bandwidth, photon flux, beam dimensions, focus, and collimation of the X-ray beam. At the end of the beam line is an experimental station, where the samples are placed in the line of the radiation and detectors (image plate or charge-coupled device) are positioned to measure the resulting diffraction. Figure 3.4 shows a schematic diagram of the X-ray diffractometer having transmission (Laue) geometry. Both white and monochromatic beams are valuable for diamond anvil cell studies. To collect a reasonably good diffraction pattern from DAC when using light hydrides, longer exposure time is required. In such cases, use of large sized image plates is preferred to get better resolution and to avoid dark current accumulation.

Figure 3. 4: Schematics of an X-ray diffractometer with transmission geometry; adapted from X17C hutch at NSLS [107].

The high pressure and temperature XRD measurements were mainly conducted at different beam lines of national synchrotron facilities. The diffracted X-rays were collected using Mar345 image plate detector. The display and control soft wares were based on MEDM, Java, and IDL. The beam resolution was 10-4. Calibration of the sample position and detector distances was carried out using CeO2 standard.  The synchrotron facilities used were;

- Sector 16-IDB, HPCAT, Advanced Photon Source of Argonne National Laboratory using X-rays of wavelength ~ 0.3681 Å (Figure 3.5). Source: Undulator.

- X17C beam line at NSLS, Brookhaven National Laboratory with facilitating radiation of λ = 0.4066 Å. Source: Superconducting wiggler.

- Station B2 of Cornell high energy synchrotron source (CHESS) in Cornell University with facilitating radiation of wavelength, λ = 0.49594 Å. Source: Bending magnet.

- X17B2 beam line of National Synchrotron Light Source in Brookhaven National Laboratory (energy- dispersive, 2θ = 6.4762º). Source: Superconducting wiggler.

### 3.2.3. Rotating anode X-ray generator

Electrons emitted from a heated cathode  is accelerated by an electric field and collide with the anode target metals like tungsten, molybdenum or copper, and accelerate other electrons, ions and nuclei within the anode material. Most of the kinetic energy contained in the electron beam is converted to heat which is dissipated via a heat sink, and about 1 % of the energy generated in the accelerated particles is emitted, usually perpendicular to the path of the electron beam, as X-rays.  At the electron focal spot, X-ray photons are emitted in all directions from the target surface, the highest intensity being around 60 to 90 degrees from the beam due to the angle of the anode target to the approaching X-ray photons. The generated beam is directed out the X-ray tube and projected on sample material which will be partially diffracted. The resulting diffraction pattern of the radiation is then detected by a medium including rare earth screens (which surround photographic film), semiconductor detectors, charge-coupled devices (CCDs) or X-ray image intensifiers. The advantage of rotating anode over stationary anode design is an effective increase in the area of anode target bombarded by accelerated electrons and hence the added brilliance. Figure 3.6 shows X-ray diffractometer at CeSMEC which consists of a rotating anode generator.

Figure 3. 5: The X-ray diffractometer stage at the beam line 16 IDB- HPCAT of Argonne National Laboratory.

A portion of the X- ray diffraction studies were carried out using Bruker- GADDS/D8 X-ray system with MacSci rotating anode of molybdenum (λ~ 0.71073 Å) and Apex Smart CCD detector. For heating experiments at ambient pressure, sample was loaded in quartz capillary and kept under vacuum overnight before sealing with Ar gas to avoid oxidation of the sample. A home- made heater coupled with temperature controller was used to heat the sample for in situ XRD experiments up to 500 oC. Temperature was calibrated from the thermal expansion of NaCl. The sample position was calibrated using LaB6.

### 3.2.4. Indexing of X-ray diffraction patterns

From angular position of diffraction lines, the unit cell parameters are deduced assuming crystal system from seven possibilities, and then assigning Miller indices (hkl) to each reflection. Number of atoms per unit cell can be computed from unit cell parameters, chemical composition and measured intensity. Position of an atom in the unit cell is determined from relative intensities of diffraction lines. In powder methods the wavelength used should not be shorter than K-absorption edge of the sample material to avoid fluorescence.  Shorter the wavelength, smaller will be the theta and therefore number of lines in the pattern will be more.

There are a number of factors affecting relative intensity of diffraction lines in a powder XRD viz; polarization factor, structure factor, multiplicity factor, Lorentz factor, absorption factor and temperature factor. Background radiation is caused by fluorescence from sample because of diffraction of continuous spectrum in the incident beam. The main causes are, diffuse scattering from sample like incoherent (Compton) scattering when the atomic size is small, coherent scattering due to temperature  in soft materials of low melting point, diffuse scattering due to crystal imperfections, diffraction and scattering from collimator, gasket, binder etc.

Figure 3. 6: A Bruker- GADDS/D8 X-ray system with molybdenum rotating anode X-ray generator at CeSMEC.

## 3.3. Raman Spectroscopy

Raman spectroscopy experiments were carried out with an argon ion (Ar+) laser system (Spectra Physics, model 177G02) of λ = 514.5 nm.  The Raman spectroscopy instrument used to conduct experiments which is equipped with a ruby fluorescence spectrometer is shown in Figure 3.7. Backscattered Raman spectra were collected by high throughput holographic imaging spectrograph (Kaiser Optical Systems, model HoloSpec ƒ/1.8i) with volume transmission grating, holographic notch filter and thermoelectrically cooled CCD detector (Andor Technology). The average spot size of the laser beam used is ~ 0.005 mm. The Raman spectrometer system has a spectral resolution of 4 cm-1 and the spectra were collected at an exposure of 600- 1800s depending on the sample.

Figure 3. 7: Raman spectroscopy setup with in situ ruby pressure measurement system at CeSMEC.

In Raman spectroscopy a light of known frequency and polarization is scattered from the sample which is analyzed for the frequency shift which is an intrinsic property of the sample. The classical vibrational frequency of a diatomic molecule is; ν = (1/2πc)(k/μ)1/2, where c is the velocity of light, k is the force constant and μ is the reduced mass of the constituting atoms. The Raman shift from incident laser frequency (ν0) is termed as Stokes (ν0– νm) and anti- Stokes (ν0+ νm) lines. The vibrational patterns of atoms and the polarization dependence of scattering are determined by the equilibrium structure of the material through the rules of group theory. The Raman shift is the change in the frequency of the scattered light from the laser frequency which implies that energy is deposited in the sample in the form of phonons. Because the Raman tensor also decomposes into the basis of irreducible representations of the crystal space group, phonons are also classified by their irreducible representation. Raman-active phonon modes can be classified according to the irreducible representations of the crystal space group and its orthogonality.

The laser beam from the argon ion laser is filtered to obtain a monochromatic beam which is directed by a system of mirrors to a focusing/collecting lens and focused onto the sample. The back scattered light from sample is then directed to the spectrometer through filters and gratings. The holographic notch filters allow collection of Raman scattered light closer to the Rayleigh line with less ripple. The holographic transmission gratings enable to acquire entire Raman spectrum simultaneously. The signal as a function of position is read by the system detector which is a multichannel CCD array in which the different positions (wavelengths) are read simultaneously. The wavelength-intensity information is then read to a computer and converted in Andor software to frequency shift versus intensity plots. To resolve a Raman peak of a certain width, the resolution of the spectrometer (final slit width) should be smaller than the peak width. The slit width determines the extent to which the image may shift along the face of the CCD array, and hence the frequency resolution. The dark current of CCD array is a function of the detector temperature which requires it to be cooled. In the present setup CCD is cooled by the use of Joule Thomson effect. When the apparatus is properly aligned, the intensity of Raman spectrum is a function of factors such as the applied laser power, the sample properties (how absorptive or reflective the sample is, and the intrinsic strength of the Raman modes), and the width of the slits.

## 3.4. Analysis of Powder X-ray Diffraction Data

### 3.4.1. Rietveld method

It is important to identify strongly overlapping reflections of the powder diffraction patterns to obtain crystal structure information. Rietveld refinement is a technique used to characterize crystalline materials. The height, width and position of the peaks can be used to determine many aspects of the materials structure. The Rietveld method uses a non linear least squares approach to fit or refine a model of crystal structure to the powder diffraction data. This analysis requires determining the structural parameters (unit cell dimensions, atom positions and displacement or thermal parameters) for all crystalline phases present, and a variety of instrumental and sample parameters (scale factors, peak broadening, background and preferred orientation). The analysis can be achieved with approximate starting values for all parameters that will be fitted. Then a computer program is used to optimize (refine) a subset of minimal number of parameters that must be fit. Finally, additional parameters are selected to be refined, until all parameters in the model which the data support are refined.

### 3.4.2. Le Bail method

Le Bail method can be used to get good experimental parameters for background, unit cell and profile before fitting structure. This method estimate best possible fit when profiles are irregular. Also an additional phase can be fitted with Le Bail method where structure is not known or where texture is a problem. The Le Bail method caused a marked and radical increase in the ability to solve structures from powder diffraction data. It includes the ability for whole profile unit cell refinement involving overlapping reflections, extraction of structure factors (|F|hkls) for crystal system and space group determination.

### 3.4.3. Data processing and analysis tools used in the study

The 2D angle dispersive diffraction patterns obtained were integrated using Fit2D [108]. Fit2D is a one and two dimensional data analysis program which can also be used for calibration and correction of detector distortions. GSAS (General Structure Analysis System) is a comprehensive system for the refinement of structural models to both X-ray and neutron diffraction data. The unit cell volumes were determined using Rietveld  analysis or Le Bail profile fitting method implemented in the GSAS-EXPGUI software package [109]. The GSAS package can be used with both single-crystal and powder diffraction data. EXPGUI is a graphical user interface (GUI) editor for GSAS experiment (.EXP) files and shell which allows all the other GSAS programs to be executed with a GUI. In addition to structure determination, GSAS is also used for lattice-constant determination even for materials with unknown structures, simulation of powder diffraction data, and for texture analysis [110, 111].

Plot85 is used to analyze energy-dispersive diffraction data created by the SAM85 or MCA data collection programs. In Plot85 it is possible to determine the channel number, energy, or d-space for any diffraction peak, either by pointing to the peak, or to fit it using GPLS (General Program for Least Squares fitting). If the diffraction data include that of  NaCl, the pressure and differential stress can also be calculated [112].

The experimental P-V data were fitted with third order Birch-Murnaghan equation of state using EosFit program [43, 113]. Except the Murnaghan, all other EoSs can be only written with pressure as a function of volume and not vice-versa. Therefore the EosFit program performs least squares fit of P-V data with pressure as the dependent variable. Uncertainties in volumes are converted into that of pressure by the effective variance method.  The value of V0 is dependent upon the calibration of the technique used to measure the volumes because the refinement of the diffraction pattern is influenced by the alignment of the monochromator, the resulting X-ray wavelength and the detector distance. Volumes measured at high pressures may be on a different scale from some high-accuracy value of V0 determined by another technique. Therefore, the fixing of V0 to an inappropriate value can lead to incorrect estimates of the other EoS parameters. For isothermal data sets, the first stage of refinement should be the refinement of V0 and K0 alone in a second-order EoS, with K′ is set to its implied value. 	Back ground subtraction and peak fitting were also carried out with Crystal Sleuth and CMPR software packages [114].  Visualization and manipulation of crystal structures were made possible using Powder Cell program [115]. The Raman spectra were fitted with Gaussian profile function in Fityk [116] to obtain Raman shift at different pressures. The correlations of properties of hydrides were studied with statistical package for social sciences (SPSS) program [117].

# CHAPTER 4. STRUCTURAL STABILITY OF Mg2FeH6 UNDER HIGH- PRESSURES AND TEMPERATURES

## 4.1. Introduction

Dimagnesium iron hydride (Mg2FeH6) is widely studied because of its possible application for hydrogen and thermo-chemical heat storage [118, 119]. Mg2FeH6 has the highest volumetric density of hydrogen (~ 150 kgH2 m-3) among all the hydrides investigated so far and has a gravimetric hydrogen density of 5.4 wt % H2.  Moreover, Mg2FeH6 is more economical for many applications compared to other hydrides because of the availability and the low cost of component metals Mg and Fe. The hydride has a K2PtCl6 type cubic structure with a space group of Fm¯3m, composed of tetrahedral Mg2+ ions and octahedral (FeH6)4- complexes. Various research groups have carried out investigations on the synthesis of Mg2FeH6 [120-130]. Herrich et al.[121], studied the influence of milling conditions and temperature on the hydride formation and obtained a 90 % yield of Mg2FeH6. Among the compositions investigated a ratio 2: 0.57 of MgH2 to Fe exhibited good results. Decomposition behavior of Mg2FeH6 was investigated based on synthesis conditions and unreacted Fe content. The observed decomposition temperatures were 428 oC and 355 oC [124].  Desorption mixture of Mg2FeH6 reversibly absorbs hydrogen to form the hydride at 550 oC and 60 bar H2 pressure. The presence of Fe/MgH2 enhances the H2 desorption, however the temperature does not enhance the synthesis rate. Hout et al. [122], reported better reversibility in Mg2FeH6 synthesized by ball milling of 2MgH2+ Fe than sintering 2Mg+ Fe under hydrogen. The enthalpy of reaction for 2MgH2+ FeH+ 0.5H2 Mg2FeH6 is reported to be -121.402 kJ/mol H2 and the dissociation enthalpy of Mg2FeH6 is 98 kJ/mol H2 [120].

Studies on MgH2 and Mg2FeH6 indicated that Mg2FeH6 reduces the formation heat of the mixture, which suggests that Mg2FeH6 acts as a catalyst. As a result the milled powder containing MgH2 and Mg2FeH6 desorbs hydrogen within the small temperature range and exhibits rapid desorption rate [127, 130]. A reduction in the decomposition temperature of about 100 oC has been observed for the Li modified Mg2FeH6 and  an enhancement in the sorption kinetics for the Ti- doped Mg2FeH6 [131]. Halilov et al. [132],  and Orgaz et al. [133],  studied electronic structure and chemical bonding in Mg2FeH6 by first-principal calculations. Calculated energy gap is ~ 1.8 eV suggesting that Mg2FeH6 is poor conductor that is consistent with experimental data [133]. However, the calculation shows that the values of the energy gap in D2MH6 (D= Mg, Ca, Sr; M= Fe, Ru, Os) series is a function of the unit cell volume. Further studies are required to a better understanding of this feature.

Instead of much experimental work, the high pressure study on Mg2FeH6 is not yet reported. The transition metal hydride having similar electronic structure, Mg2NiH4, found to be exhibiting high pressure/temperature phase transitions [134]. Therefore it is worthwhile to study the high pressure- temperature behavior of Mg2FeH6. High pressure and high temperature X-ray diffraction experiments have been carried out to find the isothermal bulk modulus and thermal expansion coefficient of Mg2FeH6.

## 4.2. Synthesis and Characterization of Mg2FeH6

4.2.1. Synthesis

Mg2FeH6 powder sample was synthesized by mechano- chemical method using a Retsch (PM 100) ball mill. A stoichiometric mixture of MgH2 and Fe in the ratio 2:1 was ball milled at a speed of 400 rpm under H2 atmosphere for 72 hrs and then annealed at 400 oC under a H2 pressure of 100 bars. The milling resulted in disappearance of the MgH2 peaks followed by the appearance of Mg2FeH6 phase which broadened on further milling. After heating the Mg2FeH6 abundant phase a significant decrease in the full width half maximum (FWHM) of the diffraction peaks was observed.

The X-ray diffraction indicates ~ 85 % yield of Mg2FeH6. Particle sizes of the as milled and the annealed samples were determined by the Le Bail profile fitting method in the general structure analysis system (GSAS) using the equation;                                                                         where, D -particle size, K- Scherer constant, λ- wavelength of X-ray (0.71073Å), Lx- Lorentzian function representing the particle size broadening [135]. Instrumental particle size broadening of the diffraction peaks was estimated by measurements of LaB6 standard sample with average particle size ≥ 1 μm. The particle sizes were also confirmed by electron microscopy experiments.

### 4.2.2. Electron microscopy

The compositional contrast and sample morphology has been investigated by the scanning electron microscopy (SEM) using Jeol JSM-6330F equipped with energy dispersive X-ray spectroscopy (EDS), and by the transmission electron microscopy (TEM) using Philips CM200.

4.2.3. X-ray diffraction

The high pressure diffraction studies were conducted at Sector 16-IDB, HPCAT, Advanced Photon Source in the Argonne National Laboratory and the X-ray wavelength was 0.368 Å. The sample was loaded into the Mao-Bell type DAC with a culet size of 400 m. The sample chamber was a steel gasket having hole of 240 μm diameter and 50 μm thick.  The high temperature X- ray diffraction studies were carried out on annealed Mg2FeH6, using Bruker- GADDS/D8 X-ray system with molybdenum MacSci rotating anode (λ~ 0.71073 Å) and Apex Smart CCD Detector. For high temperature studies, Mg2FeH6 was loaded in quartz capillary and kept under vacuum overnight before sealing with Ar gas to avoid oxidation of the sample. A homemade heater coupled with temperature controller was used to heat the sample for in situ XRD experiments up to 500 oC. Temperature was calibrated from the thermal expansion of NaCl.

### 4.2.4. Computation

The total energy of Mg2FeH6 was calculated using the density-functional theory (DFT) within the generalized-gradient approximation (GGA) for the exchange-correlation function as implemented with a plane-wave basis in the Vienna ab initio simulations package (VASP) [44, 136, 137]. Calculations were performed using the projected-augmented wave (PAW) potentials provided with the VASP [138]. The reciprocal space sampling was done with k-point grids of 5x 5x 5 which were generated according to the Monkhost-Pack scheme. Experimentally established crystal-structure data were used as input [139]. The ionic positions and lattice parameters were relaxed with the conjugated gradient method using forces and stresses for all the volumes considered. In all the calculations, self-consistency was achieved with a tolerance in the total-energy of at least 0.1 meV/ atom. The equilibrium volume V0 and bulk modulus K0 were obtained by fitting dE/dV – V (where V is unit cell volume and E is its total energy) values to the third order Birch–Murnaghan equation of state.

## 4.3. Results and Discussions

### 4.3.1. Electron microscopy

The selective area electron diffraction (SAD) pattern (dark contrast) shows poly crystalline nature of the sample and the TEM micrograph shows a distribution of particle size between 5-50 nm (Figure 4.1) in the annealed sample.  Surface morphology and component distribution of the synthesized Mg2FeH6 samples were analyzed by SEM. The backscattered and secondary images (Figure 4.2) and the EDS spectra show a homogenous distribution of Fe and Mg in the sample.  Secondary image show sample morphology of highly agglomerated particles attributing to the high surface energy of the nanoparticles. The weight percentage of different elements from EDS analysis of spots marked 1-3 in the secondary image is summarized in Table 4.1 and the EDS spectrum collected at spot 3 is given in Figure 4.3.

(a)                                                           (b)

Figure 4. 1: a) Selective area electron diffraction pattern of annealed Mg2FeH6. b) TEM image of as synthesized sample.

(a)                                                              (b)

Figure 4. 2: (a) Backscattered SEM image and; (b) secondary image of annealed Mg2FeH6.

Figure 4. 3: The EDS spectrum collected from spot 3 marked in the secondary image.

Table 4. 1: Weight % of elemental components O, Mg and Fe obtained from EDS analysis at spots marked 1-3 in the secondary image.

| Wt % | O | Mg | Fe |
| --- | --- | --- | --- |
| Spot 1 | 8.15 | 43.17 | 48.67 |
| Spot 2 | 9.31 | 41.26 | 49.43 |
| Spot 3 | 7.85 | 40.45 | 51.70 |

### 4.3.2. High pressure micro X-ray diffraction

High pressure experiments were carried out on both as synthesized and annealed samples to check the influence of ball milling on the properties of Mg2FeH6. The pressure transmitting medium used in the experiments was silicone oil of viscosity 5x10-6 m2/s (Sigma- Aldrich). Figure 4.4 shows the synchrotron XRD pattern of Mg2FeH6 collected at ambient conditions. The  Rietveld analysis of the ambient XRD pattern shows it is a cubic- Fm¯3m phase with a lattice parameter of a = 6.446(3) Å  and a unit cell volume of  V = 267.846(2) Å3, which is in good agreement with the earlier reports [122].  The atomic positions are; Mg- 8c (0.25, 0.25, 0.25), Fe- 4a (0, 0, 0) and H- 24e (0.2456, 0, 0). A unit cell contains 4 formula units which give a unit cell formula weight of 442.02 g/mol and an X-ray density of 2.74 g/cm3 for the Mg2FeH6. Weight fraction of Mg2FeH6 was 85.4 % and Fe was 14.5 %. A small fraction of MgO and Mg were also present in the sample. Particle size of as milled and the annealed samples are found to be 13.6 nm and 53.84 nm, respectively. Both compression and decompression data of Mg2FeH6 were collected in various steps between 0.2- 36.5 GPa.

Figure 4. 4: Synchrotron XRD pattern collected at ambient conditions with the results of the Rietveld analysis. Inset is the simulated crystal structure of Mg2FeH6.

Unit cell volumes at different pressure are determined by peak fitting with the CMPR software package [114]. Figure 4.5 shows the X-ray diffraction patterns collected for the annealed samples at various pressures. No structural phase transition was observed up to the highest pressure reached in the experiment. The change in the XRD peak positions corresponding to the Fe, above 10.6  GPa,  is attributed to the bcc to hcp phase transition [140, 141]. The peaks corresponds to hcp iron is overlapping with sample peaks, yet clearly visible in the XRD patterns collected above 25 GPa.

(a)                                               (b)

Figure 4. 5: (a) Debye diffraction rings collected from sample loaded in DAC, at ambient conditions. (b) X-ray diffraction patterns of Mg2FeH6 for some selected pressures during compression and decompression (pressure indicated by *).  Peaks correspond to hcp phase of Fe are marked by closed circles in the patterns at 18.9 GPa.

The bulk modulus data was determined by fitting the P-V data, Figure 4.6, with the third order Birch-Murnaghan equation of state. Bulk modulus of Mg2FeH6 calculated using the VASP was 76.3(0) GPa, while the experimental values are in the range 75-170 GPa for the samples measured at different conditions. The value of bulk modulus obtained from X-ray diffraction analysis of the sample with pressure medium was comparable with the calculated value. Table 4.2 shows a comparison of the isothermal K0 data obtained from high pressure studies on various samples of Mg2FeH6 with K'0 fixed to 4.

Figure 4. 6: A comparison of calculated and experimental variation of unit cell volume of Mg2FeH6 (MFH) with pressure fitted with the third order Birch-Murnaghan EoS under different conditions. PTM abbreviates pressure transmitting medium.

Table 4. 2: Data obtained from fitting P-V data with Birch-Murnaghan EoS for various Mg2FeH6 samples with a comparison of pressure ranges. PTM abbreviates pressure transmitting medium.

| Mg2FeH6 | P-range (GPa) | Vo (Å3) | Ko (GPa) | Vo (Å3) Ko (GPa) P- range 0- 10 Gpa |  |
| --- | --- | --- | --- | --- | --- |
| VASP | 0- 45 | 263.51(0) | 76.31(0) | 263.24(0) | 77.07(1) |
| annealed | 0- 37 | 268.2(1) | 108.75(3) | 267.61(5) | 95.26(5) |
| ball milled | 0- 21 | 264.09(1) | 170.36(8) | 265.28(1) | 139.05(10) |
| annealed+ PTM | 0- 10.5 | 267.62(1) | 75.35 (4) | 267.62(1) | 75.35(4) |
| ball milled+ PTM | 0- 12.3 | 264.02(2) | 157.11(27) | 264.81(2) | 139.15(31) |

As synthesized samples show high bulk modulus, with and without pressure medium. This can be attributed to the largely nano- morphology of the Mg2FeH6 sample synthesized by ball milling. A close analogue of dimagnesium iron hydride, Mg2NiH4, has the bulk modulus of 43 GPa [134]. Barsan et al. [142], studied ruthenium hydrides M2RuH6 (M= Ca, Sr and Eu) with a K2PtH6- type crystal structure by Raman spectroscopy up to 5 GPa. They reported bulk moduli of 18.8 GPa for Ca2RuH6, 26.73 GPa for Sr2RuH6 and 20.38 GPa for Eu2RuH6. Those values were determined in the assumption of linear correlation between cubic unit lattice parameter and vibrational frequencies. However, these values might be much underestimated taking into account the current work and the calculated bulk moduli of Ca2RuH6, which are 67.6 GPa (LDA) and 58.5 GPa (GGA) obtained by DFT [143].  The bulk modulus values obtained by fitting data up to 10.5 GPa are compared with that of the data at different rages of pressure in the Table 4.2. Results show that there is no effect of silicone oil in the bulkmodulus values obtained for the ball milled sample below 10.5 GPa. This confirms the assumption that the high bulk modulus of the ball milled materials is caused by stress or particle size reduction induced by milling.

### 4.3.3. High temperature X-ray diffraction

Figure 4.7 shows the high temperature in situ X-ray diffraction patterns of Mg2FeH6 collected at various temperatures up to 450 oC.  No temperature induced structural phase transition was observed in Mg2FeH6 before its decomposition around 425 oC. X-ray diffraction pattern collected at 450 oC shows the presence of Fe, Mg and a small amount of MgO.

Figure 4. 7: High temperature XRD patterns of the Mg2FeH6 collected at various temperatures. In the pattern taken at 450 ºC, peak marked by asterisks is due to Fe and that marked by closed circle is MgO, and others are of Mg.

The volumetric thermal expansion is calculated from the unit cell volume and temperature using the relation, . Second order polynomial fit to the ΔV/V0 versus T-T0 (Figure 4.8) gives thermal expansion as αv = 5.85(3)10-5+ 7.47(7)10-8 (T-T0)/ oC. This value is 10 times higher than the thermal expansion coefficient reported for the ZrH2 [144].

Figure 4. 8: Plot of normalized volume versus temperature for Mg2FeH6 fitted with a second order polynomial.

### 4.3.4. Raman spectroscopy

Parker et al. [145],  has reported Raman spectra of Mg2FeH6 and the laser power on the sample was 4 mW. The output laser power used in the present study was between 10 and15 mW which is the least achievable value in the Raman spectrometer used. The results show intense peaks of Fe-H bending modes in the range 800-1100 cm-1. Fe-H stretching modes (1600-2000 cm-1) are very weak which can be attributed to laser induced partial decomposition or bonding structure change. The liberational modes are observed at 356 and 585 cm-1, Fe-H bending modes at 787 and 1093 cm-1 and Fe-H stretching mode at 1866 cm-1. Figure 4.9 shows Raman spectrum (background subtracted) collected from Mg2FeH6 sample loaded in a quartz capillary at ambient conditions.

Figure 4. 9: Raman spectrum of Mg2FeH6 at ambient conditions. Liberational modes (x);  Fe-H bending modes (*); Fe-H stretching mode (o).

# CHPATER 5. STRUCTURAL STABILITY OF DIFFERENT

# POLYMORPHS OF Mg(BH4)2

## 5.1. Introduction

Magnesium borohydride, Mg(BH4)2, is a promising lightweight solid state hydrogen storage material with a theoretical hydrogen capacity of 14.8 wt%. The thermodynamical properties of Mg(BH4)2  were examined by several researchers and it was found that reaction enthalpy and entropy should give 1 bar equilibrium pressure for hydrogen at room temperature [38, 146, 147]. The low enthalpy of decomposition suggests a possibility of reversible hydrogen storage in this compound [78, 79, 147]. However, it seems as if there were high kinetic barriers involved in the hydrogen desorption leading to high operation temperature (> 270 oC), poor kinetics and difficulty to re-hydrogenate the desorption product. The possible decomposition steps for Mg(BH4)2 may be; Mg(BH4)2 MgH2+ 2B+ 3H2 Mg+ 2B+ 4H2 MgB2+ 4H2 [146]. The investigation of Ozolins et al. [148], lead to the conclusion that thermodynamically reversible hydrogen storage is possible in Mg(BH4)2 but it is kinetically hindered. Moreover, calcium analogue of Mg(BH4)2 has been demonstrated recently to show reversible hydrogen storage properties [149-151].  To improve the hydrogen absorption/ desorption properties of Mg(BH4)2, additives like Ti are explored [146]. To verify such phenomenon in Mg(BH4)2 further research is inevitable by theoretical calculations of thermodynamic properties which in turn requires a proper structural data in a wide range of temperatures and pressures. Moreover, destabilization of metal borohydrides was suggested to be achieved by application of high pressure via formation of short H∙∙∙H distances and deformation of tetrahedral BH4 anions [79, 152].

There are many reports on synthesis and crystal structure of Mg(BH4)2 [12, 38, 78, 79, 95, 153-157]. Her et al. [95],  reported that crystal structure of Mg(BH4)2 is hexagonal- P61 below 180 oC and above this temperature it transforms to an orthorhombic- Fddd  phase  which is stable up to the decomposition temperature of 340 oC. The P61 structure of Mg(BH4)2 with 30 formula units (330 atoms) in a unit cell contains five symmetry independent Mg2+cations and ten BH4- anions. Hydrogen co-ordination for Mg2+ is 8 and locally the Mg2+ network resembles an amorphous state [153]. The density of low temperature phase of Mg(BH4)2  is found to be 0.78 g/cm3 whereas that of high temperature phase is 0.76 g/cm3. The structure of high temperature phase was found to be coherent in b-c plane but not in a-direction. The bonding in Mg(BH4)2 is partially covalent similar to that of MgH2 but it has a higher bond strength than MgH2 [12].  The B-H interaction in BH4- tetrahedra is iono-covalent and that between Mg and H is ionic [78].  The hydrogen and BH4- co-ordination of Mg2+ ion is strongly related to its ionic radius/ ionic character which may be a cause of the complex bonding nature of Mg2+ ions. First-principal density functional theory calculations failed to predict ambient-pressure structure of Mg(BH4)2 due to its complexity [147, 148].

Because of the observed irreversibility of high temperature phase transition, high pressure behavior of Mg(BH4)2 is of special interest. Therefore more studies are required to find a method to accelerate the kinetics of the compound formation. To determine the proper additive to enhance kinetics of Mg(BH4)2, the actual structure and structural modifications of this compound should be understood.  Many aspects of phase transition in Mg(BH4)2 is still unknown and to be solved for better understanding of the factors affecting the polymorphism.  In order to verify structural predictions and to compare the behavior of high pressure phase to that of high temperature phase for Mg(BH4)2, micro X-ray diffraction and Raman spectroscopic studies were carried out up to 22 GPa. The results indicate an irreversible pressure induced phase transition in Mg(BH4)2.

## 5.2. Experimental Details

### 5.2.1. Synthesis

Powder sample of Mg(BH4)2 was synthesized by wet chemical method of reaction between MgH2 and triethylamine borane complex under an argon ambient followed by heating above 100 °C in two steps [146]. The mixture was then cooled to room temperature, filtered and washed with n-hexane and dried under vacuum. The triethylamine adduct of Mg(BH4)2 obtained was heated at various steps up to 160 °C under vacuum which yielded 98 % pure sample. Using an argon-filled glove-box, the sample were loaded into the Mao-Bell type DAC of a culet size 400 m and the sample chamber was a stainless steel gasket with a hole of size 190 m and thickness 50 m.

### 5.2.2. High pressure micro X-ray diffraction

The high pressure angle-dispersive micro XRD studies were conducted at Sector 16-IDB, HPCAT, Advanced Photon Source in Argonne National Laboratory (λ = 0.368138 Å) and at X17C beam line of National Synchrotron Light Source in Brookhaven National Laboratory (λ = 0.4066 Å).

## 5.3. Results and Discussion

### 5.3.1. X-ray diffraction of as synthesized Mg(BH4)2

Figure 5.1 shows the micro XRD pattern of Mg(BH4)2 pressurized to ~1 GPa and the corresponding simulated pattern of hexagonal P61 structure.  Result shows that below ~3.5 GPa, Mg(BH4)2  is a single phase and has a hexagonal P61 structure with lattice parameters a = 10.047(3) Å, c = 36.34(1) Å and V = 3176(1) Å3 at ~0.2 GPa which agree with the previously reported values [79, 156].

Figure 5. 1: Synchrotron XRD pattern of low pressure phase of Mg(BH4)2 at ~ 1GPa with the results of  Le Bail profile fitting and inset shows the corresponding hexagonal P61 structure.

Figure 5.2 shows synchrotron XRD patterns recorded during compression and decompression at various pressures up to ~11 GPa. The ambient pressure and high pressure phases coexist in the range 1.5-2.4 GPa. At 3.35 GPa the transition is complete. The high pressure phase is stable up to the highest pressure reached in the X-ray diffraction experiments. Pressure-transmitting medium was not used in the synchrotron XRD experiments. The decompression data shows the high pressure phase transition is irreversible.

(a)                                                            (b)

Figure 5. 2: The synchrotron XRD pattern obtained for Mg(BH4)2; (a) during compression (λ = 0.4066 Å) up to ~ 11GPa, (b) during decompression (λ = 0.368138 Å) at various pressures.

The irreversibility of the high pressure transformation even after the release of pressure suggests that the reverse transformation is kinetically hindered or ambient pressure polymorph of Mg(BH4)2 is a metastable phase. The later might be indicating that the structure of Mg(BH4)2 at ambient conditions can be influenced by the synthesis and processing conditions. The similar situation is observed for aluminum hydride, AlH3, with six different phases which can be prepared via chemical route by varying synthesis conditions [158].  Another aspect should be noted  is that the ambient pressure structure of magnesium borohydride is characterized by large degree of disorder which might have kinetics origin, application of high external pressure eliminates this disorder and leads to more ordered and thus more simple structure.

Because of the low intensity of Mg(BH4)2 XRD patterns, solving the structure of high pressure phase was difficult. It is observed that the structure of Mg(BH4)2 at high pressures is different from the high temperature orthorhombic- Fddd  phase [95]. It is also verified that it does not match with the structures predicted by first-principal calculations such as trigonal- P-3m1, monoclinic- P2/c [147], tetragonal- I-4m1 [148], or orthorhombic- Pmc21 [78]. The possible decomposition products of magnesium borohydride such as MgB2, Mg or B were also absent in the XRD patterns of the high pressure phase.

The XRD patterns of high pressure phase were indexed in hexagonal P63 space group with lattice parameters at 5.5 GPa: a = 8.35(5) Å, c = 4.68(4) Å and V = 283.47(8) Å3. Figure 5.3 shows variation of molar volume with pressure for the Mg(BH4)2 up to ~ 11 GPa. The P-V data of high pressure phase were fitted with third order Birch-Murnaghan equation of state and the bulk modulus was found to be 10.16(6) GPa with Vo = 378.12(7) Å3 and K0'  is fixed to 4.  The experimentally determined bulk modulus of high pressure polymorph of Mg(BH4)2 is in a good agreement with the theoretically predicted value for Mg(AlH4)2  with the P-3m1type structure (K0 = 10.87 GPa, K0' = 5.7) [78]. Low value of K0 suggests very high compressibility for the high pressure polymorph of Mg(BH4)2. To our knowledge this is the lowest bulk modulus reported for metal borohydrides, eg. K0 = 19.9– 31.1 GPa for three different phases of NaBH4 [84, 87], K0 = 14.4– 26 GPa for three different phases of LiBH4 and K0 = 16.8 GPa for KBH4 [79, 87].

Figure 5. 3: Pressure dependence of volume (circles) for the high pressure phase of Mg(BH4)2, during compression, fitted with third order Birch- Murnaghan EoS (line).

### 5.3.2. Raman spectroscopy measurements

### 5.3.2.1. As synthesized Mg(BH4)2

Raman spectra were collected with and without mineral oil as pressure transmitting medium to compare the results and observed similar results. Raman spectrum collected at ambient conditions from Mg(BH4)2 was in good agreement with the literature data [153]. The Raman spectra show liberational and translational modes in the range 50-500 cm-1, bending deformation modes ~1100-1400 cm-1 and B-H stretching modes around 2250 cm-1. The strong bending and stretching modes suggest a strong network of Mg…H-B bonds and a complex structure for Mg(BH4)2. Figure 5.4 shows the Raman spectra obtained during compression up to ~21 GPa for various modes. Spectrum recorded at ~1.1 GPa shows coexistence of both ambient and high pressure phase. The B-H stretching modes start splitting around 2.5 GPa, and around 14.4 GPa a shift in Raman vibrational frequency of B-H bending modes is observed. These changes can be attributed to phase transitions.

The weakening of B-H bending modes observed above 9.5 GPa has occurred due to existence of pressure gradient in the sample and expect that laser heating has less effect on intensity of Raman modes in this experiment [159]. The phase transition observed around 14.4 GPa is completely reversible around 4.5 GPa upon decompression. The spectrum of compressed sample after releasing pressure shows close similarity to the spectra in the range 2.5-14.4 GPa during compression which suggest that the phase transition of Mg(BH4)2 at 2.5 GPa is irreversible. Figure 5.5 shows Raman spectra collected at various pressures during decompression for bending and stretching modes. Decompression spectra of other modes are not shown in the figure due to their very low intensity.

(a)                                                            (b)

Figure 5. 4: The Raman spectra of Mg(BH4)2 collected during compression up to ~ 21 GPa at some selected pressures; (a) B-H bending modes, (b) B-H stretching modes. The peak around 1350 cm-1 is because of diamond in DAC.

A comparative study of compression and decompression data confirms a difference in structure between the compressed and non compressed sample which support the irreversible phase transition observed in XRD analysis. Therefore from combined XRD and Raman spectroscopy experiments it may conclude that the initial high pressure phase transition in Mg(BH4)2 occurs around 2.5 GPa and it is stable up to 14 GPa.

(a)                                      (b)

Figure 5. 5: The Raman spectra of Mg(BH4)2 collected during decompression to ambient pressure; (a)  B-H bending modes, (b) B-H stretching modes. Peak marked with asterisks is due to impurities in diamond.

A small amount of H2 was released in the experiment conducted without using mineral oil which can be attributed to the reaction of small amount of sample with the moisture in the gasket chamber. Table 5.1 shows change in Raman vibrational frequency as a function of pressure (dν/dp) for bending as well as liberational and translational modes during compression of as prepared Mg(BH4)2. In all these cases a significant change in slopes is observed after phase transitions. During decompression a shift in dν/dp was observed around 11 GPa for all the modes.

(a)                                                               (b)

Figure 5. 6: Change in vibrational frequency with pressure for as prepared Mg(BH4)2 during compression; (a) liberational and translational modes, (b) B-H bending modes. The pressures corresponding to change in vibrational modes during compression is marked by grid lines parallel to Y axis.

(a)                                                            (b)

Figure 5. 7: Change in vibrational frequency of B-H stretching modes with pressure for as prepared Mg(BH4)2; (a) during compression, (b) during decompression. The pressures corresponding to change in vibrational modes during compression is marked by grid lines parallel to Y axis.

The difference in dν/dP values of stretching modes (Table 5.2) during compression and decompression also confirms the irreversibility of phase transition in of Mg(BH4)2 as inferred from XRD analysis. The thermodynamically stable high pressure phase has to be further investigated to identify its potential as a hydrogen storage material in terms of kinetic and volumetric aspects.

Table 5. 1: Raman frequency shifts as a function of pressure for liberational, translational and bending modes from fitting the compression data of as synthesized sample.

Modes dν/dp (cm-1GPa-1) at P- ranges: 1 atm (cm-1) 0-2.5 GPa 2.5-14.5 Gpa 14.5-22 GPa

170 -2.61 4.24

200 4.19

210 6.12 5.06 4.13

350 2.32 4.38

1120 5.26 3.08 1.6

1200 0.48 4.38 2.76

1210 -0.35 4.91

1400 2.2 8.27 1.45

Table 5. 2: Raman frequency shifts as a function of pressure for B- H stretching modes during both compression and decompression of as prepared Mg(BH4)2.

Modes dν/dp (cm-1GPa-1) at different P- ranges (cm-1)

Compression 0- 2.5 GPa 2.5- 14.5 GPa 14.5- 22 GPa

2300 19.75 6.17 3.48

2340 10.13 9.59 4.24

2360 13.71 11.49 5.47

Decompression 3.5- 0 GPa 11- 4.5 GPa 22- 14.4 GPa

2300 9.78 5.71 6.52

2340 19.09 10.34 9.01

2360 13.17 8.86 10.97

0- 9 GPa 11- 21 GPa

2300 7.26 3.6

2340 10.55 5.33

2360 11.51 8.12

### 5.3.2.2. The high temperature phase of Mg(BH4)2

The ambient hexagonal phase of Mg(BH4)2 transforms to an orthorhombic- Pmc21 structure above 180 ºC and the phase transition is irreversible [95]. To compare the high pressure behavior of as prepared sample and the high temperature phase, Raman spectroscopic studies of the latter have also been carried out. The high temperature phase is synthesized by heating the sample loaded in DAC in an oven at 200 ºC for 18 hrs and the pressure was close to 1 atm. Figure 5.8a shows comparison of Raman spectra at the stretching mode region for as prepared and heated samples which indicate a high temperature phase has been formed. High pressure Raman spectroscopic studies were carried out on the high temperature phase after cooling down to room temperature. The high temperature phase is found to be stable up to 2 GPa. Figure 5.8b shows the pressure dependence of B-H stretching modes of high temperature phase of Mg(BH4)2.

(a)                                                                     (b)

Figure 5. 8: (a) Raman spectra of as prepared Mg(BH4)2 in comparison with the high temperature phase during compression; peak marked with asterisks is due to impurities in diamond; BH- before heating (as synthesized); AH- after heating (high temperature phase). (b) Change in B-H stretching modes with pressure for the high temperature phase.

In Raman spectroscopic study, significant mode changes were observed around 2 GPa and above 14 GPa.  From the Raman spectra it is obvious that high pressure phase of both as prepared sample and the heated sample is of similar structure as both samples show same frequency shift in the range 2.5-14 GPa. However, there is a significant difference between spectra of both phases above 14 GPa. The disordering of highly compressible B-H bonds in the BH4¯ tetrahedra can be resulting in the phase transitions.

Table 5. 3: Raman frequency shifts as a function of pressure for B-H stretching modes during both compression and decompression for the high temperature phase of Mg(BH4)2.

Modes dν/dp (cm-1GPa-1) at range of pressures: (cm-1)

Compression 0-2 GPa 2.8-14 GPa 14-22 GPa

2300 14.6 6.23 1.24

2340 16.7 10.02 3.25

2360 - 10.54 5.07

Decompression 1.8-0GPa 2.8-9 GPa 22-11 GPa

2300 16.14 6.98 3.61

2340 20.18 10.51 5.33

2360 16.33 10.96 8.11

### 5.3.2.3. High pressure phase of Mg(BH4)2

The experiments show that as synthesized Mg(BH4)2 undergoes an irreversible high pressure transition above 2.5 GPa. Therefore it is important to study the decomposition temperature of this polymorph to check if it is a kinetically destabilized phase. The high pressure phase was prepared by pressurizing as synthesized sample loaded in a DAC up to 5.6 GPa. The high pressure phase was retained when the pressure was released which can be noticed from Figure 5.9. Then it was heated at various temperatures up to 375 ºC using a gas blower, as closed in the DAC to avoid reaction with moisture. Neither phase transition nor decomposition was observed up to this temperature. The hexagonal phase was observed to undergo phase transition above 180 ºC and then decompose in two steps, at 290  and 317  ºC, respectively [37, 38].  Further studies have to be conducted to determine the decomposition temperature of the high pressure phase and also to destabilize this compound by catalytic addition.

(a)                                              (b)

Figure 5. 9: Raman spectra of  Mg(BH4)2; (a) as synthesized phase in comparison with the high pressure phase during compression at some selected pressures,(b) high pressure phase up to 375 ºC at some selected temperatures.

# CHAPTER 6. HIGH PRESSURE INVESTIGATION OF Ca(BH4)2

## 6.1. Introduction

Calcium borohydride, Ca(BH4)2, has a theoretical hydrogen storage capacity of 11.48 wt %. Complex hydrides have high gravimetric storage capacities and among them Ca(BH4)2 and  Mg(BH4)2 are promising materials because of the possibility of reversible hydrogen storage [151].  In a proposed dehydrogenation reaction, hydrogen release of 9.6 wt % is possible from Ca(BH4)2 with CaH2 and CaB6 as decomposition products [160]. The thermal decomposition behavior of Ca(BH4)2 was investigated under hydrogen pressure by Kim et al. [39], and under vacuum or inert gas flow by Aoki et al. [161]. The results show that Ca(BH4)2 undergoes transformation from an orthorhombic to a tetragonal structure below 250 °C with 5.9 % hydrogen release. The structural investigations at different temperatures and pressures help to identify various polymorphs of the material which may have better thermodynamic stability. Ca(BH4)2 exhibits polymorphism depending on the synthesis and processing conditions and also transforms to different phases at various temperatures [96, 98, 151, 162-164]. Filinchuk et al.  [96] observed three polymorphs of Ca(BH4)2 in the temperature range 30- 600 °C which are of orthorhombic- α (F2dd), tetragonal- α′ (I-42d) and tetragonal- β (P-4) structures. Below 300 °C, α and α′ polymorphs completely transforms to β phase. The second order transition from α to α′ is found to be dependent on heating rate/ sample synthesis and processing conditions. Two more possible structures of α phase are C2/c and Fddd suggested by Majzoub et al. [163], and Miwa et al. [160], respectively. Buchter et al. [98], and Lee et al. [162], independently indexed tetragonal phase in P42/m space group which seems to be more reliable than the P-4 structure, according to the results of this study. An orthorhombic (γ) phase of space group pbca was observed by Riktor et al.   [164] which transforms to β phase on heating to 290 °C and again to an unknown phase δ around 330 °C. Catalyst addition is also found to be influencing the formation of different phases in Ca(BH4)2 by Ronnebro et al. [151].

Majzoub et al.[163] observed formation of ~50 % of the  β phase after mechanical milling of α- Ca(BH4)2 which was believed to be because of the combined effect of pressure and temperature. They calculated the bulk modulus of various polymorphs of Ca(BH4)2 using first principles method and it was ~15 GPa. The same group also predicted transition of α to β phase at 5.3 GPa.   Even though there is much theoretical and high temperature work, high pressure experimental study on Ca(BH4)2  is not found in the current literature. Factors affecting the polymorphism of Ca(BH4)2 is not yet known completely. In situ X-ray diffraction and Raman spectroscopic studies on Ca(BH4)2 at high pressures  were carried out to understand the structural stability of its polymorphs and to verify the results of theoretical calculations.

## 6.2. Experimental Details

### 6.2.1. Synthesis

Powder sample of Ca(BH4)2 was synthesized by heating CaCl2 and NaBH4 in tetrahydrofuran (THF) at 80 ºC. The obtained Ca(BH4)2·2THF was dried at various temperatures and under vacuum for long time to remove THF. This process results in the formation of two polymorphs of Ca(BH4)2  in orthorhombic (α) and tetragonal (β) structures.

### 6.2.2. High pressure micro X-ray diffraction

Using an argon-filled glove box, this sample was loaded into the Mao-Bell type DAC with a diamond culet size of 400 μm.  The sample chamber was a stainless steel gasket with hole of size ~190 μm and thickness of 50 μm. Both compression and decompression data were collected at room temperature. The ruby fluorescence method was used for pressure determination. Due to high reactivity of Ca(BH4)2 any kind of pressure transmitting medium was avoided. High pressure diffraction studies were conducted at Sector 16-IDB, HPCAT, Advanced Photon Source of Argonne National Laboratory using X-rays of wavelength ~ 0.3681 Å and Mar345 image plate detector. The micro XRD experiment was repeated at the X17C beam line at NSLS, Brookhaven National Laboratory which facilitating radiation of λ = 0.4066 Å.

## 6.3. Results and Discussion

### 6.3.1. X-ray diffraction

Figure 6.1 shows synchrotron X-ray diffraction patterns of Ca(BH4)2  collected at ambient conditions and the results of Rietveld analysis. The analysis shows that sample is a homogeneous mixture of α and β polymorphs. The α-Ca(BH4)2 is indexed with orthorhombic- F2dd structure and the lattice parameters are a = 8.82(7) Å, b = 13.05(10) Å, c = 7.404(5) Å and V = 851.8(10) Å3 which agree well with the previous report [96]. All the previously reported tetragonal structures for β phase were checked and best match was obtained when space group P42/ m is used. The lattice parameters for β-Ca(BH4)2 is found to be a = 6.88(4) Å, c = 4.32(5) Å and V = 204.82(18) Å3. This result is in agreement with that reported by Buchter et al. [98], and Lee et al.[162], but contradict with P-4 structure proposed by Filinchuk et al. [96], and Majzoub et al. [163].

(a)

(b)

Figure 6. 1: Synchrotron X-ray diffraction pattern of the sample containing α and β polymorphs of Ca(BH4)2 at ambient conditions; (a) Debye ring, (b) integrated plot with the results of Rietveld analysis.

Figure 6.2 shows picture of crystal structures of both α and β polymorphs in F2dd (Z = 8) and P42/m (Z = 2) space groups, respectively. The calculated molar volumes are 64.13 and 61.68 cm3/mol for α and β phase respectively. Molar volume of β phase is less than that of α- Ca(BH4)2 implying a more close packed structure for the former. Figure 6.3 shows XRD patterns at various pressure during compression in a DAC up to 13 GPa in comparison with a pattern obtained from decompressed sample. The disappearance of peaks corresponds to β- Ca(BH4)2  above 10 GPa may corresponds to transition to a highly disordered phase as discussed later in Raman spectroscopy results.

Figure 6. 2: The refined crystal structures of Ca(BH4)2 polymorphs; (α) orthorhombic and (β) tetragonal- P42/ m phases.  The atoms Ca, B and H are represented by symbols of color blue, red, and black, respectively.

Upon decompression it is found that the transformation of β phase is irreversible while α phase is stable in the pressure range studied. The calculated formation energies of α and β phases are of the same order [98].  Therefore, both phases should coexist at similar thermodynamical conditions. The results indicate that above 10 GPa, α phase is more stable than the β phase which is compatible with previous report that the α phase has a lower free energy than the β- Ca(BH4)2 [162]. The unit cell parameters for α phase at different pressures were obtained by Le Bail method.

Figure 6. 3: Synchrotron XRD patterns of Ca(BH4)2;  during compression up to 13.6 GPa and after decompression to 0.5 GPa (marked **).

Pressure volume data obtained for α- Ca(BH4)2 was fitted with third order Birch-Murnaghan EoS (Figure 6.4) and its bulk modulus is found to be 22.95(4) GPa with Vo = 866.06(18) Å3 and Ko′ = 2.63(0.5). This is higher than the calculated bulk modulus for the polymorphs of Ca(BH4)2 by first-principles method which was ~15 GPa [163].  The compressibility of Ca(BH4)2 is of the order of many metal borohydrides [96, 97]. Any α to β phase transition was not observed in this experiment, around 5.3 GPa, as reported by Majzoub et al. [163].

Figure 6. 4: Pressure dependence of the volume (circles) for α-Ca(BH4)2 during compression, fitted with the third-order Birch-Murnaghan equation of state (line).

### 6.3.2. Raman spectroscopy

Figure 6.5 shows Raman spectrum collected at ambient conditions which confirms the presence of  both α and β- Ca(BH4)2  phases in the sample in comparison with the previous reports [160, 163]. The peaks corresponds to each phase is resolved with a Gaussian profile fitting. The analysis of BH4- liberational (50-550 cm-1) and B-H bending modes in the region 1000-1300 cm-1 are not included in Raman spectra at high pressures because of its weak intensity or its overlap with the Raman peak of diamond.

Figure 6. 5: Raman spectrum (blue line) of Ca(BH4)2 containing both α (yellow colored peaks) and β (black colored peaks) polymorphs collected at ambient conditions.

Figure 6.6 shows the Raman spectra at various pressures in the region of B-H stretching modes (2250- 2400 cm-1) collected during compression and decompression. Raman spectrum obtained in the range 0.2- 10.2 GPa shows coexistence of the α and β phases without any phase change. Above 10.2 GPa there is a shift in Raman vibrational frequency of peaks corresponds to the α phase. While peaks of the β phase disappears and a new peak originates around 2307 cm-1 at 10.2 GPa. This is much clear in the plot of variation of Raman shift with pressure (Figure 6.7). The analysis results implies a structural transition of the β phase and occurrence of a hardening or reordering of B-H bonds in the α- phase at high pressures.

- (b)

Figure 6. 6: Raman spectra of Ca(BH4)2; (a) during compression up to 25 GPa,  (b) during decompression for B-H stretching modes. The peak (marked *) around 2650 cm-1 is because of diamond in the DAC.

On decompression, the behavior of the  α- phase is found to be reversible around 5 GPa while that of the β- phase is irreversible. Change in Raman vibrational frequencies as a function of pressure (dν/dP) for B-H stretching modes during compression of Ca(BH4)2 is given in Table 6.1. During decompression a frequency shift is observed around 5 GPa, but the slopes remain unchanged for the peaks corresponds to the α-Ca(BH4)2.  On comparing Raman spectroscopic results and XRD results, it may conclude that the β phase transforms to a highly disordered structure above 10.2 GPa.

Figure 6.  7: Change in the Raman shift with pressure for B-H stretching modes of Ca(BH4)2; (a) during compression and (b) during decompression. The pressures corresponding to the change in vibrational modes are marked by grid lines parallel to the Y axis.

A partial decomposition of the Ca(BH4)2 sample leading to desorption of small amount of hydrogen was also observed in the Raman spectroscopic study ~2.5 GPa, but the possible decomposition products were absent in the XRD pattern at this pressure. The decomposition may be caused by reaction with the small amount of moisture present in the gasket chamber. A comparison of spectra collected around 0.5 GPa and after releasing pressure shows that α phase is unchanged which confirms the XRD results. It is obvious that there is a phase transition of β- Ca(BH4)2 while the α- phase is stable in the pressure range studied, except some change in the bonding structure. Because of the poor intensity of the XRD patterns at high pressure, structure of the new phase was not determined.

Table 6. 1: Change in Raman shift frequencies as a function of pressure for B-H stretching modes of Ca(BH4)2 during compression and decompression.

B-H stretching dν/dP (cm-1GPa-1) at different P- ranges modes at 0.7 GPa Compression Decompression (cm-1) 0.2-8.8 GPa 10.2-25.3 GPa 0.2-4.9 GPa 6.5-16 GPa

2298 6.04(6) -- -- 6.18(2)

2307 -- 8.38(7) 10.81(3) 10.81(3)

2330 8.69(1) 7.99(4) 12.9(8) 12.9(8)

2375 6.79(5) 8.92(6) -- --

2423 9.39 (11) -- 5.85(11) --

2466 4.5(12) -- -- --

# CHAPTER 7. HIGH PRESSURE INVESTIGATION AND

# P-T PHASE DIAGRAM OF NaBH4

## 7.1. Introduction

Sodium borohydride (NaBH4) is a potential hydrogen storage material and has a theoretical hydrogen storage capacity of 10.6 wt %.  Li et al. [165], demonstrated NaBH4 slurry as an efficient way of application and generated hydrogen by the simple reaction NaBH4+ 2H2O NaBO2+ 4H2. Due to strong covalent and ionic bonding nature, dissociation temperatures of borohydrides are very high. The improvement of the hydride properties by catalytic addition requires better understanding of the phases and its phase stability.  It is found that the hydrogen desorption in NaBH4 can be enhanced by addition of Pt or Ru [166].  Under ambient conditions, NaBH4 has a cubic structure with space group Fm-3m [85, 167].

At low temperatures, around 190 K, NaBH4 exists in a tetragonal structure [168, 169]. The well investigated high- pressure phases of NaBH4 at room temperature are tetragonal- P¯421c and orthorhombic- Pnma structure which appears above 6.3 and 8.9 GPa, respectively [85]. The previous reports suggest that the orthorhombic phase is stable in the pressure range 8.9- 30 GPa.  Lee et al. [170], have studied ab initio structural stability of cubic and tetragonal phases of NaBH4 up to 30 GPa and 4000 K but an experimental phase diagram is lacking in the current literature in these ranges. A low temperature phase diagram of NaBH4 was reported by Sundqvist et al. [169], in the P- T plane of 0-2 GPa and 100-300 K. In the phase diagram reported by Sundqvist et al. [169], tetragonal to orthorhombic phase boundary of NaBH4 is marked in the range 9-11 GPa.

Even though there are many reports on high pressure phase transitions of NaBH4, some of them failed to observe a phase transition above 10.8 GPa [169].  The ab initio calculations by Araujo et al. [171], showed a cubic to monoclinic transition at 19 GPa and to orthorhombic at 33 GPa. Through Raman spectroscopic studies, the same group observed a phase transition in the range ~10.8- 14.8 GPa and a completely new phase was formed above 15 GPa. However, the XRD experiments reported cubic to tetragonal transition at 6.3 GPa and to orthorhombic at 8.9 GPa [84, 85]. Because of these inconsistencies in reported transition pressures and structure of the phases, in situ high P-T structural measurements were carried out on NaBH4 both by XRD and Raman spectroscopy, using a DAC to obtain further understanding of its stability.

Filinchuk et al. [172], found that texture has much influence in the structure refinement of NaBH4. Theoretically predicted structures of borohydrides (Ref. [148, 173]) are found to be different from that of the experimentally observed ones [80, 85, 94, 171]. More theoretical and experimental investigations are required to explain the inconsistencies in these results. The present work is to extend the P-T plane of the experimental NaBH4 phase diagram from ambient to 17 GPa and 673 K using combined XRD and Raman spectroscopy studies. The results of the high pressure Raman spectroscopic studies of NaBH4 up to ~30 GPa is carried out and an interesting new phase is observed. A comparative symmetry analysis also has been carried out for various phases of NaBH4.

## 7.2. Experimental Details

NaBH4 of 99 % purity, purchased from Sigma Aldrich was used for the study. All sample handlings were carried out in an argon atmosphere. Mao-Bell type DAC with diamonds of 0.4 mm culets and steel gasket of 0.18 mm hole was used. For heating experiments resistive ring-heater and specially designed K- type thermocouples were employed around diamond culets. For accurate pressure measurement, NaCl and ruby chips were added to the sample. High pressure experiments were conducted with and without mineral oil as a pressure transmitting medium and observed highly non hydrostatic behavior above 12 GPa in both cases. In the heating experiments no pressure transmitting medium was used. The XRD measurements at high P-T conditions were conducted at station B2 of Cornell high energy synchrotron source (CHESS) in Cornell University with facilitating radiation of wavelength, λ = 0.49594 Å. Some part of the high P-T diffraction studies was carried out at X17B2 beam line of National Synchrotron Light Source in Brookhaven National Laboratory (energy- dispersive, 2θ = 6.4762º). High pressure XRD experiment was also carried out at HPCAT, Argonne National Laboratory with an X-ray wavelength of λ = 0.40026 Å.

## 7.3. Results and Discussion

### 7.3.1. In situ high P-T X-ray diffraction

### 7.3.1.1. Angle dispersive micro X-ray diffraction

The micro XRD patterns of NaBH4 were refined with Rietveld analysis and the obtained lattice parameter for the ambient cubic phase is a = 6.107(0.2) Å with V = 227.83 Å3 at 0.2 GPa which is in agreement with the previously reported value [85]. Figure 7.1 shows the indexed synchrotron XRD pattern of cubic NaBH4 with the results of Rietveld analysis. In the cubic phase, the Na atoms occupy 4a sites at (0,0,0) and B atoms at 4b (0.5,0.5,0.5) positions, whereas the H atoms occupy 32f sites with coordinates x = 0.400264. The orientationally disordered (BH4)- tetrahedral units are octahedrally surrounded by Na+ cations facilitating ionic nature for the compound.

Figure 7. 1: Micro X-ray diffraction pattern of the cubic phase of NaBH4 collected at 0.8 GPa using a synchrotron source with the results of Rietveld analysis. The peak positions marked in green (a) corresponds to that of NaBH4 and that marked in pink (b) are of NaCl.

Figure 7.2 shows selected X-ray diffraction patterns collected at different pressures/ temperatures. The cubic structure is stable below 6.5 GPa and further increase in pressure cause splitting of (200), (220) and (311) lines which indicate a transition to tetragonal phase. XRD pattern collected at 9 GPa shows appearance of many new peaks which corresponds to an orthorhombic phase. The tetragonal phase at 6.5 GPa transformed back to cubic phase when temperature was increased to 373 K and the compression increases this transformation temperature.

(a)                                                                 (b)

Figure 7. 2: Selected XRD patterns of the three different phases of the NaBH4, at room temperature; (a) the cubic (3.4 GPa), tetragonal (6.5 GPa) and orthorhombic (9 GPa). (b) at various temperatures and 6.5 GPa. Between 323 and 373 K, tetragonal to cubic phase transition occurs. Peaks marked * are of NaCl which was used as a pressure marker.

Figure 7.3 shows schematic representation of the crystal structures of three different phases of NaBH4. The high pressure XRD experiments were conducted up to 34 GPa to investigate a possible phase transition above 14 GPa which was observed with Raman spectroscopy (discussed later). Figure 7.4 shows XRD patterns collected above 13 GPa for some selected pressures. Even though a new peak observed above 15.7 GPa (marked by arrow in successive patterns), a phase transition is not clearly visible from the peak revolution. This is due highly non hydrostatic pressure and the broadening of peaks above 12 GPa. The experiments carried out with and without mineral oil as a pressure medium. Due to solidification of the mineral oil above 9 GPa non hydrostaticity is generated. All the phase transitions observed were reversible as can be inferred from the XRD pattern of decompressed sample.

Figure 7. 3: Crystal structures of (a) the cubic, (b) tetragonal and (c) orthorhombic phases of NaBH4. The Na, B, and H are marked in green, orange and black symbols, respectively.

In the cubic- NaBH4, various bond lengths are found to be 1.208- 1.709, 1.047, 3.03 and 2.57 Å for H-H, B-H, Na-B and Na-H, respectively at 0.8 GPa. Except Na-H bonds all the other bonds are highly compressive. On increasing pressure from 0.8- 3.8 GPa, Na-H and B-H bonds exhibit 1.45 % and 22 % compression, respectively. Hence it may expect that the distortion in (BH4)- tetrahedra can be causing the phase transitions. The H-B-H and B-H-H bond angles remain unchanged in this pressure range while Na-H-B and H-Na-H angles diverge or converge. The co-ordination number and geometry of co-ordination polyhedra vary with pressure and temperature leading to phase transition.

Figure 7. 4: Selected high pressure XRD patterns of NaBH4 above 13.4 GPa up to 34 GPa. The arrow indicated new peaks, and decompressed pattern is marked *.

### 7.3.1.2. Energy dispersive micro X-ray diffraction

A portion of the high P-T experiments on NaBH4 were carried out using multi anvil press employed with a cylindrical graphite heater and tungsten carbide (WC) anvils and the diffraction data were recorded using a CCD detector. Figure 7.5 shows an energy dispersive XRD (EDXRD) pattern of the cubic phase. NaCl was used a pressure marker. At each pressure sample was heated up to 675 K.

Figure 7. 5: An EDXRD pattern of cubic- NaBH4 at 0.2 GPa. The peaks marked (*), (o) and (#) are due to BN, NaCl and Kα, respectively.

The pressure- volume- temperature (P-V-T) data obtained for the cubic phase of NaBH4 was fitted with the third order Birch-Murnaghan equation of state and the value of K0  is found to be 18.76(1) GPa with Ko' = 3.48(0.3) and equilibrium unit cell volume of  231.817(0.9) Å3.  The temperature derivative of bulk modulus and the thermal expansion coefficient were also determined for the ambient phase and the obtained values are dK/dT = –0.01307 GPaK-1 and α = 12.5 x 10-5+ 23.21x 10-8 T/ K, respectively.  Figure 7. 6 show a comparison of P- V data at 298 and 573 K. At low pressures, below 2 GPa, the data shows slight deviation from the previously reported data at room temperature by Kumar et al. [85], which can be due to an error in pressure determination due to a buildup of anisotropic stress [174].

Figure 7. 6: Pressure dependence of the unit cell volume (circles) for the high-pressure phase of cubic NaBH4 during compression at room temperature and at 573 K, fitted with third order Birch- Murnaghan EoS (line).

The obtained value of Ko for cubic phase is in agreement with the19.9 GPa reported by Kumar et al. [85].  They have also reported that the bulk modulus of orthorhombic- NaBH4 is 31.1 GPa. The ambient cubic phase of NaH  and its high pressure phase has a bulkmodulus of 19.4 and 28.3 GPa respectively [48]. It suggests that the boron addition to NaH does not have much influence on its compressibility. The calculated values of K0 for cubic and tetragonal phases of  NaBH4 are 20.6 and 30.9 GPa, respectively at 0 K [84]. First principle calculations by Vajeeston et al. [91], shows a K0 of 7.6 GPa for the NaBH4 which is much lower than all other reported values.

### 7.3.2. Raman spectroscopy

### 7.3.2.1. High pressure in situ Raman spectroscopy

Figure 7.7 shows Raman spectra of NaBH4 at some selected pressures and temperatures in the B-H stretching region (2100-2500 cm-1).  B-H bending modes (1100-1300 cm-1) overlap with the Raman peaks due to diamond in DAC and hence were excluded them from further analysis. According to the Raman spectroscopy results, phase transitions occur at 6.3 and 8.3 GPa to tetragonal and orthorhombic structures respectively. No new Raman peaks emerged in the cubic to tetragonal transition except change of slope of the vibrational modes. There is a new peak appearing at 8.3 GPa indicating tetragonal to orthorhombic phase transition. The cubic- tetragonal transition is an order-disorder transition which was also observed below 190 K [174]. Again a new phase starts to appear above 14 GPa and form a completely new phase around 17 GPa and it is stable up to 30 GPa (Figure 7. 7b). It may be possible that the new phase is not distinguishable in XRD patters, as above 14 GPa the peaks are much broader and weak which makes it difficult to identify any splitting of peaks. Above 14 GPa the relative intensities of the peaks changes to that of a monoclinic- LiAlH4 with space group P21/c [69]. Any anomalies in Raman shift were not observed below 3 GPa as reported in Araujo et al. [171]

- (b)

Figure 7. 7: Raman spectra of NaBH4 during compression; (a) at selected pressures and the spectrum marked  ?  corresponds to the appearance of a new phase,  (b) spectra in the range 14-30 GPa.

Figure 7.8 shows Raman spectra collected at various pressures during decompression. A large hysteresis (~3 GPa) is observed in the reverse transition of orthorhombic phase at room temperature. The experimentally observed B-H stretching mode frequencies for all the four phases of NaBH4 are presented in Table 7.1. The Raman mode present at 754 cm-1 in the spectra of cubic phase was not present in that of the high pressure phases. The B-H bending mode ~1278 cm-1 at high pressures were not studied with pressure because of its overlap with the Raman peak of diamond from DAC.

Figure 7. 8: Selected Raman spectra of NaBH4 during decompression.

The decompression data shows the phase transitions occurred are reversible with a hysteresis which supports the observation of Sundqvist et al. [169]. The observed transitions are much clear from the plot of Raman shift with pressure (Figure 7.9).  It is found that pressure induced shift in Raman peaks arises from the bond compression and the energy storage exerted by compressive stress [175]. Frequency of Raman modes increase or stiffen the vibration with compression of bond under pressure whereas the bond expansion softens the vibration. There is a correlation between B- H stretching frequencies, B-H bond length and energy.

- (b)

Figure 7. 9: The Raman shift versus pressure obtained by peak fitting of B-H stretching modes at each pressure; (a) during compression and (b) decompression. Pressures corresponds to phase transition are marked with grid lines parallel to the Y axis.

In the tetragonal phase the stiffening of bond due to compression is absent where as all other phases has shift in Raman mode frequency. This can be related to the bond reordering under pressure accompanied with the transition of an orientationally disordered cubic to an orientationally ordered tetragonal phase. For a hydrogen bonded B-H stretching mode, the positive pressure dependence may be explained by H-H repulsion under compression [176].  A change in the slope of Raman shift versus pressure plots and an appearance of a new peak during compression confirms the transition of orthorhombic to another high pressure phase in the range 14-17 GPa.

It is difficult to distinguish an orthorhombic to tetragonal transition from the decompression data which can be due to the large hysteresis of the reverse transition of orthorhombic phase. Table 7.2 gives the change of slopes of Raman shift versus pressure during compression which indicates that there are four high pressure phases of NaBH4 that exist in the range 0- 30 GPa at room temperature.  First principle calculations by Araujo et al. [171], found a cubic to monoclinic - P21/c  phase transition at 19 GPa while their experimental Raman spectra ~14 GPa is very similar to that of the orthorhombic phase as observed in this study.

Calculations of Kim et al. [84], and experiments of Kumar et al. [85], found that orthorhombic phase is stable up to 30 GPa. The compression data of Araujo et al. [171], shows a complete transition to an orthorhombic phase ~ 14.8 GPa which reverse transform to low pressure phase at 7 GPa on decompression. This result deviates from the observations of transition pressures of 8.3 and 5 GPa for forward and reverse transitions of orthorhombic phase, respectively in this study. The difference in the measured pressures might be the reason why they have missed the phase transition above 14 GPa in their Raman spectroscopic study up to 16.2 GPa.

Table 7. 1: The observed B-H stretching modes in cm-1 (sh- shoulder) for different phases of NaBH4.

0GPa 6.3GPa 9.1GPa 17.2GPa cubic tetragonal orthorhombic monoclinic

2205.77 2286.62 2311.57 2368.12 sh

2236.77 2335.59 sh 2356.74 sh 2408.61 sh

2331.7 sh 2384.34 sh 2407.54 --

-- -- 2436.89 2452.84 sh

2335.66 2426.13 sh 2450.44 sh --

2350.73 2430.05 2475.74 sh 2491.05

-- -- 2492.85 2534.12 sh

2461.91 sh 2512.4 2533.68 sh 2613.65 sh

-- -- 2591.52 sh 2671.24 sh

Table 7. 2: The pressure dependence of Raman shift frequency for NaBH4 during both compression and decompression.

Raman mode Compression Decompression ν (cm-1) dν/dp (cm-1GPa-1) dν/dp (cm-1GPa-1) 0-6.3 GPa 8.3-17 GPa 17.5-28 GPa 5.2-13.6 GPa 14.2-26 GPa

2200 11.51(1) 8.2(7) 7.56(3) 9.9(0.5) 6.23(0.4)

2300 13.82(2) 8.88(2) 11.45(8) 12.97 (0.8) 6.05(0.7)

2340 15.93(1) 13.32(3) 11.97(9) 14.66 (0.6) --

2400 -- 10.39(1) -- 16.04(2) 6.07 (0.6)

### 7.3.2.2. High P-T Raman spectroscopy

High P-T Raman spectroscopic studies were carried out to construct the phase diagram of NaBH4. Pressure was measured at room temperature and then heated the sample in steps. The high pressure phase transitions were reversible with a rise in temperature as can be observed from Figures 7.10. After collecting spectra at each temperature until the phase transition, the DAC was cooled down to room temperature to increase the pressure with ruby fluorescence method. The transition temperatures were noted on both heating and cooling cycles and the average value is used as a transition point in the phase diagram.

- (b)

Figure 7. 10: The high temperature Raman spectra of NaBH4 in the B-H stretching mode region; (a) while heating at 9.5 GPa in comparison with a spectrum at 3 GPa, (b) at 14 GPa and different temperatures.

### 7.3.3. P-T phase diagram

The transition points for NaBH4 at various pressures and temperature were noted from both XRD and Raman spectroscopy experiments and constructed a P- T phase diagram. Figure 7.11 shows phase diagram of the NaBH4 in the pressure range 0- 17 GPa and temperature range 175- 673 K. The phase boundaries are obtained by heating at almost constant pressure. The cubic phase is found to be stable up to 673 K and 6 GPa. On increasing pressure at room temperature, the cubic- NaBH4 transform to tetragonal phase at 6.5 GPa and back transform to cubic at 373 K.

Figure 7. 11: P-T phase diagram of NaBH4 investigated through DAC technique using XRD and Raman spectroscopic measurements (circles)  including the results of low temperature study of Sundqvist et al. [169], (asterisks). The phase regions marked C, T, O and M are cubic, tetragonal, orthorhombic and monoclinic, respectively. The region marked  ? implies structure of phase is not confirmed.

The phase transitions observed in NaBH4 are found to be reversible with increase in temperature or decrease in pressure with some hysteresis. The available low temperature P-T data were incorporated from Sundqvist et al. [169], in the current phase diagram which is compatible with the present results. The cubic to tetragonal structural transition has a narrow phase boundary compared to that of tetragonal to orthorhombic transition implies entropy of cubic phase is comparable to that of the tetragonal phase.  A large slope observed for the cubic - tetragonal phase boundary thus can be correlated to a significant volume change according to the Clapeyron equation, dT/dP = ΔV/ΔS. The molar volumes of cubic, tetragonal and orthorhombic phases are found to be 34.3, 28.14 and 26.11 cm3/mol, respectively which suggests a larger slope for the cubic- tetragonal than the tetragonal- orthorhombic phase boundary.

### 7.3.4. Correlation of site group to factor group and Raman activity

To identify the Raman active vibrational modes of different phases of NaBH4, a factor group analysis also have been carried out [177, 178]. The lattice modes of each site and the total irreducible representations are summarized in Table 7.3.  Total irreducible representation of cubic (Oh5) phase of  NaBH4 is found to be Γtot = A1g+ A2u+ Eu+ Eg+ T2u+ 2T2g+ 4T1u+ T1g  which suggest that it has 30 degrees of vibrational freedom among which T1u is an acoustical mode and A1g, Eg and T2g are Raman active modes. Therefore there should be 4 fundamental vibrational modes in the Raman spectra of cubic phase.

Tetragonal (D2d4) phase with Γtot = 3A1+ 3A2+ 5B1+ 5B2+ 10E  has 36 degrees of vibrational freedom among which B2 and E are acoustical modes and A1, B1, B2 and E are Raman active modes. This implies there should be 21 fundamental vibrational modes in the Raman spectra of tetragonal phase. Further the orthorhombic phase of (D2h16) NaBH4  has Γtot  = 9Ag+ 6Au+ 6B1g+ 9B1u+ 9B2g+ 6B2u+ 6B3g+ 9B3u  and 60 degrees of vibrational freedom among which B1u, B2u and B3u are acoustical modes and Ag, B1g, B2g and B3g are Raman active modes. It gives 30 fundamental vibrational modes in the Raman spectra of orthorhombic phase. A monoclinic- P21/c structure (C2h5) can be assigned to the NaBH4 phase appeared above 14 GPa in comparison to the theoretical prediction of Araujo et al. [171]. The monoclinic phase has 24 degrees of vibrational freedom (Γtot = 3Ag+ 9Au+ 3Bg+ 9Bu)   and among which Au and Bu are acoustical modes and Ag and Bg are Raman active modes. Therefore there should be 6 fundamental vibrational modes in the Raman spectra of monoclinic phase.

The observed Raman spectra are in agreement with the results of the factor group analysis which shows an increment in the degrees of vibrational freedom and the number of Raman active modes with pressure, from cubic to tetragonal and to orthorhombic phase transitions and then a drop at the formation of the new phase. Therefore, it can be concluded that the high pressure phase observed above 14 GPa can be of monoclinic structure with space group P21/c as showed by calculations of Araujo et al. [171].  The theoretically predicted monoclinic phase could be observed through Raman spectroscopy unlike in XRD because of its ability to distinguish small traces of various local phases coexisting in a compound [179].

Table 7. 3: Symmetry analysis and irreducible representation of lattice modes of NaBH4.

Phase Translational modes of Total irreducible representation atoms in each site

Cubic (225; Fm¯3m; Oh5) Γtot = A1g+A2u+Eu+Eg+T2u+ 2T2g+4T1u+T1g

Na (4a) Oh : T1u

B (4b) Oh : T1u

H (32f) C3v : A1g+A2u+Eu+Eg+T2u+2T2g+2T1u+T1g

Tetragonal (114; P-421c; D2d4) Γtot = 3A1+3A2+5B1+5B2+10E

Na (2a) S4 :B1+B2+2E

B (2b) S4 :B1+B2+2E

H (8e) C1 :3A1+3A2+3B1+3B2+6E

Orthorhombic (62; Pnma; D2h16) Γtot = 9Ag+ 6Au+ 6B1g+ 9B1u+ 9B2g+ 6B2u+ 6B3g+ 9B3u

Na (4c) Cs : 2Ag+Au+B1g+2B1u+2B2g+B2u+B3g+2B3u

B (4c) Cs : 2Ag+Au+B1g+2B1u+2B2g+B2u+B3g+2B3u

H 1 (4c) Cs : 2Ag+Au+B1g+2B1u+2B2g+B2u+B3g+2B3u

H2 (8d) C1 : 3Ag+3Au+3B1g+3B1u+3B2g+3B2u+3B3g+3B3u

Monoclinic (14; P21/c; C2h5) Γtot =3Ag+ 9Au+ 3Bg+ 9Bu

Na (2a) Ci :3Au+3Bu

B (2b) Ci :3Au+3Bu

H (4e) C1 :3Ag+3Au+3Bg+3Bu

# CHAPTER 8. STRUCTURAL INVESTIGATION OF NaAlH4 AND THE INFLUENCE OF BALL MILLING ON COMPRESSION PROPERTIES

## 8.1. Introduction

Sodium alanate (NaAlH4) has been proposed as a viable hydrogen storage medium capable of supplying hydrogen at moderate temperatures and at rates required for fuel cell applications. These favorable characteristics, particularly the reversibility of NaAlH4 as a hydrogen storage media, were reported first by Bogdanovic et al. [28]. An extensive study of related complex metal hydrides including the reversibility and enhanced desorption kinetics for NaAlH4 when doped with titanium and other transition metals followed [180-183]. Phase transitions and crystal structure modifications have been studied with the thermal decomposition of NaAlH4 [184, 185]. Enhanced desorption kinetics were clearly demonstrated for NaAlH4 doped with Ti and/or Zr catalyst [186, 187]. Ab initio calculations by projected augmented plane wave method indicate that NaAlH4 undergoes a phase transformation from tetragonal- P41/a to an orthorhombic- Cmc21 structure at 6.43 GPa with a 45 % volume contraction [74]. It was also suggested that the orthorhombic phase of NaAlH4 stores more hydrogen volumetrically than the tetragonal phase and would, if stabilized at ambient conditions, be an interesting candidate for further studies with regard to hydrogen absorption/desorption efficiency. Talyzin et al. [188], performed high pressure Raman measurements of NaAlH4 up to 17 GPa. They reported two possible phase transformations: one around 3 GPa which was less obvious as a structural transformation, and a second at 12 GPa which was to an orthorhombic structure. Experimental study of Kumar et al. [73], reports a tetragonal to monoclinic phase transition above 14 GPa. Upon release of pressure, the tetragonal structure was found to reappear at ~4 GPa. In this study, XRD measurements of unmilled or as received NaAlH4 showed the phase transformation to an orthorhombic structure which is in agreement with the prediction of Vajeeston et al. [74], followed by an amorphization at 13.6 GPa. A close analogue, LiAlH4, has a monoclinic structure at ambient conditions with space group P21/c and undergoes a slow transition to a tetragonal phase between 2.2 and 3.5 GPa [69].

It has been reported that ball milling improves the hydrogen storage properties of hydrides including NaAlH4 [180, 182, 183, 189-191]. In general, the enhanced hydrogen sorption properties of hydrides after ball milling have been attributed to: the formation of large surface area, the reduction in grain size, and the introduction of lattice defects [192]. Milling essentially results in increasing the surface to bulk ratio, increasing grain and fault boundary densities that assist diffusion and the rate of H2 sorption. Therefore, it would be of great interest to study mechano-chemically milled NaAlH4 to understand the effect of milling on the structural behavior using high-pressure methods. To understand the possible structure relations with respect to processing conditions of NaAlH4, X-ray diffraction and Raman spectroscopy measurements were performed on both unmilled and milled samples. In-situ measurements were carried out on unmilled NaAlH4 wet with mineral oil and found a structural transformation from a tetragonal to an orthorhombic phase above 8.6 GPa. Above 13 GPa, the sample shows an amorphous behavior. Ball-milled NaAlH4 wet with mineral oil was studied with micro X-ray diffraction using a synchrotron radiation source. Amorphization was started at 6.5 GPa and completed at around 13.5 GPa without any other phase transition. The intensity of the powder diffraction patterns decreased with increasing pressure. The structural transformation was found to be reversible when the pressure was released.

## 8.2. Unmilled NaAlH4

### 8.2.1. Experimental details

In-situ powder XRD and Raman spectroscopy measurements were carried out simultaneously on the NaAlH4 sample of 95 % purity purchased from Sigma Aldrich. A sample wet with mineral oil was used for the study because of high reactivity of the NaAlH4 towards moisture. The sample was loaded along with tiny ruby chips in a DAC of culet size 600 m. Sample chamber was a steel gasket with a hole size of 300 m and thickness 100 m. XRD was carried out using a diffractometer equipped with rotating anode generator (Bruker) and facilitating radiation of wavelength 0.71073 Å. The 2D diffraction data were collected using a CCD detector.

### 8.2.2. Results and discussion

### 8.2.2.1. X-ray diffraction

At ambient conditions, the NaAlH4 has a tetragonal structure with space group I41/a. The lattice parameters of the unmilled sample were found to be a = 5.02629(2) Å and c = 11.3562(7) Å, which gives a unit cell volume of 286.898(4) Å3 that is in good agreement with the previous report [193].  Figure 8.1 shows the angle dispersive X-ray diffraction pattern of NaAlH4 obtained at various pressures upto 15 GPa. It can be noted from XRD results that the phase transformation begins at 8.6 GPa and completes at around 12.4 GPa. The appearance of new peaks at high pressures between 8.6 and 9.5 GPa is a clear indication of the phase transition.

Figure 8. 1: The XRD patterns of unmilled NaAlH4 recorded at various pressures up to 13.6 GPa. Peaks due to orthorhombic phase are marked by asterisks at 12.4 GPa.

It was not possible to obtain the structural parameters above 6.5 GPa because of poor quality of diffraction patterns. The signals became very weak at higher pressures and only two diffraction lines, which can be assigned to (1 0 3) and (2 0 0) atomic planes were observed indicating partial amorphization of the sample [194]. A material can go to an amorphous phase instead of a high pressure phase due to the strong stress effect [195].  Variation of lattice parameters with pressure was determined by structure refinement using Le Bail method. Figure 8.2 shows the obtained P-V plot of unmilled NaAlH4 fitted with third order Birch- Murnaghan EoS.

Figure 8. 2: The P-V plot of unmilled NaAlH4 (circles) fitted with Birch- Murnaghan equation of state (line).

The compression along c- axis was found to be three times that along a- axis of the unit cell of NaAlH4.  The experimental data were fitted with third order Birch-Murnaghan equation of state. Bulk modulus was found to be 25.65 GPa with K0′ constrained to 4 and V0 = 288.3 Å3. Transition to an orthorhombic phase was observed just before amorphization. The transition pressure observed in this study was 2 GPa above the computational result of Vajeeston et al. [74]. Amorphization of unmilled NaAlH4 loaded with mineral oil was observed between 12.4 and 13.6 GPa. The structural parameters were not refined for the orthorhombic- NaAlH4, but the peak positions shows orthorhombic structure with space group Cmc21 similar to that predicted by Vajeeston et  al. [74].

### 8.2.2.2. Raman spectroscopy

Raman spectrum of NaAlH4 obtained at ambient conditions with mode assignment was reported by Ross et al. [196]. Peaks observed in the range of 1600 and 1900 cm-1 are of the Al-H stretching modes, and that between 700 and 950 cm-1 is due to Al-H bending modes, whereas those vibrations lower than 600 cm-1 show the librational and torsional modes which are in good agreement with the literature [74, 188, 196]. Figure 8.3 shows Raman spectra collected at various pressures up to 15 GPa during compression of unmilled NaAlH4.

Figure 8. 3: Raman spectra of unmilled NaAlH4 at various pressures up to 15GPa. The change in Raman modes under pressure are marked with arrow.

From the Raman spectroscopy data, it is evident that the sample becomes amorphous between 12.4 and 15 GPa. A change in the peaks at liberational and stretching mode regions was observed around 3 GPa which are indicated by arrows in Figure 8.3. Raman spectra show changes in the collective vibration modes such as the splitting of the peak at 130 cm-1, and separation of the shoulder at 250 cm-1 and appearance of a peak at 1685 cm-1. Above 3 GPa, the splitting of peak at 210 cm-1 is very prominent and which separates out completely at ~12.4 GPa. Also, splitting of a peak in the region of collective vibration is observed between 9 and 12.4 GPa. The Al-H stretching mode disappears at 1700 cm-1 and reappears at 1800 cm-1. The changes in the vibrational modes of unmilled NaAlH4 with pressure are evident from the Raman spectrum which confirms the phase transformation. The anharmonicities observed by Raman spectroscopy below 3 GPa may be attributed to an inhomogeneous pressure distribution within the sample or the local bonding structure change due to larger compression along c-axis as compared to a- axis. In comparison to the X-ray diffraction data, it is evident that the changes in the Raman spectrum around 3 GPa corresponds to strong changes in the vibrational frequencies caused by distortion of the tetragonal structure and not a phase transition. The experiments were repeated three times with fresh loading of the sample and confirmed the occurrence of the orthorhombic phase around 9 GPa.

## 8.3. Mechano-chemically Milled NaAlH4

### 8.3.1. Experimental details

Powder sample of NaAlH4 having 99 % purity was purchased from Sigma–Aldrich, and was ball-milled for 60 min in a Spex 8000 ball mill machine. A vial with stainless steel balls of diameters 6.35 and 12.7 mm are used to mill the sample at room temperature under a dry argon atmosphere. Milling typically resulted in a reduction of particle size without decomposition. The crystal structure and purity of the milled alanate were checked by XRD. The high-pressure micro X-ray diffraction experiments were performed at 16-IDB at HPCAT of Argonne National Laboratory. The monochromatic beam of wavelength 0.45657 Å was focused to approximately 100 μm2 and the data was recorded by a Mar345 image plate.

The sample was loaded with mineral oil in a Mao-Bell type DAC. A stainless steel gasket with a hole of size 200 μm and thickness 50 μm, was used as the sample chamber. Grains of platinum metal were loaded with the sample as a pressure marker. Analysis of the XRD patterns of the ball-milled sample shows single phase NaAlH4 having tetragonal structure with space group I41/a identical to the unmilled sample. In order to determine particle size, LaB6 crystals of particle size 2 μm were used as the standard. XRD patterns of NaAlH4 (both as-received and ball-milled) and LaB6 were recorded at the same conditions. Lattice parameters were determined from Rietveld structure refinement using GSAS. Refined value of Lorentzian–Scherrer broadening term in the GSAS profile function of LaB6 was used as an instrumental broadening parameter. This value was subtracted from the corresponding broadening term of the NaAlH4 samples to determine diffraction line broadening related to the particle size effect.

### 8.3.2. Results and discussions

Gomes et al. [189], reported decreasing of the unit cell volume and c/a ratio after ball milling which is in agreement with our results. These observations can be attributed to the increase of surface to volume ratio in the particles.  Average particle size (X) was determined using the relation: ; Where K is the Scherrer constant (0.9), λ is the wavelength of X-rays in Å, and Lx is the Lorentzian broadening term in GSAS profile function. From the above equation, particle size of as-received and ball-milled NaAlH4 samples were found to be 1.08 μm and 715 nm, respectively. It was found that ball milling of the NaAlH4 decreases the particle size by ~ 30 %. Figure 8.4 shows the XRD patterns of  the ball milled NaAlH4 collected at various pressures up to 13.5 GPa.

Figure 8. 4: The XRD patterns of the ball-milled NaAlH4 collected at various pressures. Pattern marked * is from decompressed sample, and Pt metal was used as a pressure marker.

Lattice parameters of the ball milled NaAlH4 are determined by Rietveld refinement of the micro XRD data and found to be: a = 4.800(1) Å; c = 10.56(1) Å which gives a unit cell volume of 243.48(2) Å3. From the analysis of the XRD data it is observed that the lattice parameters decrease with increasing pressure with a c/a ratio of ~2.2 is maintained. The amorphization of the ball-milled sample was occurred at approximately 12 GPa, whereas for unmilled NaAlH4 it was at 13.6 GPa. Structural refinement was not possible at high pressures > 6.8 GPa, due to the peak broadening and disappearance of all Bragg reflections other than that of (0 1 3) and (1 1 2). This is an indication of the onset of amorphization of milled NaAlH4. The previous report of XRD study of NaAlH4 indicates a phase transformation to a monoclinic phase which corresponds to the amorphization pressure in our observation. This pressure-induced amorphization must have been influenced by the presence of mineral oil, which can be explained by the variation of the hydrostatic conditions [197]. High-pressure phases were absent in the ball-milled samples as observed from both the micro XRD and Raman spectroscopy experiments. The increase in the surface area (with strong stress effects) to bulk volume ratio, resulting from ball milling could have forced the system to an amorphous phase, as an easier path during the phase transformation [195].

The experimental P-V data were fitted with a third order Birch– Murnaghan equation of state using the Marquardt–Levenberg least square procedure with a sigma plot program. Figure 8.5 shows the behavior of unit cell volume with pressure and the EoS fit with K0′ constrained to 4. The ball-milling of NaAlH4 caused an increase of  K0 from 25.3(1) to 52.16(1) GPa, which is a surprisingly large positive effect. This can be attributed to the lattice defects induced during milling. The experiment was repeated two times to confirm the amorphization pressure and presence of the high-pressure phase. The difference in properties of ball milled sample from that of milled NaAlH4 may be caused by the size-induced pressure effect due to larger surface area in the material when compared to their bulk or due to the lattice defects generated during milling [198, 199]. To check the size effect with pressure, milled NaAlH4 was loaded with mineral oil and the XRD pattern was recorded up to 11.45 GPa. The pressure was then released to 2 GPa and once again increased to 13.5 GPa but did not observe any changes other than the amorphization. No high-pressure phase was observed prior to amorphization contrary to the unmilled NaAlH4. Hence, it can be concluded that pressurizing the sample to 11 GPa did not have any effect on the particle size.

Figure 8. 5: Birch Murnaghan EoS fit (line) to the P-V data (circles) of ball milled NaAlH4.

# CHAPTER 9. HIGH PRESSURE INVESTIGATION OF

# STRUCTURAL STABILITY OF LiAlH4

9.1. Introduction

High-pressure modification of lithium alanate (LiAlH4) reported to be a very interesting material for hydrogen storage applications, if it could be stabilized upon release of pressure [71].  LiAlH4 and NaAlH4 have received considerable attention due to their high theoretical hydrogen storage capacities and light weight [200]. Under ambient conditions LiAlH4 has a monoclinic structure with space group P21/c and four formula units per unit cell [201]. The structure consists of AlH4‾ units separated by Li+ ions, and the hydrogen atoms are arranged around the aluminum atoms in an almost regular tetrahedral configuration. According to the computation results of Vajeeston et al. [71], the monoclinic phases of LiAlH4 transforms above 2.6 GPa into a tetragonal- I41/a structure which is  isostructural to that of the ambient phase of NaAlH4 with a volume collapse of 17 %. Again, at 33.8 GPa, LiAlH4 undergoes a transition from tetragonal to an orthorhombic- Pnma structure [71].

Existing experimental data on high-pressure phase transformations of LiAlH4 are relatively old and were obtained using ex- situ methods [72, 202]. High- pressure Raman spectroscopy experiments of LiAlH4 by Talyzin and Sundqvist [70], and Chellappa et al. [69], confirmed a phase transition between 2 and 3.5 GPa. However, compression studies of LiAlD4 using neutron diffraction by Pitt et al. [203], showed no transitions up to 7.15 GPa, and a two-phase mixture was observed on increasing temperature above this pressure. A reversible phase transition at ambient temperature was impossible to observe in such experiments, but the low pressure monoclinic phase of LiAlH4 was recovered after pressure treatment up to 9 GPa. The tetragonal and orthorhombic phases reported in these early studies were observed only when high pressure was combined with high-temperature treatment. High pressure phase transitions of pure LiAlH4 investigated using in situ Raman spectroscopy and computation which shows that  ~3 GPa the ambient monoclinic- P21/c phase of LiAlH4 transform to a high pressure phase with a distorted AlH4- tetrahedron  [69, 70]. The phase transition is reversible below 1.4 GPa on decompression. In this study, in situ XRD and Raman spectroscopy measurements were carried out on the LiAlH4.

## 9.2. Experimental Details

The powder sample of LiAlH4 was obtained from Sigma Aldrich. The sample used for the study was loaded in DAC with mineral oil to avoid its reaction to moisture.  The X-ray diffraction pattern were collected in steps of pressure using a rotating anode generator (Brucker) with facilitating radiation of wavelength 0.71073 Å. Raman spectrum were recorded is steps of pressure up to 50 GPa. Ruby fluorescence method was used for the pressure measurement.

## 9.3. Results and Discussion

### 9.3.1. X-ray diffraction

The analysis of powder X-ray diffraction pattern of LiAlH4 collected at ambient conditions  suggest that it has a monoclinic- P21/c structure with lattice parameters; a = 4.858(3) Å, b = 7.832(6) Å, c = 7.909(2) Å and β = 112.53º.  A high pressure phase transition at room temperature was observed above 2.16 GPa. Figure 9.1 shows the XRD patterns collected up to 23 GPa at some selected pressures during compression.

Figure 9. 1: Comparison of the high pressure XRD patterns of LiAlH4 collected at room temperature.

The change of unit cell volume with pressure has been determined from the analysis of XRD patterns. The P-V data thus obtained was fitted with third order Birch- Murnaghan EoS (Figure 9.2). The bulk modulus of the ambient phase is found to be 13.87 GPa with a K0′ = 4 and V0 = 300.58 Å3 which agree with the theoretical calculations [71].

Figure 9. 2: The P-V data (circles) obtained for monoclinic phase of LiAlH4 fitted with third order Birch-Murnaghan EoS (line).

### 9.3.2. Raman spectroscopy

Figure 9.3 shows the Raman spectrum of monoclinic phase collected at ambient conditions. The strong characteristic peaks observed between 1600 and 1850 cm-1 are due to Al-H stretching modes. Al-H bending modes are found in the range 700-1500 cm-1.  The liberational and translational lattice modes are very weak and observed between 270 and 550 cm-1. Raman spectra collected at high pressures show that a change in the vibrational modes occurs between 3.3 and 6.3 GPa. This can be attributed to a monoclinic to tetragonal structural phase transition. The phase transformation predicted by Vajeeston et al. [71], at 33 GPa from computation was not observed in the Raman spectroscopic studies up to 50 GPa. Softening of Al-H stretching modes and corresponding shift to lower frequencies were observed beyond the transition pressure. The pressure quenched high pressure phase shows the Al-H stretching mode shift again to lower frequencies, suggesting a weakening of the Al-H bond. A weaker Al-H bond of the high pressure phase of LiAlH4 implies its structural instability. Therefore it is hypothesized that similar structural changes may be possible due to increased coordination number of Al3+ and the formation of AlH6 octahedra by ball milling of LiAlH4, which will result in enhanced dehydrogenation kinetics [69].

Figure 9. 3: Raman spectrum of LiAlH4 in at ambient conditions (dotted line) fitted with a Gaussian profile function.

Figure 9.4 shows a comparison of the Raman spectra of LiAlH4 collected at various pressures up to 6.3 GPa. Between 3.3 to 6.3 GPa, the structural phase transition is evident from the  appearance of a strong new peak at 1668 cm-1 and the disappearance of the Al-H stretching modes of monoclinic- LiAlH4.

Figure 9. 4: Raman spectra of LiAlH4 collected at various pressures and at room temperature.

# CHAPTER 10. PRINCIPAL COMPONENT ANALYSIS ON

# PROPERTIES OF BINARY AND TERNARY HYDRIDES

## 10.1. Introduction

Material informatics is a developing area in material science in which a new knowledge system is built by collecting and classifying information with the help of calculations and databases. If experience and knowledge, captured and preserved in a database format, it helps to investigate new materials efficiently. The abundance of parameters causes difficulties in the interpretation of their relation. Many datum sets can be correlated to define a single material property with the help of a mathematical technique. The main challenge in this field is the difficulty in correlating many properties of different set of materials. Most of the classical analytical methods for finding characteristics of data set are very laborious and time consuming.

Lot of experimental and theoretical work has been done on hydrides in search of a suitable material. A detailed hydride research database is required for proper retrieval of information already available.  Data were collected from available journal publications and constructed a property database. Data sets in the hydride database can be correlated to define a single material property using an available mathematical technique such as principal component analysis (PCA) which is a widely used tool for dimensionality reduction and for visualization of variable patterns.  In this work, only binary (of the form MHx, where x = 1, 2 or 3 and M is a metal) and ternary (of the form AaBbHx, where a, b and x are integers and A, B are metals) metal hydrides have been considered. Other hydrides were excluded from the study due to the presence of large missing data and associated error on analysis. This work investigates correlation among material properties using PCA method.

## 10.2. Data

The property data  include but not limited to specific heat (Cp), entropy (S), molar volume (V) and hydrogen weight percentage (H wt %) of metal hydrides as well as the sum of elemental properties of the metals corresponds to each compound and constructed a database. Light metal hydrides of alkali and alkali-earth elements have good hydrogen storage capacity but operation temperature is very high while transition metal hydrides (eg. LaNi5H6) release H2 at room temperature but with less storage capacity.  In order to understand property interrelationships of hydrides PCA have been carried out by considering the properties such as entropy of metal hydrides (SMH), molar volume of metal hydrides (VMH), sum of specific heat of metals (CpM) in each hydride, specific heat of metal hydrides (CpMH), sum of entropy of metals (SM) in each hydride, hydrogen weight per cent (H w%) of hydrides and sum of the molar volume of metals (VM) in each hydride. Only these properties have been included in the current study due to the unavailability of enough data on other properties.

## 10.3. Method

The property data of both binary and ternary hydrides are used for the study of their interrelationships. If there are large number of variables and some of which are correlated, it is required to consider only fewer variables that capture maximum variation in the original data set.  For this purpose, a better approach is to consider all properties and carry out principal component analysis. PCA can reveal certain characteristics or combinations of the original variables that mostly determine the structure of the data distribution which may not be related to known influencing factors in the data set. PCA is one of the widely used techniques for dimensionality reduction with widespread applications to pattern recognition, data classification, exploratory data analysis, economics, life sciences, chemistry, geology and material science [204-208]. Due to fascinating interrelationships of material properties, use of PCA analysis has wide application in material science.

The data reduction in PCA is achieved by transforming variables to principal components, which are uncorrelated (orthogonal) and ordered so that the first few retain most of the variation in the total set of original variables with descending importance. If some of the variables in data set are correlated, only a minimum number of linear combinations are needed to describe most of the variability in the data set. Correspondingly, for less-correlated data sets, more combinations are necessary. Such linear combinations are called principal components (PC). As an example, if the first three components explain ~90 % of the variability among the original data set of 10 variables, the number of variables to be analyzed has been reduced from 10 to 3. In PCA the initial data matrix is represented as the inner product of row/ score matrix and column/ loading matrix. The row matrix has the dimensionality r x n, where r is the number of observations (i.e., compounds) in the initial data set, and n is the number of principal components. The column matrix has the dimensionality n x c, where c is the number of observable properties (variables) in the initial data set. In a plot of a score vector against another score vector, compounds with similar properties will cluster [209-211].

PCA analyses have been carried out by forming a matrix with columns as hydride properties and rows corresponds to various hydrides. Based on the matrix diagonalization procedure in SPSS- 15 (Statistical Package for Social Sciences), principal components (eigenvectors) of the matrix were obtained. The eigenvectors are termed component loadings and they are used to calculate the component scores. PCA eigenvectors provide information about contribution of each variable to a component. This study helps to correlate variables having common behavior and hence to classify hydrides with respect to their chemical or physical nature.

The PCA option for factor analysis (FA) in SPSS is used in this study. FA is solely concerned with correlations among variables. The methodology of FA is very similar to PCA except that unique variability is excluded from the analysis. The output from the SPSS program is not identical to that of generally used PCA analysis. By default it will only extract factors whose eigenvalue is greater than one. By adjusting the number of factors equal to variables it is possible to overcome the difference between PCA and FA. Then the communalities (sum of the common components) are all 1.00 thus all the variability is assumed to be common. In SPSS, factor loadings (component matrix) are eigenvector normalized by the square root of its eigenvalue. The actual PCA can be found from the eigenvectors of the loadings by dividing each loading with the square root of the eigenvalue. The PCA derive a small number of linear combinations (PCs) of a set of variables that retain most of the information in the original variables. The projection of variables onto a PC is called scores. Plots of the scores for two or more PCs help us to find graphically the similarities and differences among variables. The distance between points in a score plot shows if they are similar or different [205]. Thus it may be able to find materials with similar properties (corresponds to closer points) which will help us to select new hydrides for particular applications.

Because of randomly distributed missing data in the dataset, pair wise deletion option is used in PCA to have a reasonable result.  To achieve a clear pattern of coefficients, PC axes can be rotated in any direction without changing the relative locations of the points to one another with a change in actual coordinates of the points. The rotated solutions explain the same amount of variance as the original solution [212]. Varimax method of orthogonal rotation is an analytical way for rotation of PC solutions. The varimax rotation maximizes the sum of the variances of the squared coefficients within each eigenvector while the rotated axes remain orthogonal. The varimax normalised rotation has been carried out to maximize the values of the loading factors of each compound analyzed.

## 10.4. Results and Discussion

A data set of hydride properties with ~200 compounds is interpreted.  PCA has been carried out on a set of data which consists of both binary and ternary hydrides as well as on sets of data which contain just binary or just ternary hydrides. Figure 10.1 shows eigenvalues and the variance explained by each principal components (PCs) obtained from the analysis of a set of data with both binary and ternary metal hydrides. Number of factors to be considered for extracting proper information is determined from the screeplot (plot of eigenvalue versus component number) and the percent variance. From the sudden fall of eigenvalues or the loadings of PCs (Figure 10.1) it is obvious that the first two PCs (which explains 62.89 % and 30.15 % variance, respectively) reduced the seven dimensional data set to a two dimensional data set, with an average 6.96 % loss of detail.

Figure 10. 1: Eigen value and total variance explained by each component obtained from PCA of a set of data with both binary and ternary metal hydrides.

The component matrix obtained after applying varimax rotation from PCA of a set of data which contain both binary and ternary hydrides is shown in Table 10.1. First column represent the variable and next seven columns represent eigenvectors correspond to the seven components. Contribution of first five variables to component one and last two variables to component two are considerable defining an arbitrary limit of 0.75. The correlation matrix for this analysis is given in Table 10.2. In order to evaluate the correlation between variables, it is important to know the magnitude or strength of the correlation coefficient (Table 10.2) as well as the significance of the correlation. The results show correlations among CpM, CpMH, SMH, and VMH.

Table 10. 1: The component matrix obtained from PCA of a set of data with both binary and ternary hydrides. Subscript M denotes metal and MH abbreviates metal hydride.

Property Components

1 2 3 4 5 6 7

SMH 0.984 0.085 -0.086 0.004 -0.120 -0.024 -0.033

VMH 0.968 -0.019 0.036 -0.233 0.068 0.014 -0.039

CpM 0.935 0.216 -0.185 0.192 0.074 -0.051 0.002

CpMH 0.872 0.471 -0.013 -0.110 -0.019 0.013 0.070

SM 0.759 -0.628 -0.022 0.143 -0.001 0.087 0.003

Hwt% 0.208 0.901 0.360 0.116 0.003 0.024 -0.018

VM 0.491 -0.792 0.360 0.011 -0.002 -0.051 0.017

Table 10. 2: Correlation matrix obtained from PCA of a set of data with both binary and ternary hydrides. M and MH abbreviates metal and metal hydride, respectively.

VM SM CpM CpMH VMH H wt% SMH

VM 1.000 0.859 0.226 0.049 0.499 -0.482 0.386

SM 0.859 1.000 0.602 0.352 0.714 -0.398 0.694

CpM 0.226 0.602 1.000 0.897 0.855 0.343 0.948

CpMH 0.049 0.352 0.897 1.000 0.857 0.587 0.899

VMH 0.499 0.714 0.855 0.857 1.000 0.171 0.940

Hwt % -0.482 -0.398 0.343 0.587 0.171 1.000 0.251

SMH 0.386 0.694 0.948 0.899 0.940 0.251 1.000

The plot of first two PCs obtained from PCA of a set of data which contain both binary and ternary hydrides is shown in the Figure 10.2. The selected properties are found to be confined to PC1-PC2 plane of the component plot which suggests that the first two components explain most of the variability in the data set as predicted from the screeplot.

Figure 10. 2: Component plots for a set of data with both binary and ternary hydrides.  Subscript M denotes metal and MH denotes metal hydride. S- entropy, Cp- specific heat, V- molar volume and H wt %- hydrogen weight percent in each compound.

As two PCs cover ~93 % of the variance, plot of first two component scores is enough to visualize any possible patterns. From the score plot, shown in Figure 10.3, it can be observed that the ternary hydrides exhibits different phenomenon compared to binary hydrides. Therefore PCA of binary and ternary hydrides were carried out separately.

Figure 10. 3: Plot of score 2 versus score 1of a set of data with both binary and ternary hydrides.

The score plots obtained are presented in Figures 10.4 and 10.5.  The outliers found in these plots can be due to erroneous data for corresponding compounds. The score plots help us to select materials for specific applications from its position in the plot. The clustering of various hydrides in the score plots gives insight into similarity in their properties. If the PCA plots show interrelationship among many properties, it is not required to study all the properties of a hydride to determine its overall performance.

Figure 10.  4: Plot of scores of first two principal components for binary hydrides.

Figure 10.  5: Plot of scores of first two principal components for ternary hydrides.

# CHPATER 11. INVESTIGATION OF MIXTURES OF HYDRIDES

## 11.1. High Pressure Raman Spectroscopic Investigation of LiNH2BH3

### 11.1.1. Introduction

Ammonia borane, NH3BH3, is a promising candidate material for hydrogen storage with 19.6 wt % of H2. A thermal decomposition of pure ammonia borane proceeds in three steps and the release of all the hydrogen atoms occur only above 500 °C. NH3BH3 releases hydrogen via catalyzed hydrolysis in an aqueous solution [213, 214], catalyzed dehydrocoupling under non-aqueous conditions [215, 216], or thermolysis at elevated temperatures [217, 218]. Catalyzed dehydrogenation, such as acid-catalyzed solvolysis significantly reduces gravimetric density of the material due to the presence of solvent. As a hydrogen storage material, NH3BH3 also face drawback of difficulty in its regeneration after dehydrogenation. Decomposition of pure NH3BH3 releases volatile byproducts like borazine that are unfavorable for fuel cell operation. The release of first equivalent of H2 from NH3BH3 typically occurs upon its melting at 110 ºC. The subsequent release of the second equivalent of H2 occurs above 130 ºC, but is generally concurrent with the generation of borazine,(BH)3(NH)3, and diborane (B2H6) gas impurities.

Xiangdong et al. [219, 220], reported that mechanically milling 1:1 mixture of ammonia borane and lithium hydride yields a destabilized hydrogen storage material, lithium amidotrihydroborate (LiNH2BH3). It has a hydrogen storage capacity of around 10 wt %. Advantage of LiNH2BH3 is that it can release over 7 wt % pure hydrogen at around 100 ºC, free of gas impurities. The decomposition temperature of the NH3BH3 sample destabilized by LiH was found to be lowered to 80 ºC. LiNH2BH3 has an orthorhombic- Pbca structure at ambient conditions [221]. The enthalpy of the reaction: NH3BH3+ LiH LiNH2BH3+ H2↑, is -16 kcal/mol [222]. The decomposition reaction may be a two step process: LiNH2BH3 LiNHBH2+ H2LiNBH+ H2.

The lightest metal hydride, LiH, has 12.5 wt % hydrogen content and 0.1 MPa equilibrium hydrogen pressure at 910 ºC. The ambient phase has a cubic structure which is much compressible and densely packed [49]. Stephens and Lilley [51], investigated LiH with isotopic substitution at room temperature. High pressure experiments revealed that LiH is stable under compression up to 36 GPa  [52, 223]. The computationally predicted high pressure phase transition of LiH is at 0.66 TPa [53]. Melting curve of LiH under compression was computed up to 200 GPa and 2725 ºC by Ogitsu et al. [224], and observed a change in electronic structure of the compressed melt at high temperatures.

The H-H interaction between the protonic (N-H) and hydridic (B-H) hydrogen atoms of adjacent molecules attributes to the high melting point of NH3BH3 as compared to similar compounds. Neutron diffraction studies at low-temperature show that in NH3BH3, the N–H…H–B interactions has the shortest H…H bond length of 2.02 Å. This is shorter than the the van der Waals distance (2.4 Å) between the H atoms. Under  ambient conditions, NH3BH3 crystallizes in a tetragonal- I4mm structure with a unit cell containing two molecules. At low temperature of about –48 ºC, NH3BH3 exhibits a first order rotational order-disorder phase transition to an orthorhombic-Pmn21 structure [225]. Raman spectroscopy studies of NH3BH3 shows that the vibrational modes involving the NH3 group show negative pressure dependences whereas that of BH3 group have a positive shift, which support the existence of the dihydrogen bond [226].

Raman spectroscopy studies of NH3BH3 at high pressures by Lin et al. [227], observed N-H stretching modes in the range 3170- 3320 cm−1. Changes in the N-H stretching region were occurred at 5, 12 and 14.4 GPa during compression. The B–H stretching modes (2200 and 2700 cm−1) and B-N stretching modes (700- 1000 cm-1) show transitions at 2 and 12 GPa [227]. B-H bending vibrational modes was observed at 1171 and 1192 cm−1. The results suggest that NH3BH3 shows three phase transitions at approximately 2, 5, and 12 GPa [227]. At 2 GPa, the asymmetric B–H stretching mode, the asymmetric B–H bending mode, as well as the low frequency rocking mode started to split into two modes. Around 5 GPa, coalescence of the asymmetric N–H stretching mode, as well as the splitting of the combined B–H and N–H rocking modes occurred. It is proposed that NH3BH3 is dimerized at high pressure, forming diammonite of diborane, H2B(NH3)2BH4. Ammonia borane shares the same empirical formula (BNH6) with diamonite of borane and are products of symmetrical and unsymmetrical cleavages of borane by ammonia, respectively.

Chitra et al. [228], investigated pressure- induced structural transformations of diborane (B2H6) using in situ Raman spectroscopy. Diborane is found to exist in the liquid phase up to pressures of less than 4 GPa.  At 4 GPa, it undergoes a liquid- solid phase transformation to a new high- pressure phase with a possible structure similar to that of its low- temperature orthorhombic phase. Again, above 6 GPa a new phase with a possible extended network structure of higher hydrides of borane has formed. At pressures above 14 GPa, diborane transforms to a third high-pressure phase. All of the observed pressure-induced structural transformations of B2H6 are completely reversible upon decompression. In the present study, LiNH2BH3 is investigated under pressure using in situ Raman spectroscopy experiments. Because of poor quality of Raman spectra collected in the bending mode region, only the B-H and N-H stretching modes are analyzed in detail.

### 11.1.2. Results and Discussions

Raman spectroscopy studies of LiNH2BH3 were conducted at ambient and high pressure conditions on both compression and decompression. Table 11.1 lists the vibrational modes observed for LiNH2BH3 at ambient conditions.  Figures 11. 1 and 11.2 shows the obtained Raman spectrum of LiNH2BH3 collected at ambient conditions from the sample loaded in a quartz capillary. In comparison to the computational results of the vibratonal modes by Lee et al. [229], it can be concluded that the Raman spectrum collected at ambient condition is that of pure LiNH3BH3. Because of low intensity of B-H and N-H bending modes collected from DAC, only B-H and N-H stretching regions are considered for further analysis. After loading the sample in a DAC, the Raman spectrum of the sample is different from the as synthesized phase which was confirmed in repeated experiments. Results show that the LiNH2BH3 sample just closed in DAC (< 0.1 GPa) undergoes partial transition/decomposition. Figure 11.3 shows images of the sample chamber at different pressures. Portion of the sample which is transparent (W) and opaque (D) to light are marked in the image at 4.2 GPa.

Figure 11. 1: Lattice, bending and B-H stretching modes in the Raman spectrum of LiNH2BH3, collected at ambient conditions fitted with a Gaussian profile function.

Figure 11.4 shows Raman spectra of the sample at different pressures collected from both W and D regions. The Raman shift frequencies of B-H and N-H stretching modes at 4.2 GPa which corresponds to two different phase regions, D and W, are listed in Table 11.2. The frequencies given in bold letters in the table can not be due to LiNH2BH3. The dark regions in the sample can be a two phase region which contains an unidentified phase along with LiNH2BH3. The high pressure phase transitions were reversible on decompression. The decompressed patterns show LiNH2BH3 in both W and D regions.

Figure 11. 2: N-H stretching modes in the Raman spectrum of LiNH2BH3, collected at ambient conditions fitted with a Gaussian profile function.

W

D

4.2 GPa			  17.2 GPa 			DP0

Figure 11. 3: The sample loaded in DAC with two phase regions marked W and D at different pressures. DP0 implies decompressed sample at ambient conditions.

Figure 11. 4: Raman spectra of LiNH2BH3 during compression (right) and decompression (left) for the regions W (top) and D (bottom), respectively.

| LAB | AB [230] |  | LAB | AB [230] | LAB | AB [230] |
| --- | --- | --- | --- | --- | --- | --- |
| Bending/str. |  |  | B-H str. | B-H str. | N-H str. | N-H str. |
| 806.01, 800* | 727 | N-B-H rock | 2016.9 | x | 3271.09, 3197* | 3176, 3195* |
| 819.968 | 784 | B-N str. | 2141.32, | x | 3301.85, 3253* | 3250, 3253* |
| 834.154, 842* | 800 | B-N str. | 2143.72 2148* | x | 3303.19, | 3316, 3314* |
| 862.465 | x |  | 2182.37, 2196* | x | 3355.82 3359* |  |
| 903.248, 901* B-N str. | x |  | 2200.69 | x | 3359.5 |  |
| 910.905 | x |  | 2226.71 | x | 3664.92, 3675* |  |
| 1021.78, 1016*, 1066* | 1065 | N-B-H rock | 2237.66 2287* | 2279, 2287* |  |  |
| 1132.58 | 1155 | BH3 | 2308.96 | 2328 |  |  |
| 1177.97, 1177* B-H | 1189 | BH3 | 2354.97, 2349* | 2375 2343* |  |  |
| 1261.03 | 1357 | NH3 |  |  |  |  |
| 1261.31, 1261*, B-H 1381* | 1450 | ov |  |  |  |  |
| 1534.8, 1543*, N-H 1616* | 1600 | NH3 |  |  |  |  |

Table 11. 1: Raman shift frequencies in cm-1for LiNH2BH3 (LAB) in this study at ambient conditions in comparison with that of NH3BH3 (AB); str. Abbreviates stretching modes. The mode frequencies marked * are from FTIR study [229].

The peak observed at 3664 cm-1 is very weak at ambient conditions, but is stronger in the Raman spectra collected from the LiNH2BH3 sample loaded in a DAC. Lee et al. [229], observed a peak at 3675 cm-1 in FTIR study which was unidentified. They proposed that it may be due to an impurity of –OH or –NH origin. It can not be due to a Li related mode because that is observed around 1380 cm-1. Other possibilities of origin of the peak at 3675 cm-1 was suggested to be due to disordered orientations of NH3 and BH3 groups in the sample or an effect of peak splitting due to crystal field. This peak disappears above 4.2 GPa with the observed phase transition and hence it may conclude that the peak at  3664 cm-1 is of LiNH2BH3. The observed phase separation can not be due to inhomogeneus pressure distribution, as the opaque region is not only located at the center of the sample chamber but also at the corners of the gasket hole. The sharp ruby fluorescense spectra  observed during compression also suggest somewhat hydrostatic conditions in the sample. High precausion was taken while loading the sample in the DAC in an argone atmosphere of the glove box. Therefore, reaction with moisture is least expected. Another possibility is the exposure to laser and the heating effect. This was sorted out after long time laser exposure to both transparent and opaque regions without any change. Therefore, it is expected that the phase separation is due to partial decomposition of LiNH2BH3.  The Raman spectra at any pressure does not show any hydrogen peaks. Above 14 GPa, similar spectra was obtained from sample in both regions and the sample was found to be transparent to light above this pressure. Hence, it may be concluded that there may be a slow chemical reaction in the sample under pressure which completes around 14 GPa and the sample become the unidentified new phase above this pressure.

Table 11. 2: B-H and N-H stretching modes of the LiNH2BH3 in cm-1 at 4.2 GPa as observed from Raman spectra of two different phase regions, D and W. The wave numbers given in bold are of an unidentified phase.

| D | W | D | W |
| --- | --- | --- | --- |
| 2309.61 | 2317.27 | 3157.22 | 3157.12 |
| 2327.62 | 2332.94 | 3234.76 | 3234.13 |
| 2329.96 | 2334.34 | 3239.16 | 3237.94 |
| 2378.98 | x | 3257.33 | x |
| 2379.84 | 2392.01 | 3266.69 | 3270.21 |
| 2421.87 | 2425.58 | 3296.16 | 3295.75 |
| 2449.54 | 2466.52 | 3306.38 | 3309.17 |
| 2486.48 | x | 3331.15 | x |
| 2511.57 | 2514.68 | 3386.41 | x |
|  |  | 3393.75 | x |
|  |  | 3513.64 | 3513.41 |
|  |  | 3516.23 | 3514.95 |
|  |  | 3679.03 | 3679 |

Figure 11.5 shows the change of Raman shift frequency with pressure for both W and D regions. It may be concluded that the W portion is pure LiNH2BH3 up to 4.2 GPa and above which it undergoes a phase transition. The D portion is a mixture of LiNH2BH3 and an unidentified phase. From the Raman shift versus pressure plots, the phase boundaries can be indentified at 4.2, 9 and 15 GPa in W region. Whereas, in the D region, the phase boundaries can be marked between 11-12 and 14-15 GPa. In this experiment, Raman spectra were collected from the D region only above 4.2 GPa. A repeated experiment shows a phase transition of the D region below 5 GPa as well. Therefore it may be summarized that LiNH2BH3 undergoe three phase transitions around 5, 10 and 14 GPa.

Figure 11. 5: Change of Raman shift  with pressure for LiNH2BH3 during compression of B-H  (left) and N-H (right) stretching modes for the regions W (top) and D (bottom), respectively.

The N-H stretching modes in the region W show softening similar to NH3BH3 under pressure where as the spectra from region D show mixed behavior (both compression and softening of different modes) which also confirms the existence of structurally different phases in that region. The electron density can be tuned with rapidly reducing volumes upon compression [228]. Therefore, pressure-induced chemical reactions are highly possible in borane complexes. Drastic spectral changes observed above 6 GPa in diborane was suggested to be due to enhanced intermolecular interaction with a covalent nature. At higher pressures, as the mobility of the atoms is restricted, the most facilitated phase transformations are the ones which are not associated with large atomic movements. Hence, in a similar way the formation of higher hydrides may be possible in LiNH2BH3 without drastic changes in the atomic positions at high pressures [228].

## 11.2. High P-T investigation of mixture of MgH2 and AlH3

### 11.2.1. Introduction

Magnesium alanate, Mg(AlH4)2, is an interesting complex metal hydride with 9.3 wt % of hydrogen content. Computational studies suggest that at ambient conditions, Mg(AlH4)2 is of trigonal- P‾3m1 structure which transform to a monoclinic- C2/m structure around 0.68 GPa. Above 10.28 GPa, transition to an orthorhombic- Pbca structure is expected [77]. The decomposition of Mg(AlH4)2 occurs in three steps, first in the range 110- 200 ºC, and second and third around 240- 380 and 400 ºC, respectively [31]. By the second step, hydrogen is fully released and the third step corresponds to the formation of Al3Mg2. The enthalpy of reaction for MgH2+ 2AlH3 Mg(AlH4)2 is calculated in the range 11-29 kJ/mol and for AlH3+ MgH2 MgAlH5 it is 12 kJ/mol, which suggest that both are endothermic processes which may occur in the same temperature range [231].  In an earlier study, Mg(AlH4)2 was synthesized by ball milling the mixture of AlH3 and MgH2 and its decomposition enthalpy was reported as ~0 kJ/ mol H2 [232].  Aim of this study was to synthesize Mg(AlH4)2 under high P-T conditions from the stochiometric mixture of AlH3 and MgH2.  The sample was heated under pressure up to 150 ºC in steps and the results indicate a reaction has occurred and an unidentified new phase has been formed.

Aluminium hydride is a covalent binary hydride which usually forms polymeric compound (AlH3)n and exist in more than six crystal structures depending on synthesize and processing conditions [158]. AlH3 has a hydrogen content of 10.1 wt % and decomposes into elements in one step. The decomposition temperature is in the range 60- 200 ºC for different polymorphs of AlH3. The hydrogenation of Al needs about 2.5 GPa of H2 pressure. The AlH3 phases are metastable at room temperature possibly due to the Al2O3 layer formation. The rhombohedral phase of AlH3 has a reported decomposition temperature of 175 ºC, and a 1 hr ball milling reduces it to 125 ºC. Sandrock et al. [233], report that controlling particle-size and doping of AlH3 with small levels of alkali-metal hydrides results in accelerated desorption rates. It is found that addition of 20 mol % of LiH reduces the desorption temperature of AlH3 to below 100 ◦C which is good enough to supply vehicles. In the present study a rhombohedral– R-3C polymorph (α-AlH3) has been used.

High pressure investigations show that α-AlH3 exhibit a monoclinic distortion around 8 GPa and it has a bulk modulus value of 40 GPa [234, 235]. The reduced cell volume at high pressure is accommodated by an octahedral tilting and a decrease of the Al-H bond distance. The formation enthalpy for the rhombohedral phase of AlH3 is reported to be around −8.2 kJ/mol H2 and it has absolute entropy of 20 J/K mol H2. High-pressure experiments have demonstrated that Al absorbs hydrogen and form aluminum hydride at 2.8 GPa of H2 pressure at 300 °C [236].

MgH2 contains 7.7 wt % of hydrogen and the decomposition temperature is more than 325 °C. Several high pressure phases have been observed under 19 GPa for MgH2 which are of tetragonal- P42/mnm (0- 5.5 GPa), orthorhombic- Pbcn (5.5- 9.5 GPa), cubic- Pa‾3 (9.35- 10.36 GPa) and orthorhombic– Pbca (above 10 GPa) structures [60]. The orthorhombic- Pbcn and tetragonal phases coexist up to 9.5 GPa. MgH2 can be synthesized by low cost means; however its enthalpy of formation is much higher which is around -76 kJ/mol [61]. Equilibrium pressure of MgH2 is found to be about 0.1 MPa at 275  ºC and for a mixture of MgH2/Si it is around 10 MPa at 150 ºC [50, 237]. Thermodynamic properties of MgH2 were computed up to 1273 ºC which indicates an enhanced hydrogen property for this material at high temperature [238]. The bulk modulus for different polymorphs of MgH2 has been determined in the range 44- 50 GPa. The computationally determined transition pressures are found to be lower than the experimental values [239]. Among the high pressure phases, Pbcn structure of MgH2 is stable under ambient conditions owing to its structural similarity with the P42/mnm system.

Compared to other alkali- earth metal hydrides, MgH2 has more number of phases at high pressures and temperatures. Slow diffusion and kinetics prevent usage of MgH2 as an efficient candidate for hydrogen storage. MgH2 can be synthesized under pressure and temperature of 3 MPa and 440 ºC, respectively [240]. Bortz et al. [241], studied neutron powder diffraction of Pbcn-MgH2 formed by heating tetragonal phase to 800  ºC at 2 GPa and quenching to ambient conditions. The reverse transition of orthorhombic to tetragonal phase occurs at 1 atm and 297 ºC. The orthorhombic and tetragonal phases are also found to be coexisting in the pressure ranges 2-8 GPa and 250-900 ºC other than between 5.5 and 9.5 GPa at room temperature [60, 241].

### 11.2.2. Results and discussions

### 11.2.2.1. X-ray diffraction

X-ray diffraction experiments were conducted using a Mo radiation of  λ = 0.71073 Å and synchrotron source with λ = 0.495937 Å. The loaded DAC was heated ex- situ in an oven. Figure 11.6 shows micro XRD patterns collected using a synchrotron source at room temperature after heating the sample at different pressures. The XRD pattern collected at ambient conditions shows the sample is a homogeneous mixture of MgH2 and AlH3. After heating at 110 ºC and 0.7 GPa for more than 12 hrs, the XRD patterns show MgH2 and Al. This imply decomposition of AlH3 at this pressure and temperature. When pressure was increased to 3.4 GPa, a shoulder was observed in the Al peak which may be due to a partial reaction of Al with MgH2 and H2.  Pure Al metal do not show any phase transition up to 27 GPa [242]. After increasing pressure to 7.2 GPa,  the sample was again heated at 150 ºC for about 12 hrs and found new peaks in the XRD pattern which was stable on decompression. Therefore we may conclude that some of the new peaks observed after heating at 7.2 GPa is due to orthorhombic- Pbcn phase which coexist with tetragonal- MgH2 up to 9.5 GPa. The highest pressure achieved in the present experiment was ~9 GPa which is below the complete transition pressure of MgH2. Therefore, even after release of pressure both MgH2 phases were present along with Al and an unidentified phase. The experimental results show that Mg(AlH4)2 formation did not occur as expected.

Figure 11. 6: The micro XRD patterns of mixture of AlH3 and MgH2 collected at various pressures and room temperature.  Abbreviations: bh- before heating, ah- after heating.

Figure 11.7 shows there are two unidentified peaks  at  2θ~ 13o  and ~ 14.5 o  which may corresponds to a new phase. Appearance of a new peak was also observed in Raman spectroscopic study ~3.4 GPa suggesting a partial reaction between MgH2, Al and H2 around this pressure. The expected reaction of Al and H2  was not occurred above 2.8 GPa which may be due to the low partial pressure of hydrogen in the sample chamber.

2θ (degrees)

Figure 11. 7: The XRD pattern from decompressed sample at room temperature after heating under pressure up to 9 GPa matched with peaks corresponds to MgH2 (shorter lines) and Al (longer lines).

Rietveld analysis of the obtained XRD pattern  shows that the sample, after high P-T treatment, is not a single  phase like MgAlH5, but a mixture of two or three phases. MgAlH5 is a possible decomposition product of magnesium alanate in the temperature range 120- 155 oC by the reaction: 2Mg(AlH4)2 2MgAlH5+ 2Al+ 3H2 [243]. In summary, a partial reaction of the components is found to be occurred and a M-Al-H system is formed.

High pressure XRD patterns of Mg(AlH4)2 with LiCl (marked*) impurities are shown in Figure 11.8. The micro XRD experiments were conducted with X-rays of wavelength ~0.4151 Å. At ambient conditions Mg(AlH4)2 is of trigonal- P¯3m1 structure.   At 0.68 GPa it transform to a monoclinic- C2/m structure. It agrees with theoretical calculations of  Hu et al. [77].  Above 10.28 GPa transition to an orthorhombic- Pbca structure is expected but was not observed in this study up to 13 GPa.

Figure 11. 8: XRD patterns of Mg(AlH4)2 containing LiCl (marked *) at some selected pressures.

### 11.2.2.2. Raman spectroscopy

The mixture of 2AlH3+ MgH2 was heated at ~110 oC and  0.1 MPa for 12 hrs. After heating AlH3 was decomposed to Al and H2. The mixture was then cooled to room temperature and compressed in steps of pressure. A new peak was emerged in the Raman spectra at 3.5 GPa which is marked with arrow in Figure 11.9. This resembles the Al-H bending mode at 766 and 821 cm-1  of Mg(AlH4)2 and hence the reaction of Al with MgH2 or H2 can be expected.

Figure 11. 9: Raman spectra of the 2AlH3+ MgH2 mixture collected at various pressures in comparison with the Raman spectra of Mg(AlH4)2 .

The pressure was gradually increased up to 10 GPa. The new peak was disappeared at 10 GPa and was reappeared on decompression below 4 GPa. Which implies that the new peak is not due to MgH2 as the orthorhombic phase is stable on decompression confirming a possible reaction of Al with MgH2 or H2. While, in the XRD pattern at 10 GPa, the new peaks were not disappeared and was stable on decompression. Therefore, it may be expected that the disappearence of peaks in the Raman spectra above 10 GPa can be due to freezing of vibrations other than amorphization or decomposition. Figure 11.10 shows Raman spectra of pure Mg(AlH4)2 at various pressures.

Figure 11. 10: Raman spectra of Mg(AlH4)2 collected at various pressures. Spectrum marked * is of the decompressed sample and ‘ah’ abbreviates after heating.

In the high pressure study of pure Mg(AlH4)2, small amount of H2 was released above 0.35 GPa. This may be caused by the reaction of Mg(AlH4)2 with moisture on the gasket hole surface. When pressure was increased above 5 GPa, the strong Al- H stretching mode ~1800 cm-1 disappeared and this transition was irreversible.  Raman spectroscopic studies of LiAlH4 and NaAlH4 also show disappearance of Al-H stretching modes at high pressures. To check effect of stress field, the sample cell was heated at 150 oC for about 6 hrs at 5 GPa (spectrum marked ah in Figure 11. 10) and found no change.

## 11.3. Mixtures of Si and MgH2

### 11.3.1. Introduction

MgH2 contains 7.7 wt % of hydrogen and the decomposition temperature is above 325 °C. Thermodynamic properties of MgH2 were computed up to 1273 ºC which indicates an enhanced hydrogen storage property for this material at high temperatures [238]. The slow diffusion and kinetics prevent usage of MgH2 as an efficient candidate for hydrogen storage. Hence it is important to identify the best additive for destabilizing this light metal hydride. MgH2 can be synthesized by low cost means; however its enthalpy of formation is much higher, around -76 kJ/mol [61]. Equilibrium pressure of MgH2 at 275  ºC is about  0.1 MPa and for a mixture of MgH2 and Si it is about10 MPa at 150 ºC [50, 237]. This result indicates that the MgH2/Si system, which has a hydrogen capacity of 5 wt %, could be applicable for hydrogen storage at reduced temperatures. The MgH2/ Si system was found to be not readily reversible and the hydrogenation of the Mg2Si appears to be kinetically limited.

If a compound is stable with respect to its constituent elements, then the hydride will be effectively destabilized. This occurs because the system can be cycled between the hydride and the compound instead of the elemental metals and H2. For pure MgH2, hydrogen desorption begins at approximately 295 °C, and an equilibrium pressure of 0.17 MPa was attained at 300 °C [50]. After milling the mixture of MgH2 and Si and thermal dehydrogenation up to 400 °C, Mg2Si was the predominant phase, with a small amount of residual Si [50]. The reaction can be represented as: 2MgH2+ Si Mg2Si+ 2H2. The standard enthalpy of formation of Mg2Si is -77.8 kJ/ mol [50]. Therefore, formation of Mg2Si reduces the standard enthalpy of dehydrogenation, which is ~75.3 kJ/mol for pure MgH2 to 36.4 kJ/ mol for MgH2+ 1/2Si. High temperature studies of Mg2Si up to 700 °C show it is stable in that temperature ranges [244]. The present study aim to synthesize a compound by the reaction: 3MgH2+ Si MgSiH6+ 2Mg.

### 11.3.2. Results and discussion

The high pressure experiments at room temperature on the mixture of Si and MgH2 showed only phase transitions of MgH2.  Figure 11.11 shows XRD patterns of the mixture and the components Si and MgH2 collected at using X-rays of λ = 0.71073 Å. When the sample mixture was heated at 3.8 GPa and 600 oC formation Mg and H2 implying the decomposition of MgH2 without reacting to Si. In another experiment, the mixture of MgH2 and Si was heated at 0.5 GPa and 600 oC with a fresh loading using a zirconia anvil cell. After cooling down the cell, Raman spectra shows formation of Mg2Si alloy. Further studies has to be conducted to estimate the H2 pressure required to rehydrogenate Mg2Si. The observed reaction is: 3MgH2+ Si Mg2Si+ MgH2+ 2H2.

(a)                                                       (b)

Figure 11. 11: (a) The XRD pattern of the mixture of Si and MgH2 in comparison to that of pure components. (b) Raman spectra of MgH2+ Si mixture before and after heating at 0.5 GPa and 600 oC and that of pure Mg2Si; bh and ah abbreviates before and after heating, respectively.

# CHAPTER 12. COMPARISON OF PROPERTIES OF HYDRIDES

## 12.1. Properties of Metals and Hydrides: A Comparison

Estimation of different thermodynamic properties is required to determine the stability of a hydride for suitable technological applications. In general, hydride formation is accompanied by a structural phase transformation of the metal which has effect on their properties. Therefore, it is important to correlate properties of both metal and metal hydride to understand how the hydrogen influences the material properties. Table 12.1 shows approximate value of molar volume of hydrogen atom in the boron hydrides. The molar volume of boron hydrides are calculated from their unit cell volume. The molar volume of B metal is ~4.5 cm3/mol.  The difference of the molar volumes of the boron hydride and boron atoms gives an approximate value of the volume occupied by the hydrogen atoms. Average increase in molar volume per H- atom in the boron hydrides   is found to be ~6 cm3/mol. The values of thermodynamic properties of metal may increase or decrease when it form a hydride. Table 12.2 summarizes structure and entropy change due to hydride formation of some metal hydrides. Decrease or increase of entropy may be a combined effect of structural transformation and charge transfer between the metal and H- atom.

Table 12. 1: Approximate values of molar volumes of hydrogen atoms in boron hydrides.

| Hydride BxHy [245] | Vmol (cm3/mol) | ∑ Vmol B (cm3/mol) | ΔVmol of H in BxHy |
| --- | --- | --- | --- |
| B10H14 | 123.41 | 45.6 | 5.56 |
| B10H16 | 145.83 | 45.6 | 6.26 |
| B12H16 | 158.47 | 54.7 | 6.48 |
| B13H19 | 176.08 | 59.3 | 6.15 |
| B14H20 | 176.54 | 63.9 | 5.63 |
| B16H20 | 197.91 | 73 | 6.24 |
| B18H22 | 215.21 | 82.1 | 6.05 |
| B18H23 | 213.41 | 82.1 | 5.71 |
| B20H26 | 246.52 | 91.2 | 5.97 |
| B2H6 | 46.65 | 9.13 | 6.25 |
| BH3 | 23.6 | 4.5 | 6.37 |
| B4H10 | 73.60 | 18.3 | 5.53 |
| B5H11 | 87.44 | 22.8 | 5.87 |
| B5H9 | 78.26 | 22.8 | 6.16 |
| B6H10 | 88.50 | 27.4 | 6.11 |
| B8H12 | 110.99 | 36.5 | 6.21 |

Table 12. 2: Variation of the entropy of hydrogen in some binary metal hydrides (MHx).

| MHx | MHx structure | M structure | ΔS |
| --- | --- | --- | --- |
| PrH2 | fcc- Fm‾3m | hcp- P63/mmc | -8.58 |
| NdH2 | fcc - Fm‾3m | hcp- P63/mmc | -6.09 |
| LaH2 | fcc - Fm‾3m | hcp- P63/mmc | -2.61 |
| ZrH2 | fcc - Fm‾3m | hcp - P63/mmc | -1.92 |
| YH2 | fcc - Fm‾3m | hcp - P63/mmc | -3.03 |
| TiH2 | fcc - Fm‾3m | hcp - P63/mmc | -0.52 |
| LiH | fcc - Fm‾3m | bcc – Im3m | -9.05 |
| CsH | fcc - Fm‾3m | bcc – Im3m | 0.24 |
| RbH | fcc - Fm‾3m | bcc – Im3m | 8.62 |
| KH | fcc - Fm‾3m | bcc – Im3m | -14.46 |
| NaH | fcc - Fm‾3m | bcc – Im3m | -11.44 |

A detailed hydride research database is required for proper retrieval of information already available. In this study, data of various properties of more than 950 hydrides were collected from previous publications and public databases. The dataset thus generated is an efficient tool to disseminate the material properties for hydrogen storage technology. The aim of this work is to design new, better hydrides by combining or interpreting the already available data. The hydride database has enabled the study of inter-relationships of hydride material properties such as entropy, molar volume, density, unit cell volume etc., with those of corresponding metals or metal alloys. Figures 12.1-12.6 show comparative study of various properties of hydrides and the constituent metals.

Alkali metal hydrides have less molar volume than the corresponding metals. The entropy-molar volume relationship (Figure 12.3) of hydrides is found to be different from that of host metals. Analyzing the Figure 12.3, entropy of a hydride can be related to its molar volume by the simple formula SMH = -3.074+ 2.153VMH. Molar volume of a hydride can be represented as VMH = VM+ VH+ Δ, where VM is the molar volume of metal/alloy, VH is the molar volume of hydrogen as a metal (~1.7 cm3/mol), Δ is molar volume due to charge transfer between metal and hydrogen atoms. There may be an influence of crystal structure on the value of Δ and hence molar volume of hydride [246]. Larger the difference between electro-negativities of metal and hydrogen, greater will be the charge transfer effects and hence the change in molar volume. The density of the alkali metal hydride is higher than the corresponding metals may be caused by the crystal structure difference. The alkali- hydrides have fcc (face centered cubic) metal lattice with a packing density of 0.74 compared to 0.68 for corresponding bcc (body centered cubic) metal lattice.

Figure 12. 1: Comparison of molar volume of binary hydrides and corresponding metal.

Figure 12. 2: Molar volume of Li containing hydrides versus the element sum  [70, 71, 73, 83, 170, 247-249].

Figure 12. 3: A comparison of entropy versus molar volume of metals and metal hydrides. Subscript M denotes metal and MH denotes metal hydride.

In summary, the increase or decrease of entropy, density and volume can be a combined effect of structural transformation and charge transfer between metal and H-atom during the hydride formation. From Figure 12.5 it is obvious that hydrogenating a metal results in large increase of its specific heat which may be due to hydrogen induced optical vibration [250]. The hydrides which contain elements of same group or period also show some similarity in their properties.  Plot of molar volume of various alkali metal hydrides versus the sum of that of host metals is shown in Figure 12.6. This plot suggests that there may be an interrelationship between crystal chemistry and hydrogen induced properties. Hydrides having similar symmetry should show interrelationship among their properties which may vary from those of different symmetry.

Figure 12. 4: Plots of entropy of binary metal hydrides versus that of corresponding metals.

Figure 12. 5: Plot of specific heat of various binary metal hydrides versus that of the host metal. The dotted line corresponds to the specific heat of metals.

Figure 12. 6: A comparison of molar volumes (cm3/mol) of various alkali hydrides with that of the corresponding host metals.

## 12.2. Inter-relationships of Thermodynamic Properties of Hydrides

Purpose of this study is to explore the thermodynamic properties of metal hydrides which have no established relationships. This type of studies can give insight into the influence of atomic or structural properties on the thermodynamics of the hydrides. Figures 12.7- 12.11 show the interrelation of entropy (taken from FactSage database), hydrogen content, specific heat, enthalpy and bulk modulus to molar volume of metal hydrides. The enthalpy of alkali hydrides is found to be increasing with atomic number, where as it is decreasing in the case of alkali earth metal hydrides.  This can be due to large number of H-H bonds in the alkali- earth metal hydrides or because of the partially ionic nature of M-H bonds. The entropy is found to be increasing in both cases with increase in atomic number while CsH and BeH2 show some deviation. This may be attributed to covalent nature of BeH2 while others are ionic. The large size of Cs and the orintational freedom of hydrogen atoms may be causing a partially ionic bonding of CsH. This in turn can result in the deviation of properties of CsH from that of similar hydrides.

Figure 12. 7: Variation of entropy with molar volume of various hydrides [62, 249-253].

Figure 12. 8: The variation of hydrogen content versus molar volume for the rare-earth metal hydrides.

Figure 12. 9: The variation of specific heat versus molar volume for binary metal hydrides [70, 71, 73, 83, 170].

From the plot of variation of bulk modulus with molar volume (Figure 12. 11) of metal hydrides, it can be observed that heavy alkali hydrides are more compressible than the alkaline earth metal hydrides. The high compressibility of heavy alkali metal hydrides suggests that tuning of electron density is possible in these compounds under pressure. Therefore, chemical reaction with additives should be investigated for these hydrides as a step towards their destabilization. There is some disparity in the data of BaH2 as it has a lower value of bulk modulus (experimental: 24 GPa, calculated: 31 GPa) as compared to similar hydrides. This deviation from behavior of other alkali- earth metal hydrides implies that the high pressure study of BaH2 has to be redone to confirm the accuracy of the data.

Figure 12. 10: Plot of enthalpy versus molar volume of alkali and alkali- earth metal hydrides.

Figure 12. 11: Plot of bulk modulus versus molar volume of alkali and alkali- earth metal hydrides.

Figure 12.12 shows plot of decomposition temperature versus density of alkali and alkali- earth metal hydrides.  High density alkali hydrides decompose at lower temperatures than the low density compounds. The alkali- earth metal hydrides show opposite behavior. This may be caused by the difference in hydrogen bonding in those hydrides.

Figure 12. 12: Plot of decomposition temperature versus density of alkali and alkali- earth metal hydrides.

Alanates are less stable than corresponding borohydrides because the Al-H bonds are weaker than the B-H bonds. The decomposition temperature rises as size of the metal increases from Li to Cs for alkali borohydrides (Figure 12.13). Plot of bulk modulus versus molar volume of alkali and alkali- earth complex hydrides (Figure 12.14) show some similarity between light borohydrides and heavy alanates and vice versa. The bulk modulus values indicate that complex hydrides are more compressible than metals and metal hydrides. Therefore, it will be interesting to study their destabilization by additives/catalysts. This is possible by tuning the electron density of these complex hydrides under pressure.

Figure 12. 13: Plot of decomposition temperature versus density of alkali and alkali- earth complex hydrides.

Figure 12. 14: Plot of bulk modulus versus molar volume of alkali and alkali- earth complex hydrides.

## 12.3. Structural Properties of Complex Metal Hydrides

The high pressure structural behavior of alkali and alkali- earth metal borohydrides is widely investigated. High pressure phase transitions of alkali metal borohydrides are found to be first-order and fully reversible whereas that of alkali- earth complex hydrides are irreversible. Due to strong covalent and ionic bonding nature, dissociation temperatures of borohydrides are very high. The improvement of the hydride properties by catalytic addition requires better understanding of the crystal structure and stability of the phases. The ambient phase of LiBH4 which has an orthorhombic- Pnma structure transforms initially into a tetragonal- Ama2 at 1.2 GPa and then to a cubic- Fm‾3 m phase at 10 GPa [79, 152].  The cubic phase of NaBH4 transforms into a tetragonal- P‾421c structure above 6 GPa and then to an orthorhombic- Pnma phase above 8 GPa [84]. KBH4 exhibits structural transitions from a cubic- Fm‾3m to a tetragonal- P‾421c phase at 3.8 GPa and then to an orthorhombic- Pnma phase at 6.8 GPa [87].

The study of structural stability of RbBH4 at room temperature shows a transition from the ambient cubic- Fm‾3m phase to an orthorhombic- Pnma phase around 2.5 GPa, and then to a monoclinic- P21/c phase above 8 GPa [90]. The reduction in the cubic to tetragonal transition pressure and the absence of a tetragonal high-pressure phase in RbBH4 suggest that the transition pressure is influenced by the size of the alkali atom during the structural rearrangement of BH4‾ anions and alkali cations. A comparison of the transition pressure among first group metal borohydrides shows that the increase in the size of the alkali cation leads to a decrease in the transition pressure. A lower bulk modulus and a large volume collapse during the first transition imply that both the Rb–H bonds and the BH4‾ units are more compressible and rearranged than that of NaBH4. This may favor a direct transition from the cubic phase to the orthorhombic phase without an intermediate structure. Raman spectra as a function of temperature measured for these cubic borohydrides by Hageman et al. [254], also suggest a similar scenario where the energy barrier of the reorientation of the BH4‾ anions decreases as a function of cation size. Like Na, K, and Rb borohydride counterparts, CsBH4  also crystallizes in Fm‾3m structure at room temperature with a disordered BH4‾ complex [89]. Low temperature order-disorder phase transitions are observed in the alkali borohydrides, which ranges from -83 ◦C for NaBH4 to -246 ◦C for CsBH4 [88]. Compared to other alkali metal borohydrides, CsBH4 has a higher symmetry structure [91]. High temperature Raman spectroscopic studies of alkali borohydrides show BH4‾ ions are easily reoriented in CsBH4 [254].

Among alkali- earth metal borohydrides, Be(BH4)2 is found to be of tetragonal- I41cd structure with a covalent bonding.The estimated decomposition temperature of Be(BH4)2 is -111 ◦C, even though the compound is found to be stable at room temperature [36, 92]. The crystal structure and the electronic density of states suggest formation of [−BH4−Be−]n  helical polymers. In general BH4‾ units in borohydrides have a tetragonal co-ordination, whereas in Be(BH4)2 it has a trigonal co-ordination [99]. Dehydrogenation of Be(BH4)2 to elements is more favorable than that to BeH2 unlike other complex hydrides. Ca(BH4)2 has an orthorhombic- F2dd and Mg(BH4)2 has a complex hexagonal structure with space group P6122 and both of them exhibits polymorphism [94, 97, 160]. Therefore it is interesting to study structural behavior of metal borohydrides under various conditions of pressures and temperatures. Above 2.5 GPa magnesium borohydride transform to a high pressure phase with P63 structure which is metastable at ambient conditions. Raman spectroscopic studies show another structural transition of Mg(BH4)2 above 14 GPa to an unidentified phase. At 180 ◦C an irreversible transition of Mg(BH4)2  which occurs from P6122 to an orthorhombic- Fddd phase. The Fddd phase of Ca(BH4)2 transforms  to a F2dd structure at -182 ◦C. At high temperatures, three tetragonal phases of Ca(BH4)2 are found which are P‾4 (~32 ◦C), P‾4/2m (207 ◦C) and I‾42d (222 ◦C). The P‾42/m phase is stable at ambient conditions and formed as a result of synthesizing and processing conditions. Mechano- chemical synthesize of Ca(BH4)2 show formation of a small amount of Pbca with the Fddd phase [98].

Except LiAlH4 (monoclinic) and NaAlH4 (tetragonal), alkali alanates are of orthorhombic symmetry. Around 3 GPa the ambient monoclinic- P21/c phase of LiAlH4 transform to a high pressure phase with a distorted AlH4- tetrahedron [69, 70]. NaAlH4 undergoes a phase transformation from a tetragonal- I41/a to an orthorhombic- Cmc21 structure at 6.43 GPa with 45 % volume contraction [71]. Experimental study of Kumar et al. [73], reports a tetragonal to monoclinic of NaAlH4 phase transition above 14 GPa. First principle density functional theory studies show that RbAlH4 and CsAlH4 exist in orthorhombic- Pnma structure at room temperature [26]. Computation of crystallographic data suggest that at ambient conditions, Mg(AlH4)2 has a trigonal- P‾3m1 structure which transform to a monoclinic- C2/m structure around 0.68 GPa. Above 10.28 GPa, transition to an orthorhombic- Pbca structure is expected [77]. The decomposition of Mg(AlH4)2 occurs in three steps, first in the range 110- 200 ºC, and second and third around 240- 380 and 400 ºC, respectively [31]. Density functional theory calculations predict that Ca(AlH4)2 is a insulator with orthorhombic- Pbca structure [33].

The bulk modulus of several borohydrides and alanates has been determined by high pressure studies.  Among that, LiBH4 has bulk modulus values in the range 14.4– 26 GPa for three different phases [79]. For  KBH4,  the K0 is found to be 16.8 GPa [87], whereas  for RbBH4 it is 14.5 GPa [90]. The orthorhombic phase of Ca(BH4)2 and the high pressure phase of Mg(BH4)2 have bulk moduli of 22.9 and 10.16 GPa, respectively [94, 97]. Alanates of alkali and alkali- earth metals also has experimental and computed values of bulk modulus in the range 8- 35 GPa [69-71, 73, 75-78]. Among alkali-earth compounds, studies of Sr and Ba based complex hydrides are lacking. It is interesting to note that all these borohydrides and alanates have bulk modulus in the same range and they are highly compressible. Figure 12.15 shows the change in molar volume under applied pressure for various complex hydrides. Results show that the borohydrides and alanates are highly compressible solids and hence they may be destabilized under pressure with additives/catalysts to enhance the hydrogenation kinetics. The reordering of Al-H and B-H bonds in the complex hydrides is responsible for the observed phase transitions in them.

Figure 12. 15: A comparison of the change of molar volume with pressure for the complex hydrides investigated in this study.

# CHAPTER 13. SUMMARY

Important results derived from this dissertation are concluded below. These include inferences from the high pressure and temperature investigations of Mg2FeH6, Mg(BH4)2, Ca(BH4)2, NaBH4, NaAlH4, LiAlH4 , LiNH2BH3 and mixture of MgH2 with AlH3 or Si. Interesting features derived from the study of inter- relationships of various properties of hydrides are also summarized.

## 13.1. Conclusions

High pressure phase transitions and physical properties of the selected complex hydrides were investigated with X-ray diffraction and Raman spectroscopy studies. The observed phase transitions and structural data are summarized in the Table 13.1.  High pressure phase transitions of alkali metal complex hydrides are found to be first order and fully reversible whereas that of the alkali-earth metal complex hydrides are irreversible. A P-T phase diagram of NaBH4 was also constructed which confirms all the transitions observed for this compound were first order and exothermic. Mg2FeH6 did not show any phase transition up to the highest pressure reached which indicate high stability of Fe-H bonds. Transition pressure is influenced by the size of alkali atom and the rearrangement of anions and cations. A comparison of the bulk modulus values indicates that complex hydrides are more compressible than their metals and metal hydrides. The reordering of the highly compressible Al-H and B-H bonds in alanates and borohydrides, respectively are responsible for the observed phase transitions in these compounds. With high capacity and favorable thermodynamics, Mg(BH4)2 and Ca(BH4)2 are suitable for reversible hydrogen storage.

Large thermal expansion observed for the hydrides can be due to the hydrogen induced optical vibration. Bulk modulus values of ball milled sample were found to be higher than that of the unmilled sample. This can be attributed to the particle size reduction and related stress effect due to milling. It is also noted that the alanates and borohydrides have bulk modulus in the same range and they are highly compressible. The high compressibility of the complex metal hydrides suggests that tuning of electron density is possible in these compounds under pressure. Therefore, alanates and borohydrides can be destabilized with additives/catalysts under pressure to enhance the hydrogenation kinetics. On a comparison with the literature data, the decomposition temperature and bulk modulus of alkali metal complex hydrides are found to be increasing with the size of the metal atom due to stronger covalent and ionic bonding in them. The transition pressure is found to be independent of size of metal atoms in complex hydrides unlike the metal hydrides. Bulk modulus of alkali and alkali earth hydrides are higher than that of corresponding metals, suggesting a hydrogen induced hardening of these materials. B-H bond energy is larger than the Al-H bond energy and hence the bulk modulus of borohydrides is higher than that of their alanate counterparts. An unidentified new phase was formed in the high pressure- temperature study of the mixture of AlH3 and MgH2. Investigation of LiNH2BH3 with high pressure Raman spectroscopy show phase transitions approximately at 5, 10 and 15 GPa. MgH2 was destabilized by Si and formed Mg2Si at 0.5 GPa and 600 ºC.

Table 13.1. Summary of the results obtained from the high pressure and/or temperature investigations of the complex hydrides. Data marked * are of ball milled sample.

| Hydride | P (GPa) | Structure/ Space group | Ko (GPa) | K'o | V0/f.u (Å3) | α (10-5K-1) |
| --- | --- | --- | --- | --- | --- | --- |
| LiAlH4 | 0- 2.16 >3 | Monoclinic/ P21/c Tetragonal/ I41/a | 13.87 | 4 | 75.15 |  |
| NaAlH4 | 0- 6 >6.3 | Tetragonal/ I41/a Orthorhombic/Cmc21 | 25.3, 52.2* | 4 | 72.08 |  |
| NaBH4 | 0- 6.3 6.3- 8.9 8.9- 14 >14 | Cubic/ Fm‾3m Tetragonal/ P‾421c Orthorhombic/ Pnma Monoclinic/ P21/c | 18.76 | 3.5 | 57.95 | 12.06 |
| Mg(BH4)2 | 0- 2.5 2.5- 14 >14 | Hexagonal/ P6122 Hexagonal/ P63 Unidentified | 10.16 | 4 | 94.53 |  |
| Ca(BH4)2 | > 0 0- 10.2 | Orthorhombic/ F2dd Tetragonal/ P42/m | 22.95 | 2.6 | 108.26 |  |
| Mg2FeH6 | 0- 36 | Cubic/ Fm‾3m | 75.4, 139* | 4 | 66.95 | 5.85 |

Entropy, molar volume, specific heat and hydrogen content of both binary and ternary metal hydrides were analyzed with principal component analysis method. The comparison of properties between metals and their corresponding hydrides gives insight into a combined effect of charge transfer between metal and H-atom, and structural transformation. The specific heat of binary hydrides is higher than that of the corresponding metals, whereas the molar volume and entropy of certain hydrides were less than that of corresponding metals which suggests an interrelationship between crystal chemistry and hydrogen induced properties. The average value of molar volume of H- atom in the boron hydrides was determined to be ~6 cm3/mol. The thermodynamic properties of various metal hydrides were correlated and found many interesting features. The entropy- molar volume relationship of hydrides is found to be different from that of the host metals. Entropy of a hydride can be related to the molar volume of the metal by the equation: SMH = -3.074+ 2.153 (VM+ VH+ Δ). Larger the difference between electro- negativities of metal and hydrogen, greater will be the charge transfer effects (Δ) and hence the change of entropy of the hydride.

## 13.2. Recommendations for Future Research

  - The hydrides investigated are promising hydrogen storage materials. Further studies are required to understand the mechanism to overcome kinetic barriers of dehydrogenation of the complex hydrides. The additives should be selected such that it weakens the B-H and Al-H bonds in the borohydrides and alanates, respectively. Improved hydrogenation properties are expected for the complex hydrides owing to their high compressibility which should be investigated under pressure.  The decomposition temperature of the high pressure phases of the hydrides which are metastable at ambient conditions has to be determined to confirm whether they are usable.

  - Some of the complex hydrides like LiAlH4 exhibit high ionic conductivity and hence potential for their application as a solid electrolyte should be investigated.

- Further studies of Mg(AlH4)2 has to be carried out to determine the structure of the high pressure phase which was observed above 0.68 GPa. The influence of synthesis and processing conditions on the crystal structure of Mg(AlH4)2 is interesting as the borohydride counterpart show irreversible phase transitions under pressure and temperature.

- The new phase formed in the high P-T study of the mixture of AlH3 and MgH2 has to be identified using high quality data such as neutron diffraction.

- The XRD patterns of the mixture of Si and LiAlH4 after heating to 500 ºC show formation of a new phase above 11.2 GPa. Hence it will be interesting to study the structure and thermodynamic stability of this mixture.

- A mixture of Si and H2O was studied under high temperature using a moissanite anvil cell up to 600 oC. The sample at 1.5 GPa was heated with a gas blower. A reaction between Si and H2O might have occurred as can be concluded from the appearance of a new peak in the Raman spectroscopy experiment. The unidentified phase should be further investigated with large amount of sample to get good quality X-ray diffraction patterns for further analysis.

- LiNH2BH3 was investigated with high pressure Raman spectroscopy and found phase transitions approximately at 5, 10 and 15 GPa. Phase identification of LiNH2BH3 has to be carried out with high quality X-ray diffraction or neutron diffraction.

- MgH2 was destabilized by Si and formed Mg2Si at 0.5 GPa and 600 ºC. Hydrogenation of Mg2Si under high H2 pressure and temperature will need to identify potential of this mixture.

- The high pressure structural data of alkali-earth alanates and borohydrides are scarce owing to their high reactivity and difficulty to synthesize. Alanates and borohydrides of Sr and Ba have to be investigated under pressure and temperature to draw a general conclusion from their structural properties.

# LIST OF REFERENCES

[1] 	F.Waelbroeck, P.Wienhold, J.Winter, Journal of Nuclear Materials 2011, 111-112, 185.

[2] 	J.Kleperis, G.Wojcik, A.Czerwinski, J.Skowronski, M.Kopczyk, B.M.Beltowska, Journal of Solid State Electrochemistry 2001, 5, 229.

[3] 	V.E.Antonov, Journal of Alloys and Compounds 2002, 330-332, 110.

[4] 	B.Baranowski, S.Filipek, Journal of the Less Common Metals 1982, 88, 290.

[5] 	B.Baranowski, Journal of the Less Common Metals 1984, 101, 115.

[6] 	T.Palasyuk, M.Tkacz, P.Vajda, Solid State Communications 2005, 135, 226.

[7] 	M.Tkacz, The Journal of Chemical Thermodynamics 2001, 33, 891.

[8] 	M.Tkacz, R.Burtovyy, Solid State Communications 2004, 132, 37.

[9] 	W.Grochala, P.P.Edwards, Chemical Reviews 2004, 104, 1283.

[10] 	H.Smithson, C.A.Marianetti, D.Morgan, A.Van der Ven, A.Predith, G.Ceder, Physical Review B 2002, 66, 144107.

[11] 	C.Y.Xiao, J.L.Yang, K.M.Deng, Z.H.Bian, K.L.Wang, Journal of Physics: Condensed Matter 1994, 6, 8539.

[12] 	T.Noritake, M.Aoki, S.Towata, Y.Seno, Y.Hirose, E.Nishibori, M.Takata, M.Sakata, Applied Physics Letters 2002, 81, 2008.

[13] 	R.Yu, P.K.Lam, Physical Review B 1988, 37, 8730.

[14] 	P.Vajeeston, P.Ravindran, A.Kjekshus, H.Fjellvag, Applied Physics Letters 2004, 84, 34.

[15] 	"New World Encyclopedia", 2008.

[16] 	L.George, R.Hrubiak, K.Rajan, S.K.Saxena, Journal of Alloys and Compounds 2009, 478, 731.

[17] 	R.Gupta, F.Agresti, S.Lo Russo, A.Maddalena, P.Palade, G.Principi, Journal of Alloys and Compounds 2008, 450, 310.

[18] 	J.Huot, I.Swainson, R.Schulz, Annales de Chimie-Science des Materiaux 2006, 31, 135.

[19] 	S.A.Jin, Y.S.Lee, J.H.Shim, Y.W.Cho, Journal of Physical Chemistry C 2008, 112, 9520.

[20] 	X.Kang, P.Wang, H.Cheng, Rare Metals 2006, 25, 266.

[21] 	O.M.Lovvik, Journal of Alloys and Compounds 2004, 373, 28.

[22] 	M.Yoshino, K.Komiya, Y.Takahashi, Y.Shinzato, H.Yukawa, M.Morinaga, Journal of Alloys and Compounds 2005, 404-406, 185.

[23] 	Z.F.Hou, Journal of Power Sources 2006, 159, 111.

[24] 	V.P.Balema, K.W.Dennis, V.K.Pecharsky, Chemical Communications, 1665.

[25] 	M.Matsuo, A.Remhof, P.Martelli, R.Caputo, M.Ernst, Y.Miura, T.Sato, H.Oguchi, H.Maekawa, H.Takamura, A.Borgschulte, A.Zuttel, S.i.Orimo, Journal of the American Chemical Society 2009, 131, 16389.

[26] 	P.Vajeeston, P.Ravindran, R.Vidya, H.Fjellvag, A.Kjekshus, Crystal Growth & Design 2004, 4, 471.

[27] 	B.Bogdanovic, M.Schwickardi, Journal of Alloys and Compounds 1997, 253-254, 1.

[28] 	B.Bogdanovic, R.A.Brand, A.Marjanovic, M.Schwickardi, J.Tolle, Journal of Alloys and Compounds 2000, 302, 36.

[29] 	F.Schuth, B.Bogdanovic, M.Felderhoff, Chemical Communications 2004, 2249.

[30] 	H.Morioka, K.Kakizaki, S.C.Chung, A.Yamada, Journal of Alloys and Compounds 2003, 353, 310.

[31] 	M.Fichtner, O.Fuhr, O.Kircher, Journal of Alloys and Compounds 2003, 356-357, 418.

[32] 	A.Fossdal, H.W.Brinks, M.Fichtner, B.C.Hauback, Journal of Alloys and Compounds 2005, 387, 47.

[33] 	O.M.Lovvik, Physical Review B 2005, 71, 1144111.

[34] 	L.Mosegaard, B.Moller, J.E.Jorgensen, U.Bosenberg, M.Dornheim, J.C.Hanson, Y.Cerenius, G.Walker, H.J.Jakobsen, F.Besenbacher, T.R.Jensen, Journal of Alloys and Compounds 2007, 446-447, 301.

[35] 	A.G.Ostroff, R.T.Sanderson, Journal of Inorganic and Nuclear Chemistry 1957, 4, 230.

[36] 	M.J.van Setten, G.A.de Wijs, G.Brocks, Physical Review B 2008, 77, 165115.

[37] 	J.Voss, J.S.Hummelshoj, Z.Lodziana, T.Vegge, Journal of Physics: Condensed Matter 2009, 21, 012203.

[38] 	T.Matsunaga, F.Buchter, P.Mauron, M.Bielman, Y.Nakamori, S.Orimo, N.Ohba, K.Miwa, S.Towata, A.Znttel, Journal of Alloys and Compounds 2008, 459, 583.

[39] 	J.H.Kim, S.A.Jin, J.H.Shim, Y.W.Cho, Journal of Alloys and Compounds 2008, 461, L20-L22.

[40] 	L.Liu, W.A.Bassett, Elements, oxides, Silicates: High pressure phases with  implications for the earth's interior, Oxford University Press, USA, 1986.

[41] 	R.Ahuja, O.Eriksson, B.Johansson, Physica B 1999, 265, 87.

[42] 	F.D.Murnaghan, Proceedings of the National Academy of Sciences of the United States of America 1944, 30, 244.

[43] 	F.Birch, Journal of Geophysical research 1978, 83, 1257.

[44] 	F.Birch, Physical Review 1947, 71, 809.

[45] 	Y.Filinchuk, D.Chernyshov, R.Cerny, The Journal of Physical Chemistry C 2008, 112, 10579.

[46] 	R.Ahuja, O.Eriksson, J.M.Wills, B.Johansson, Journal of Physics: Condensed Matter 1998, 10, L153-L158.

[47] 	S.Filipek, Journal of Advanced Science 2007, 19, 1.

[48] 	S.J.Duclos, Y.K.Vohra, A.L.Ruoff, S.Filipek, B.Baranowski, Physical Review B 1987, 36, 7664.

[49] 	I.O.Bashkin, T.N.Dymova, E.G.Ponyatovskii, Physica Status Solidi B 2006, 100, 87.

[50] 	J.J.Vajo, F.Mertens, C.C.Ahn, C.Robert, B.Fultz, The Journal of Physical Chemistry B 2004, 108, 13977.

[51] 	D.R.Stephens, E.M.Lilley, J. Appl. Phys. 1968, 39, 177.

[52] 	B.Olinger, P.M.Halleck, Applied Physics Letters 1974, 24, 536.

[53] 	G.Li, D.Wang, Q.Jin, D.Ding, Physics Letters A 1990, 143, 473.

[54] 	J.Sangster, A.Pelton, Journal of Phase Equilibria 1997, 18, 387.

[55] 	J.Sangster, A.Pelton, Journal of Phase Equilibria 1994, 15, 87.

[56] 	J.Songster, A.Pelton, Journal of Phase Equilibria 1994, 15, 84.

[57] 	K.Ghandehari, H.Luo, A.L.Ruoff, S.S.Trail, F.J.Disalvo, Physical Review Letters 1995, 74, 2264.

[58] 	U.Hantsch, B.Winkler, V.Milman, Chemical Physics Letters 2003, 378, 343.

[59] 	M.Ahart, J.L.Yarger, K.M.Lantzky, S.Nakano, H.K.Mao, R.J.Hemley, Journal of Chemical Physics 2006, 124, 014502.

[60] 	P.Vajeeston, P.Ravindran, B.C.Hauback, H.Fjellvag, A.Kjekshus, S.Furuseth, M.Hanfland, Physical Review B 2006, 73, 224102.

[61] 	J.Hector, J.F.Herbst, W.Wolf, P.Saxe, G.Kresse, Physical Review B 2007, 76, 014121.

[62] 	J.S.Tse, D.D.Klug, S.Desgreniers, J.S.Smith, R.Flacau, Z.Liu, J.Hu, N.Chen, D.T.Jiang, Physical Review B 2007, 75, 134108.

[63] 	B.Li, Y.W.Li, K.F.Yang, Q.L.Cui, Y.M.Ma, G.T.Zou, Journal of Physics-Condensed Matter 2007, 19, 226205.

[64] 	Y.W.Li, B.Li, T.Cui, Y.Li, L.J.Zhang, Y.M.Ma, G.T.Zou, Journal of Physics-Condensed Matter 2008, 20, 045211.

[65] 	J.S.Smith, S.Desgreniers, D.D.Klug, J.S.Tse, Solid State Communications 2009, 149, 830.

[66] 	K.Kinoshita, M.Nishimura, Y.Akahama, H.Kawamura, Solid State Communications 2007, 141, 69.

[67] 	J.S.Smith, S.Desgreniers, J.S.Tse, D.D.Klug, Journal of Applied Physics 2007, 102, 043520.

[68] 	W.Luo, R.Ahuja, Journal of Alloys and Compounds 2007, 446, 405.

[69] 	R.S.Chellappa, D.Chandra, S.A.Gramsch, R.J.Hemley, J.F.Lin, Y.Song, Journal of Physical Chemistry B 2006, 110, 11088.

[70] 	A.V.Talyzin, B.Sundqvist, Physical Review B 2004, 70, 180101.

[71] 	P.Vajeeston, P.Ravindran, R.Vidya, H.Fjellvag, A.Kjekshus, Physical Review B 2003, 68, 212101.

[72] 	B.Bulychev, Russian Journal of Inorganic Chemistry 1977, 22, 2461.

[73] 	R.S.Kumar, E.Kim, O.Tschauner, A.L.Cornelius, M.P.Sulic, C.M.Jensen, Physical Review B 2007, 75, 174110.

[74] 	P.Vajeeston, P.Ravindran, R.Vidya, H.Fjellvag, A.Kjekshus, Applied Physics Letters 2003, 82, 2257.

[75] 	P.Vajeeston, P.Ravindran, A.Kjekshus, H.Fjellvag, Journal of Alloys and Compounds 2004, 363, L7-L11.

[76] 	P.Ravindran, P.Vajeeston, R.Vidya, H.Fjellvag, A.Kjekshus, Journal of Power Sources 2006, 159, 88.

[77] 	C.H.Hu, D.M.Chen, Y.M.Wang, D.S.Xu, K.Yang, Journal of Physics-Condensed Matter 2007, 19, 176205.

[78] 	P.Vajeeston, P.Ravindran, A.Kjekshus, H.Fjellvag, Applied Physics Letters 2006, 89, 071906.

[79] 	Y.Filinchuk, D.Chernyshov, A.Nevidomskyy, V.Dmitriev, Angewandte Chemie-International Edition 2008, 47, 529.

[80] 	A.V.Talyzin, O.Andersson, B.Sundqvist, A.Kurnosov, L.Dubrovinsky, Journal of Solid State Chemistry 2007, 180, 510.

[81] 	T.J.Frankcombe, G.J.Kroes, Physical Review B 2006, 73, 174302.

[82] 	M.R.Hartman, J.J.Rush, T.J.Udovic, J.Bowman, S.J.Hwang, Journal of Solid State Chemistry 2007, 180, 1298.

[83] 	J.P.Soulie, G.Renaudin, R.Cerny, K.Yvon, Journal of Alloys and Compounds 2002, 346, 200.

[84] 	E.Kim, R.Kumar, P.F.Weck, A.L.Cornelius, M.Nicol, S.C.Vogel, J.Z.Zhang, M.Hartl, A.C.Stowe, L.Daemen, Y.S.Zhao, Journal of Physical Chemistry B 2007, 111, 13873.

[85] 	R.S.Kumar, A.L.Cornelius, Applied Physics Letters 2005, 87, 261916.

[86] 	L.George, V.Drozd, H.Couvy, J.Chen, S.K.Saxena, The Journal of Chemical Physics 2009, 131, 074505.

[87] 	R.S.Kumar, E.Kim, A.L.Cornelius, Journal of Physical Chemistry C 2008, 112, 8452.

[88] 	C.C.Stephenson, D.W.Rice, W.H.Stockmayer, The Journal of Chemical Physics 1955, 23, 1960.

[89] 	G.Renaudin, S.Gomes, H.Hagemann, L.Keller, K.Yvon, Journal of Alloys and Compounds 2004, 375, 98.

[90] 	R.S.Kumar, A.L.Cornelius, Journal of Alloys and Compounds 2009, 476, 5.

[91] 	P.Vajeeston, P.Ravindran, A.Kjekshus, H.Fjellvag, Journal of Alloys and Compounds 2005, 387, 97.

[92] 	D.S.Marynick, W.N.Lipscomb, Inorganic Chemistry 2002, 11, 820.

[93] 	Y.Filinchuk, R.Cerny, H.Hagemann, Chemistry of Materials 2009, 21, 925.

[94] 	L.George, V.Drozd, S.K.Saxena, E.G.Bardaji, M.Fichtner, Journal of Physical Chemistry C 2009, 113, 486.

[95] 	J.H.Her, P.W.Stephens, Y.Gao, G.L.Soloveichik, J.Rijssenbeek, M.Andrus, J.C.Zhao, Acta Crystallographica Section B 2007, 63, 561.

[96] 	Y.Filinchuk, E.Ronnebro, D.Chandra, Acta Materialia 2009, 57, 732.

[97] 	L.George, V.Drozd, S.K.Saxena, E.G.Bardaji, M.Fichtner, The Journal of Physical Chemistry C 2009, 113, 15087.

[98] 	F.Buchter, Z.Lodziana, A.Rernhof, O.Friedrichs, A.Borgschulte, P.Mauron, A.Zuttel, D.Sheptyakov, G.Barkhordarian, R.Bormann, K.Chlopek, M.Fichtner, M.Sorby, M.Riktor, B.Hauback, S.Orimo, Journal of Physical Chemistry B 2008, 112, 8042.

[99] 	Y.Filinchuk, D.Chernyshov, V.Dmitriev, Zeitschrift fur Kristallographie 2008, 223, 649.

[100] 	T.Hayashi, K.Tobita, S.Nishio, K.Ikeda, Y.Nakamori, S.Orimo, Fusion Engineering and Design 2006, 81, 1285.

[101] 	"http://hydpark.ca.sandia.gov/DBFrame.html",  2010.

[102]    "http://www1.eere.energy.gov/hydrogenandfuelcells/storage.html”,  2010.

[103] 	W.A.Bassett, High Pressure Research: An International Journal 2009, 29, 163.

[104] 	H.K.Mao, J.Xu, P.M.Bell, Journal of Geophysical research 1986, 91, 4673.

[105] 	I.F.Silvera, A.D.Chijioke, W.J.Nellis, A.Soldatov, J.Tempere, Physica Status Solidi B 2007, 244, 460.

[106] 	N.M.Balzaretti, E.J.Gonzalez, G.J.Piermarini, T.P.Russell, Review of Scientific Instruments 1999, 70, 4316.

[107] 	"http://www.nsls.bnl.gov/beamlines/beamline.asp?blid=X17C", 2009.

[108] 	A.P.Hammersley, Internal Report ESRF97HA02T; EuropeanSynchrotron Radiation Facility, Grenoble, France 1997.

[109] 	A.C.Larson, R.B.Von Dreele, Los Alamos National Laboratory Report LAUR 2004, 86.

[110] 	"http://www.ccp14.ac.uk/solution/gsas/",  2010.

[111] 	"http://www.ncnr.nist.gov/xtal/software/gsas.html",  2010.

[112] 	"http://sbmp95.ess.sunysb.edu/sam85/Plot85/plot85_windows.htm",  2010.

[113] 	R.J.Angel, High-pressure, high-temperature crystal chemistry 2001, 41, 35.

[114] 	B.Toby, Journal of Applied Crystallography 2005, 38, 1040.

[115] 	W.Kraus, G.Nolze, Journal of Applied Crystallography 1996, 29, 301.

[116] 	"http://www.unipress.waw.pl/fityk/",  2010.

[117] 	"https://www.spss.com/statistics/",  2010.

[118] 	B.Bogdanovic, A.Reiser, K.Schlichte, B.Spliethoff, B.Tesche, Journal of Alloys and Compounds 2002, 345, 77.

[119] 	A.Reiser, B.Bogdanovic, K.Schlichte, International Journal of Hydrogen Energy 2000, 25, 425.

[120] 	F.C.Gennari, F.J.Castro, J.J.A.Gamboa, Journal of Alloys and Compounds 2002, 339, 261.

[121] 	M.Herrich, N.Ismail, A.Handstein, A.Pratt, O.Gutfleisch, Materials Science and Engineering B-Solid State Materials for Advanced Technology 2004, 108, 28.

[122] 	J.Huot, S.Boily, E.Akiba, R.Schulz, Journal of Alloys and Compounds 1998, 280, 306.

[123] 	S.L.Li, R.A.Varin, Transactions of Nonferrous Metals Society of China 2004, 14, 649.

[124] 	S.L.Li, R.A.Varin, O.Morozova, T.Khomenko, Journal of Alloys and Compounds 2004, 384, 231.

[125] 	T.Ohtsuji, T.Akiyama, J.Yagi, Journal of the Japan Institute of Metals 2000, 64, 656.

[126] 	J.A.Puszkiel, P.A.Larochette, F.C.Gennari, Journal of Alloys and Compounds 2008, 463, 134.

[127] 	J.A.Puszkiel, P.A.Larochette, F.C.Gennari, International Journal of Hydrogen Energy 2008, 33, 3555.

[128] 	S.S.S.Raman, D.J.Davidson, J.L.Bobet, O.N.Srivastava, Journal of Alloys and Compounds 2002, 333, 282.

[129] 	P.Selvam, K.Yvon, International Journal of Hydrogen Energy 1991, 16, 615.

[130] 	C.X.Shang, M.Bououdina, Z.X.Guo, Journal of Alloys and Compounds 2003, 356, 626.

[131] 	J.J.Didisheim, P.Zolliker, K.Yvon, P.Fischer, J.Schefer, M.Gubelmann, A.F.Williams, Inorganic Chemistry 1984, 23, 1953.

[132] 	S.V.Halilov, D.J.Singh, M.Gupta, R.Gupta, Physical Review B, 2004,70, 195117.

[133] 	E.Orgaz, M.Gupta, Journal of Physics-Condensed Matter 1993, 5, 6697.

[134] 	E.Ronnebro, Y.Fukai, S.Yamamoto, T.Sakai, Journal of Alloys and Compounds 385 (2004) 276-282 2004, 385, 276.

[135] 	A.C.Larson, R.B.Von Dreele, "General Structure Analysis System (GSAS). Los Alamos National Laboratory Report." 2000.

[136] 	J.P.Perdew, A.K.Burke, International Journal of Quantum Chemistry 1996, 57, 309.

[137] 	J.P.Perdew, K.Burke, M.Ernzerhof, Physical Review Letters 1996, 77, 3865.

[138] 	G.Kresse, J.Furthmnller, Physical Review B 1996, 54, 11169.

[139] 	P.E.Blochl, Physical Review B 1994, 50, 17953.

[140] 	V.E.Antonov, M.Baier, B.Dorner, V.K.Fedotov, G.Grosse, A.I.Kolesnikov, E.G.Ponyatovsky, G.Schneider, F.E.Wagner, Journal of Physics: Condensed Matter 2002, 14, 6427.

[141] 	S.K.Saxena, L.S.Dubrovinsky, P.Haggkvist, Y.Cerenius, G.Shen, H.K.Mao, Science 1995, 269, 1703.

[142] 	M.M.Barsan, J.Moyer, I.S.Butler, D.F.R.Gilson, Journal of Alloys and Compounds 2006, 424, 73.

[143] 	L.M.Lawson Daku, H.Hagemann, Physical Review B 2007, 76, 014118.

[144] 	C.P.Kempter, R.O.Elliott, J.Gschneidner, The Journal of Chemical Physics 1960, 33, 837.

[145] 	S.F.Parker, K.P.J.Williams, M.Bortz, K.Yvon, Inorganic Chemistry 1997, 36, 5218.

[146] 	K.Chlopek, C.Frommen, A.Leon, O.Zabara, M.Fichtner, Journal of Materials Chemistry 2007, 17, 3496.

[147] 	Y.Nakamori, K.Miwa, A.Ninomiya, H.Li, N.Ohba, S.i.Towata, A.Zuttel, S.i.Orimo, Physical Review B 2006, 74, 045126.

[148] 	V.Ozolins, E.H.Majzoub, C.Wolverton, Physical Review Letters 2008, 100, 135501.

[149] 	G.Barkhordarian, T.R.Jensen, S.Doppiu, U.Bosenberg, A.Borgschulte, R.Gremaud, Y.Cerenius, M.Dornheim, T.Klassen, R.Bormann, Journal of Physical Chemistry C 2008, 112, 2743.

[150] 	J.H.Kim, J.H.Shim, Y.W.Cho, Journal of Power Sources 2008, 181, 140.

[151] 	E.Ronnebro, E.H.Majzoub, Journal of Physical Chemistry B 2007, 111, 12045.

[152] 	V.Dmitriev, Y.Filinchuk, D.Chernyshov, A.V.Talyzin, A.Dzwilevski, O.Andersson, B.Sundqvist, Physical Review B 2008, 77, 174112.

[153] 	R.Cerny, Y.Filinchuk, H.Hagemann, K.Yvon, Angewandte Chemie International Edition 2007, 46, 5765.

[154] 	H.W.Li, K.Kikuchi, Y.Nakamori, K.Miwa, S.Towata, S.Orimo, Scripta Materialia 2007, 57, 679.

[155] 	T.Matsunaga, F.Buchter, K.Miwa, S.Towata, S.Orimo, A.Znttel, Renewable Energy 2008, 33, 193.

[156] 	R.A.Varin, C.Chiu, Z.S.Wronski, Journal of Alloys and Compounds 2008, 462, 201.

[157] 	P.Zanella, L.Crociani, N.Masciocchi, G.Giunchi, Inorganic Chemistry 2007, 46, 9039.

[158] 	F.M.Brower, N.E.Matzek, P.F.Reigler, H.W.Rinn, C.B.Roberts, D.L.Schmidt, J.A.Snover, K.Terada, Journal of the American Chemical Society 1976, 98, 2450.

[159] 	G.Lucazeau, Journal of Raman Spectroscopy 2003, 34, 478.

[160] 	K.Miwa, M.Aoki, T.Noritake, N.Ohba, Y.Nakamori, S.Towata, A.Zuttel, S.Orimo, Physical Review B 2006, 74, 155122.

[161] 	M.Aoki, K.Miwa, T.Noritake, N.Ohba, M.Matsumoto, H.W.Li, Y.Nakamori, S.Towata, S.Orimo, Applied Physics A-Materials Science and Processing 2008, 92, 601.

[162] 	Y.S.Lee, Y.Kim, Y.W.Cho, D.Shapiro, C.Wolverton, V.Ozolins, Physical Review B 2009, 79, 104107.

[163] 	E.H.Majzoub, E.Ronnebro, Journal of Physical Chemistry C 2009, 113, 3352.

[164] 	M.D.Riktor, M.H.Sorby, K.Chlopek, M.Fichtner, F.Buchter, A.Zuttel, B.C.Hauback, J. Mater. Chem. 2007, 17, 4939.

[165] 	Z.P.Li, B.H.Liu, K.Arai, K.Asaba, S.Suda, Journal of Power Sources 2004, 126, 28.

[166] 	E.Shafirovich, V.Diakov, A.Varma, International Journal of Hydrogen Energy 2007, 32, 207.

[167] 	P.Fischer, A.Zuttel, European Powder Diffraction Epdic 2004, 443-4, 287.

[168] 	H.L.Johnston, N.C.Hallett, Journal of the American Chemical Society 2002, 75, 1467.

[169] 	B.Sundqvist, O.Andersson, Physical Review B 2006, 73, 1092102.

[170] 	G.Lee, J.Y.Lee, J.S.Kim, Solid State Communications 2006, 139, 516.

[171] 	C.M.Araujo, R.Ahuja, A.V.Talyzin, B.Sundqvist, Physical Review B 2005, 72, 054125.

[172] 	Y.Filinchuk, A.V.Talyzin, D.Chernyshov, V.Dmitriev, Physical Review B 2007, 76, 092104.

[173] 	T.J.Frankcombe, G.J.Kroes, A.Znttel, Chemical Physics Letters 2005, 405, 73.

[174] 	B.Sundqvist, O.Andersson, A.V.Talyzin, Journal of Physics: Condensed Matter 2007, 19, 425201.

[175] 	G.Ouyang, C.Q.Sun, W.G.Zhu, The Journal of Physical Chemistry B 2008, 112, 5027.

[176] 	A.K.Kleppe, A.P.Jephcoat, N.L.Ross, American Mineralogist 2001, 86, 1275.

[177] 	W.G.Fateley, N.T.McDevitt, F.F.Bentley, Applied Spectroscopy 1971, 25, 155.

[178] 	E.Kroumova, M.I.Aroyo, J.M.Perez-Mato, A.Kirov, C.Capillas, S.Ivantchev, H.Wondratschek, Phase Transitions 2003, 76, 155.

[179] 	D.Errandonea, F.J.Manjon, Progress in Materials Science 2008, 53, 711.

[180] 	D.L.Anton, Journal of Alloys and Compounds 2003, 356-357, 400.

[181] 	S.Satyapal, J.Petrovic, C.Read, G.Thomas, G.Ordaz, Catalysis Today 2007, 120, 246.

[182] 	A.Zaluska, L.Zaluski, J.O.Strom-Olsen, Journal of Alloys and Compounds 2000, 298, 125.

[183] 	R.A.Zidan, S.Takara, A.G.Hee, C.M.Jensen, Journal of Alloys and Compounds 1999, 285, 119.

[184] 	R.K.Ahluwalia, International Journal of Hydrogen Energy 2007, 32, 1251.

[185] 	E.C.Ashby, P.Kobetz, Inorganic Chemistry 1966, 5, 1615.

[186] 	M.P.Balogh, G.G.Tibbetts, F.E.Pinkerton, G.P.Meisner, C.H.Olk, Journal of Alloys and Compounds 2003, 350, 136.

[187] 	K.J.Gross, G.J.Thomas, C.M.Jensen, Journal of Alloys and Compounds 2002, 330-332, 683.

[188] 	A.V.Talyzin, B.Sundqvist, High Pressure Research 2006, 26, 165.

[189] 	S.Gomes, G.Renaudin, H.Hagemann, K.Yvon, M.P.Sulic, C.M.Jensen, Journal of Alloys and Compounds 2005, 390, 305.

[190] 	C.M.Jensen, R.Zidan, N.Mariels, A.Hee, C.Hagen, International Journal of Hydrogen Energy 1999, 24, 461.

[191] 	G.P.Meisner, G.G.Tibbetts, F.E.Pinkerton, C.H.Olk, M.P.Balogh, Journal of Alloys and Compounds 2002, 337, 254.

[192] 	R.A.Dunlap, Z.H.Cheng, G.R.MacKay, J.W.O'Brien, D.A.Small, Hyperfine Interactions 2000, 130, 109.

[193] 	J.W.Lauher, D.Dougherty, P.J.Herley, Acta Crystallographica Section B 1979, 35, 1454.

[194] 	E.Husson, C.Proust, P.Gillet, J.P.Itie, Materials Research Bulletin 2009, 34, 2085.

[195] 	S.Klotz, G.Hamel, J.S.Loveday, R.J.Nelmes, M.Guthrie, A.K.Soper, Physical Review Letters 2002, 89, 285502.

[196] 	D.J.Ross, M.D.Halls, A.G.Nazri, R.F.Aroca, Chemical Physics Letters 2004, 388, 430.

[197] 	L.C.Ming, S.R.Shieh, A.Jayaraman, S.K.Sharma, Y.H.Kim, Journal of Physics and Chemistry of Solids 1999, 60, 69.

[198] 	V.Selva, S.R.Kulkarni, S.K.Saxena, H.P.Liermann, S.V.Sinogeikin, Applied Physics Letters 2006, 89, 261901.

[199] 	Z.Wang, Y.Zhao, D.Schiferl, C.S.Zha, R.T.Downs, T.Sekine, Applied Physics Letters 2003, 83, 3174.

[200] 	L.Schlapbach, A.Zuttel, Nature (London) 2001, 414, 353.

[201] 	B.C.Hauback, H.W.Brinks, H.Fjellvag, Journal of Alloys and Compounds 2002, 346, 184.

[202] 	J.P.Bastide, J.C.Bureau, J.M.Letoffe, P.Claudy, Materials Research Bulletin 1987, 22, 185.

[203] 	M.P.Pitt, D.Blanchard, B.C.Hauback, H.Fjellvag, W.G.Marshall, Physical Review B 2005, 72, 214113.

[204] 	S.Wold, K.Esbensen, P.Geladi, Chemometrics and Intelligent Laboratory Systems 1987, 2, 37.

[205] 	M.R.Euerby, P.Petersson, Journal of Chromatography A 2003, 994, 13.

[206] 	K.Heberger, K.Milczewska, A.Voelkel, Colloids and Surfaces A: Physicochemical and Engineering Aspects 2005, 260, 29.

[207] 	E.R.Malinowski, "Factor Analysis in Chemistry",  Wiley NY, 1991.

[208] 	M.Otto, "Chemometrics: Statistics and Computer Application in Analytical Chemistry",  Wiley-VCH, Weinheim, 1999.

[209] 	K.Polat, S.Gnnes, Applied Mathematics and Computation 2007, 186, 898.

[210] 	J.Bajorath, Journal of Chemical Information and Computer Sciences 2001, 41, 233.

[211] 	B.Hess, Physical Review E 2000, 62, 8438.

[212] 	M.Viana, X.Querol, A.Alastuey, J.I.Gil, M.Menendez, Chemosphere 2006, 65, 2411.

[213] 	T.J.Clark, G.R.Whittell, I.Manners, Inorganic Chemistry 2007, 46, 7522.

[214] 	M.Chandra, Q.Xu, Journal of Power Sources 2007, 168, 135.

[215] 	M.E.Bluhm, M.G.Bradley, R.Butterick, U.Kusari, L.G.Sneddon, Journal of the American Chemical Society 2006, 128, 7748.

[216] 	M.C.Denney, V.Pons, T.J.Hebden, D.M.Heinekey, K.I.Goldberg, Journal of the American Chemical Society 2006, 128, 12048.

[217] 	A.Feaver, S.Sepehri, P.Shamberger, A.Stowe, T.Autrey, G.Cao, The Journal of Physical Chemistry B 2007, 111, 7469.

[218] 	J.Baumann, F.Baitalow, G.Wolf, Thermochimica Acta 2005, 430, 9.

[219] 	X.Kang, Z.Fang, Kong, H.Cheng, X.Yao, G.Lu, P.Wang, Advanced Materials 2008, 20, 2756.

[220] 	Z.Xiong, C.K.Yong, G.Wu, P.Chen, W.Shaw, A.Karkamkar, T.Autrey, M.O.Jones, S.R.Johnson, P.P.Edwards, W.I.F.David, Nature Materials 2008, 7, 138.

[221] 	M.Ramzan, F.Silvearv, A.Blomqvist, R.H.Scheicher, S.Lebegue, R.Ahuja, Physical Review B 2009, 79, 132102.

[222] 	T.B.Lee, M.L.McKee, Inorganic Chemistry 2009, 48, 7564.

[223] 	P.Loubeyre, R.Le Toullec, M.Hanfland, L.Ulivi, F.Datchi, D.Hausermann, Physical Review B 1998, 57, 10403.

[224] 	T.Ogitsu, E.Schwegler, F.Gygi, G.Galli, Physical Review Letters 2003, 91, 175502.

[225] 	W.T.Klooster, T.F.Koetzle, P.E.M.Siegbahn, T.B.Richardson, R.H.Crabtree, Journal of the American Chemical Society 1999, 121, 6337.

[226] 	S.Trudel, D.F.R.Gilson, Inorganic Chemistry 2003, 42, 2814.

[227] 	Y.Lin, W.L.Mao, V.Drozd, J.Chen, L.L.Daemen, The Journal of Chemical Physics 2008, 129, 234509.

[228] 	C.Murli, Y.Song, The Journal of Physical Chemistry B 2009, 113, 13509.

[229] 	S.M.Lee, X.D.Kang, P.Wang, H.M.Cheng, Y.H.Lee, Chemphyschem 2009, 10, 1825.

[230] 	N.J.Hess, M.E.Bowden, V.M.Parvanov, C.Mundy, S.M.Kathmann, G.K.Schenter, T.Autrey, The Journal of Chemical Physics 2008, 128, 034508.

[231] 	M.Palumbo, F.J.Torres, J.R.Ares, C.Pisani, J.F.Fernandez, M.Baricco, Calphad 2007, 31, 457.

[232] 	V.Iosub, T.Matsunaga, K.Tange, M.Ishikiriyama, International Journal of Hydrogen Energy 2009, 34, 906.

[233] 	G.Sandrock, J.Reilly, J.Graetz, W.M.Zhou, J.Johnson, J.Wegrzyn, Applied Physics A: Materials Science and Processing 2005, 80, 687.

[234] 	J.Graetz, S.Chaudhuri, Y.Lee, T.Vogt, J.T.Muckerman, J.J.Reilly, Physical Review B 2006, 74, 214114.

[235] 	M.Tkacz, T.Palasyuk, J.Graetz, S.Saxena, Journal of Raman Spectroscopy 2008, 39, 922.

[236] 	M.Tkacz, S.M.Filipek, B.Baranowski, Polish Journal of Chemistry 1984, 57, 651.

[237] 	T.Kelkar, S.Pal, D.G.Kanhere, Chemphyschem 2008, 9, 928.

[238] 	T.Kelkar, D.G.Kanhere, S.Pal, Computational Materials Science 2008, 42, 510.

[239] 	P.Vajeeston, P.Ravindran, A.Kjekshus, H.Fjellvag, Physical Review Letters 2002, 89, 175506.

[240] 	J.F.Stampfer, C.E.Holley, J.F.Suttle, Journal of the American Chemical Society 2002, 82, 3504.

[241] 	M.Bortz, B.Bertheville, G.Bottger, K.Yvon, Journal of Alloys and Compounds 1999, 287, L4-L6.

[242] 	B.Baranowski, H.D.Hochheimer, K.Strossner, W.Honle, Journal of the Less-Common Metals 1985, 113, 341.

[243] 	A.Klaveness, P.Vajeeston, P.Ravindran, H.Fjellvag, A.Kjekshus, Physical Review B 2006, 73, 094122.

[244] 	E.Fuglein, U.Schubert, Chemistry of Materials 1999, 11, 865.

[245] 	A.Belsky, M.Hellenbrandt, V.L.Karen, P.Luksch, Acta Crystallographica Section B 2002, 58, 364.

[246] 	J.van Straaten, I.F.Silvera, Physical Review B 1987, 36, 9301.

[247] 	A.Zuttel, P.Wenger, S.Rentsch, P.Sudan, P.Mauron, C.Emmenegger, Journal of Power Sources 2003, 118, 1.

[248] 	Y.Fukai, "The metal-hydrogen systembasic bulk properties",  1993, Ch. 21.

[249] 	A.El Gridani, R.Drissi El Bouzaidi, M.El Mouhtadi, Journal of Molecular Structure: THEOCHEM 2002, 577, 161.

[250] 	B.Huang, F.Gingl, K.Yvon, J.Rodriguez-Carvajal, Journal of Alloys and Compounds 1995, 227, 131.

[251] 	M.T.Hagstrom, J.P.Vanhanen, P.D.Lund, Journal of Alloys and Compounds 1998, 269, 288.

[252] 	R.K.Kremer, J.K.Cockcroft, H.Mattausch, A.Simon, G.J.Kearley, Journal of Physics: Condensed Matter 1994, 6, 4053.

[253] 	D.Kyoi, T.Sato, E.Ronnebro, N.Kitamura, A.Ueda, M.Ito, S.Katsuyama, S.Hara, D.Noreus, T.Sakai, Journal of Alloys and Compounds 2004, 372, 213.

[254] 	H.Hagemann, S.Gomes, G.Renaudin, K.Yvon, Journal of Alloys and Compounds 2004, 363, 129.

# APPENDIX

# VITA

LYCI GEORGE

EDUCATION AND PROFESSIONAL EXPERIENCE

1997-2000	Bachelor of Science (B.Sc.) in Physics, Mahatma Gandhi University, Kottayam, India

2000-2002	Master of Science (M.Sc.) in Physics, Mahatma Gandhi University, Kottayam, India

2003-2005	Master of Technology (M.Tech.) in Materials Science, Indian Institute of Technology, Kanpur, India

Junior Research Fellow, University Grant Commission (UGC), India

2005-2006		Senior Research Fellow, UGC and Indian Institute of Technology,

Kanpur, India

2006-2010		Research Assistant (2006-2007),

CDAC (Carnegie/ DOE alliance center) student (2007-2008),

Dissertation Evidence Acquisition Fellow (2008-2009) and

Dissertation Year Fellow (2009-2010),

Florida International University,   Miami, FL

PUBLICATIONS AND PRESENTATIONS

- Gajbhiye, N.S., Pandey, P. K., George, L. and Kumar, A. “Characterization of nano structured PZT prepared by chemical routes”, Journal of Nanoscience and Nanotechnology 7 (2007) 1975-1979.

- Gajbhiye, N.S., Pandey, P. K., George, L. and Kumar, A. “Dielectric properties of nanostructured PZT prepared by chemical routes”, Defense Science Journal, 57(2007) 61-68.

- Gajbhiye, N.S., Pandey, P. K., George, L. and Kumar, A.  “Thermal, structural and electrical studies of nanostructured PZT synthesized by low temperature technique”, Thermans (2006) 284-286.

- Gajbhiye, N.S., Pandey, P. K., George, L. and Kumar, A.  “Studies on homogeneous lead zirconate titanate powder synthesized by hydroxide co-precipitation”, Proceedings of the DAE Solid State Physics Symposium (2005) 267-268.

- George, L., Drozd, V., Chen, J, Couvy, H. and Saxena, S. K. “An extended high pressure- temperature phase diagram of NaBH4”, Journal of Chemical Physics 131 (2009) 074505.

- George, L., Drozd, V., Bardaji, E. G., Fichtner, M. and Saxena, S. K. “High pressure investigation on calcium borohydride”, Journal of Physical Chemistry: C 113 (2009) 15087-15090.

- George, L., Drozd, V., Durygin, A., Chen, J.  and Saxena, S. K. “Bulk modulus and thermal expansion of mechano-chemically synthesized Mg2FeH6 from high temperature and high pressure studies” International Journal of Hydrogen Energy 34 (2009) 3410-3416.

- George, L., Drozd, V., Bardaji, E. G., Fichtner, M. and Saxena, S. K.  “Structural phase transitions of Mg(BH4)2 under pressure”, Journal of Physical Chemistry: C 113 (2009) 486-492.

- George, L., Hrubiak, R., Rajan, K. and Saxena, S. K. “Principal component analysis on properties of binary and ternary hydrides and a comparison of metal versus metal hydride properties”, Journal of Alloys and Compounds 478 (2009) 731–735.

- George, L. and Saxena, S. K. “Structural stability of metal hydrides, alanates and borohydrides of alkali and alkali- earth elements: A review”, International Journal of Hydrogen Energy 35 (2010) 5454-5470.

- Hrubiak, R., George, L., Saxena S. K. and Rajan, K. “A materials database for exploring material properties”, Journal of Metals 61(2009) 59-62.

- Vennila, R. S., Drozd, V., George, L. , Saxena, S.K., Liermann, P.,  Liu, H., Stowe, C. A., Berseth, P., Anton D. and Zidan, R. “Structural study of ball-milled sodium alanate under high pressure”, Journal of Alloys and Compounds 473 (2009) 576–578.

Also attended and presented the work at 10 national and international conferences during the dissertation period.